SYNTHESIS AND CHARACTERIZATION OF OXIDE NANOSTRUCTURES

VIA A SOL-GEL ROUTE IN SUPERCRITICAL CO2

(Spine Title: Synthesis and Characterization of Oxide Nanostructures in ScCO2)

(Thesis format: Monograph)

by

#### Ruohong Sui

Graduate Program

in

Engineering Science

Department of Chemical and Biochemical Engineering

A thesis submitted in partial fulfillment

of the requirements for the degree of

Doctor of Philosophy

Faculty of Graduate Studies

The University of Western Ontario

London, Ontario, Canada

( Ruohong Sui    2007

THE UNIVERSITY OF WESTERN ONTARIO

FACULTY OF GRADUATE STUDIES

#### CERTIFICTE OF EXAMINATIONS

| Joint Supervisor ______________________________ Prof. Paul Charpentier Joint-Supervisor ______________________________ Prof. Amin Rizkalla Supervisory Committee ______________________________ Prof. Wankei Wan ______________________________ Prof. Hugo deLasa | Examiners ______________________________ Dr. Keith P. Johnston ______________________________ Dr. Zhifeng Ding ______________________________ Dr. Mita Ray ______________________________ Dr. Argyrios Margaritis |
| --- | --- |

The thesis by

Ruohong Sui

Entitled:

Synthesis and Characterization of Oxide Nanostructures

Via a Sol-Gel Route in Supercritical CO2

is accepted in partial fulfillment of the

requirements for the degree of

Doctor of Philosophy

Date____________________________               _______________________________

Chair of Thesis Examination Board

Abstract and Key Words

Fundamental and applied research on synthesizing oxide nanomaterials in supercritical CO2 (scCO2) is of potential importance to many industrial and scientific areas, such as the environmental, chemistry, energy, and electronics industries. This research has focused on synthesizing silica (SiO2), titania (TiO2) and zirconia (ZrO2) nanostructures via a direct sol-gel process in CO2, although it can be extended to other metal oxides and hybrid materials. The synthesis process was studied by in situ FTIR spectrometry. The resulting nanomaterials were characterized using electron microscopy, N2 physisorption, FTIR, X-ray diffraction and thermal analysis.

Silicon, titanium and zirconium alkoxides were used as precursors due to their relatively high solubility in scCO2. Acetic acid was used as the primary polycondensation agent for polymerization of the alkoxides, not only because it is miscible in scCO2, but also as it is a mild polycondensation agent for forming well-defined nanostructures. The synthesis was carried out in a batch reactor, either in an autoclave connected with the in situ FTIR, or in a view cell with sapphire windows for observation of phase changes. The process was controlled by means of a LabView software through a FieldPoint® interface. The nano spherical particles of SiO2 aerogel with a diameter of ca. 100 nm were obtained by means of rapid expansion of supercritical solution (RESS). TiO2 nanofibers with diameters of ca. 10 ~ 80 nm and nanospheres with a diameter of 20 nm were prepared in the high-pressure vessel by means of controlling the synthesis conditions followed by extraction of organic components using scCO2. The mechanism of fibrous and spherical nanostructure formation was studied using in-situ ATR-FTIR spectrometry. It was found that the nanofibers were formed through polycondensation of a Ti acetate complex that leads to 1-dimensional condensation, while the nanospheres were formed through polycondensation of a Ti acetate complex that leads to 3-dimensional condensation. Using the same method, ZrO2 nanospherical particles with a diameter of ca. 20 nm and mesoporous monoliths were also produced. The reaction rate and product properties were found to be a function of initial concentration of the precursor, the ratio of acid/alkoxides, the temperature, and the pressure. In order to obtain crystalline phases, the as-prepared aerogels were calcined under several different temperatures in the range of 300-600 °C. Anatase and rutile TiO2 nanocrystallites, as well as tetragonal and monoclinic ZrO2 were obtained depending on calcination temperature. The resulting materials exhibited a mesoporous structure and a high surface area.

The in situ ATR-FTIR spectra during the sol-gel process were studied using a chemometrics method. The pure-component spectra of the various reaction ingredients and products were extracted from the overlapped spectra, and the pure-component concentration profiles as well as the precursor conversion curves were subsequently obtained. The concentration-time curves allowed an assessment of the reaction kinetics. The silica alkoxide was found to react with acetic acid gradually to form SiO2, and the reaction was favored by a higher temperature and a lower pressure. The titanium and zirconium alkoxides, however, reacted with acetic acid quickly to form metal acetate complexes, which subsequently grew into metal oxide particles.

ScCO2 was found to be a superior solvent for synthesizing oxide nanomaterials, because of its zero surface tension that maintains the nanostructures and the high surface areas of the nanomaterials. Acetic acid was an excellent polycondensation agent for synthesizing SiO2, TiO2 and ZrO2 nanomaterials, because of the formation of Si, Ti and Zr acetate coordination compounds that can be stabilized in CO2. Stabilization of the colloidal particles in CO2 was studied using both the ATR-FTIR and solubility parameter approaches. According to the ATR-FTIR study, the interaction between CO2 molecules and the metal-bridging acetate is featured by Lewis-acid and Lewis-base interactions, which facilitates solubility. The solubility parameter calculation results showed that the acetate group decreases the solubility parameters of the macromolecules, improving solubility in CO2.

This research showed that the direct sol-gel process in CO2 is a promising technique for synthesizing SiO2, TiO2 and ZrO2 materials with high surface areas and various nanoarchitectures.

Key Words: SiO2 nanospheres, TiO2 nanofibers, TiO2 nanospheres, ZrO2 nanospheres, mesoporous ZrO2 monolith, aerogel, sol-gel, supercritical CO2, metal alkoxides, carboxylic acid, acetic acid, ATR-FTIR, chemometrics, SIMPLISMA modeling, self-assembly, LA-LB interaction.

Dedication

To my dearest wife and daughters:

Jingyan, Gayle and Florrie.

Acknowledgements

First and foremost, I would like to thank my mother, Qingjie, and my father, Qinglu Sui, for the guidance when I got lost and the freedom when we have different opinions. To my wife, Jingyan, and daughters, Gayle and Florrie, for their sacrifice of my presence at home for five years and their support of my study thousands of miles away. I cannot thank my wife enough for my whole life for all her understanding and hard work and taking care of my whole family.

I am grateful to my supervisors, Professor Paul Charpentier and Amin Rizkalla, for their continuous guidance throughout my PhD study at Western. I would like to thank Professor Wankei Wan and Hugo DeLasa, for their kind help during my research.

I would like to express my sincere gratitude to Mr. Fred Pearson of the Brockhouse Institute for Materials Research, McMaster University, and Mr. Ron Smith of the Biology Department, UWO, for training me on the HRTEM and TEM, many thanks go to Dr. Todd Simpson of the Nanotech Laboratory, and Mr. Kobe Brad of the Surface Science Western for their help on SEM, and to Ms. Tatiana Karamaneva for her help in XRD analysis.

I would like to express my passion to all the colleagues in my group: to Ming Jia for his kind orientation of the campus and his contribution to the high-pressure appliances, to Yousef Bakhbakhi and Xinsheng Li for their sharing their knowledge of ATR-FTIR, to SM Zahangir Khaled and Ms. Behnez Hojjati for their cooperation on synthesis of the nanocomposites, to William Xu for helping me with Matlab, and to Ms. Rahima Lucky, Jeff Wood, Shawn Dodds, Kevin Burgess, Muhammad Chowdhury, Niraj Pancha and Colin Ho for their friendship and help.

I would like to thank Professor Keith Johnston of University of Texas (Austin) for his time of reading of my thesis and the corrections he made, although he could not attend the tele-examination as the external examiner due to the flood in Austin, Texas.

I would like to thank OGS scholarship and the financial funding from the Canadian Natural Science and Engineering Research Council (NSERC) and the Materials and Manufacturing Ontario EMK program.

Table of Contents

Title Page ………………………………………………………………………………….i

Certificate of Examination ………………………………………………………………..ii

Abstract and Key Words	iii

Dedication	vi

Acknowledgements	vii

Table of Contents	ix

List of Tables	xivv

List of Figures	xv

List of Appendices	xxvii

List of Abbreviations, Symbols, Nomenclature	xxviii

Chapter 1. Introduction	1

1.1. Overview	2

1.2. Motivation of the Research	2

1.3. Potential Applications of Oxide Nanomaterials	3

1.4. Methodology of Synthesizing Oxide Nanomaterials	4

1.5. Supercritical Fluids and Supercritical Carbon Dioxide	7

1.5.1. Supercritical Fluids (SCFs)	7

1.5.2. Particle Formation in SCFs	10

1.5.3. Chemical Reactions in SCFs	12

1.5.4. Commercial Implementation of SCFs	14

1.5.5. ScCO2	14

1.6. Sol-Gel Synthesis and Aerogel	15

1.6.1. Sol-Gel Technique and Aerogel	15

1.6.2. Conventional Method of Aerogel Synthesis	16

1.6.3. Direct Synthesis of Aerogel via a Sol-Gel Route in SCFs	18

Chapter 2. Direct Sol-Gel Process in SCF: A Review	19

2.1. Overview	20

2.2. Supercritical and Subcritical Water or Alcohol	21

2.3. Direct Sol-Gel Process in CO2	25

2.3.1. Surfactant-Assisted Hydrolysis	25

2.3.2. Hydrolysis without Surfactant	27

2.3.3. Carboxylic Acids as Polycondensation Agents	29

2.4. Summary	29

Chapter 3. Materials and Methods	31

3.1. Outline	32

3. 2. Synthesis Setup	32

3.2.1. View Cell, Pump, Valves and Connections	32

3.2.2. View cell with LabView VI control	34

3.2.3. Instrumentation	35

3.2.4. Temperature Controller	37

3.2.5. Reactor Equipped with In situ FTIR	37

3.3. Synthesis Procedures	39

3. 4. Characterization Methods	40

3.4.1. Online FTIR	40

3.4.2. Electron Microscopy	42

3.4.3. Crystals and Powder X-Ray Diffraction	45

3.4.4. N2 Adsorption/Desorption	47

3.4.5. Thermal Analysis	52

Chapter 4. Synthesis and Characterization of Silica Aerogel Particles	54

4.1. Introduction	55

4.2. Experimental Details	57

4.3. Results and Discussion	59

4.3.1. In situ FTIR Analysis of the Sol-gel Reactions.	59

4.3.2. Activity of Various Acids	61

4.3.3. Effect of Temperature and Pressure	63

4.3.4. Experimental Phase Behavior	65

4.3.5. Particle Formation	66

4.4. Conclusions	67

Chapter 5. Synthesis and Characterization of Titania Nanofibers and Nanospheres	69

5.1. Introduction	71

5.1.1. Applications of TiO2 Aerogel and TiO2 Nanomaterials	71

5.1.2. TiO2 Synthesis Method	71

5.1.3. Ti-Carboxylate Complex	72

5.2. Experimental Details	75

5.2.1. Materials	75

5.2.2. Experimental Setup	75

5.2.3. Preparation of TiO2 Nanoparticles	75

5.2.4. Characterization	77

5.3. Results and Discussion	78

5.3.1. N2 Adsorption/Desorption	79

5.3.2. SEM	84

5.3.3. TEM	92

5.3.4. Thermal Analysis	94

5.3.5. XRD	97

5.3.6. Spheres or Fibers?	100

5.3.7. CO2’s Effect on the formation of TiO2 Microstructures	109

5.4. Conclusion.	110

Chapter 6. Synthesis and Characterization of ZrO2 Nanoarchitectures	111

6.1. Introduction	112

6.2. Experimental Details	114

6.3. Results and Discussion.	116

6.4. Conclusion	130

Chapter 7. Kinetics Study on Direct Sol-Gel Reactions in CO2 by Using In Situ ATR-FTIR Spectrometry	132

7.1. Introduction	133

7.2. Experimental	138

7.3. Results and Discussion	139

7.3.1. Conversion of TEOS	139

7.3.2. Concentration Profiles of Ti-Acetate and TiO2 Aerogels	146

7.3.3. Concentration Profiles of Zr-Acetate and ZrO2 Aerogels	154

7.4. Conclusion	158

Chapter 8. Stabilization of the Colloidal Particles in CO2	160

8.1. Introduction	161

8.2. Experimental	164

8.3. Results and Discussion	165

8.3.1. FTIR Spectroscopy and LA-LB interaction	165

8.3.2. Solubility Parameter Study	173

8.4. Conclusion	178

Chapter 9. Summary and Conclusions	180

9.1. Outline	181

9.2. Synthesis, Characterization and Mechanism Studies	182

9.3. Chemistry of the Direct Sol-gel Process in CO2	183

9.4. The Synthesis Parameters of Direct Sol-Gel Process in CO2	184

9.5. Future Work Recommendation	184

Bibliography	186

Appendices	206

Curriculum Vitae	229

List of Tables

Table 1.1.  The selected viscosities and densities of CO2 in vapor, liquid and supercritical phases.59, 60	8

Table 1.2. Critical properties for selected supercritical fluids in chemical reactions57	10

Table 3.1. Crystallographic data for rutile and anatase.	46

Table 5.1. IR absorption peaks corresponding to COO-1 stretching vibration in various acetates.	74

Table 5.2. Results of the reaction of TBO with acetic acid in CO2.	80

Table 6.1. Synthesis conditions of ZrO2 structures in CO2 and characterization results.	118

Table 8.1.  Solubility parameters of scCO2 under selected temperatures and pressures. 300, 303	174

Table 8.2. The thermodynamic properties and the average solubility parameters of the alkoxides.	175

Table 8.3. The related atomic and group contributions to the energy of vaporization and mole volume at 25 °C.305	176

Table 8.4. Solubility parameters of the macromolecules calculated using the group contribution method.	177

List of Figures

Figure 1.1. Schematic: the phase diagram of a typical material.	7

Figure 1.2.  Surface tension of saturation liquid CO2 vs. pressure.  The data points were labeled with the corresponding saturation temperatures at the specific pressures.  In the supercritical region, the surface tension is zero.60	9

Figure 1.3. Flow chart of conventional sol-gel route.	17

Figure 1.4. Mechanisms of hydrolysis and condensation of metal alkoxides.105	18

Figure 3.1. The view cell.	33

Figure 3.2. Schematic of experimental setup: (A) computer with LabView Virtual Instrument, (B) FieldPoint by National Instruments, (C) temperature controller, (D) thermocouple, (E) pressure transducer (F) stainless steel view cell equipped with sapphire windows, (G) pneumatic control valve, (H) needle valve, (I) check valve, (J) syringe pump, (K) CO2 cylinder.	35

Figure 3.3. The Front Panel of Pressure Control. A: switch for automatic or manual control; B: pressure cylinder indicator; C: pneumatic valve open-close indicator; D: pneumatic valve; E: read error out; F: write error out; G: pressure setpoint; H: setpoint and real pressure indicator; I: PID tuning parameters; J: stop button.	36

Figure 3.4. Schematic of experimental setup: autoclave with online FTIR and GC-MS. (A) computer; (B) FTIR; (C) temperature and RPM controller with pressure display; (D) 100 ml autoclave equipped with diamond IR probe; (E) needle valves; (F) check valves; (G) syringe pump; (H) container for carboxylic acid; (I) CO2 cylinder.	38

Figure 3.5. Schematic of particle collection vessel for the RESS process.	39

Figure 3.6. Schematic of the reactor with the ATR-FTIR probe assembly.	41

Figure 3.7. Schematic of the DicompTM probe.  Infrared radiation is reflected into the chemically resistant ATR disk that is in contact with the reaction mixture.  The drawing is adapted from ASI.	42

Figure 3.8. Schematic: interactions of a specimen with incident electrons (redrawn from Ref. 154).	43

Figure 3.9. Schematic of a unit cell of crystals.158	45

Figure 3.10. Schematic of X-ray reflection on the crystal planes.	47

Figure 3.11.  BET plot of N2 adsorption on silica gel at 91 K. The data was obtained from Ref. 161	49

Figure 3.12. Classification of hysteresis loops as recommended by the IUPAC.164	51

Figure 3.13. A schematic DSC curve demonstrating the appearance of glass transition, crystallization and melting.	53

Figure 4.1. ATR-FTIR plot of the progress of an aerogel reaction in CO2, where the lines are experimental data: 4.4 mmol TEOS + 22 mmol HOAc + 4.4 mmol H2O at 3000 psig and 60 C from 1 to 7 h at 1-h intervals.	60

Figure 4.2. FTIR spectrum of the SiO2 aerogel powder, there are three obvious absorptions (1065, 928 and 797cm-1) in the range between 4000 and 600 cm-1 (The small absorptions at 3294 and 1709 cm-1 are due to water and acetic acid residue respectively).	61

Figure 4.3. Effect of acid type on TEOS condensation activity in CO2. The points are experimental data from the ATR-FTIR absorbance at 1066 cm-1 (n = 3). The experimental conditions are 60 °C and 3000 psig, 0.044 M TEOS, 0.176 M acid, and 2.75 M acetone.	62

Figure 4.4. Effect of water and acid concentration on TEOS condensation activity in CO2. The points are experimental data from the ATR-FTIR absorbance at 1066 cm-1 (n = 3). Series 1 (♦) : 0.088 M TEOS + 0.352 M HOAc; Series 2 (■): 0.088 M TEOS + 0.352 M HOAc + 0.088 M H2O; Series 3 (▲): 0.088 M TEOS + 0.704 M HOAc. The experimental conditions are 50 °C and 3000 psig.	63

Figure 4.5. Effect of temperature on TEOS condensation activity in CO2. The points are experimental data from the ATR-FTIR absorbance at 1066 cm-1 (n = 3). The experimental conditions are 3000 psig, 0.088 M TEOS, and 0.352 M acetic acid.	64

Figure 4.6. Effect of pressure on TEOS condensation activity in CO2. The points are experimental data from the ATR-FTIR absorbance at 1066 cm-1 (n = 3). The experimental conditions are 50 °C, 0.088 M TEOS, and 0.352 M acetic acid.	65

Figure 4.7. SEM of SiO2 aerogel powder. The experimental conditions are: (a) 1.1 mmol TEOS + 7.7 mmol 96% HCOOH in the 25-mL view cell, at 40 °C and 2000 psig; (b) 0.176 mmol TEOS + 2.64 mmol 96% HCOOH in the 25-mL view cell, at 40 °C and 2000 psig.	66

Figure 4.8. SEM of SiO2 aerogel powder: (a) collected from the high pressure mixer upon decompression. The experimental conditions are 0.044 M TEOS + 0.176 M HOAc, at 60 °C and 3000 psig; (b) collected using the Rapid Expansion of Supercritical Solutions (RESS) process. The experimental conditions are 0.044 M TEOS + 0.176 M HOAc, at 60 °C and 6000 psig.	67

Figure 5.1. Reported structures of TA oligomers with acetate ligands: (a) chelating bidentate; (b) bridging bidentate; (c) monodentate; (d) Ti6O4(OBun)8(OAc)8, rutilane shape; (e) Ti6O6(OPri)6(OAc)6, hexaprismane shape.   (a) ~ (c), Ref.229; (d) and (e) images were modified from Ref.231. The black balls stand for Carbon, the red ones stand for Oxygen, Titanium is in the middle of the octahedrons.	74

Figure 5.2. Photographs following the reaction in the view cell: (a) start of the reaction; (b) the moment directly proceeding gel-formation.	76

Figure 5.3. Photographs: (a) the low-density monolith, and (b) the cracked high-density monoliths.	78

Figure 5.4. Isotherms of TiO2-1 high-density monolith: (a) as-prepared and calcined at (b) 380 °C, (c) 500 °C, and (d) 600 °C.	83

Figure 5.5. Isotherm: TiO2-13 low-density monolith. (a) as-prepared and calcined at (b) 380 °C, (c) 500 °C, and (d) 600 °C.	84

Figure 5.6. SEM: (a) TiO2-1 monolith at low magnification, and (b) at high magnification. The sample was calcined at 500 °C. The arrows indicate where the mesopores are present.	87

Figure 5.7. SEM of as-prepared TiO2-11 monolith at increasing magnification: (a) 50 times; (b) 100 times; (c) 1,000 times and (d) 10,000 times. The arrow indicates where the macropores are present.	88

Figure 5.8. SEM: (a) as-prepared TiO2-11; (b) TiO2-11 calcined at 380 °C (the sample was coated with gold to prevent charging); (c) TiO2-13 nanofiber clusters under a low magnification; and (d) TiO2-13 nanofiber clusters under a high magnification.	89

Figure 5.9. SEM: (a) TiO2-18 nanofibers with a diameter of 40 nm, calcined at 380 °C; (b) TiO2-17 curled nanofibers, calcined at 380 °C.	90

Figure 5.10. SEM. The TiO2-10 rods calcined at 380 °C: (a) at a low magnification, and (b) at a high magnification.	90

Figure 5.11. SEM. The result of scCO2 drying before the complete condensation.	91

Figure 5.12. TiO2 synthesized in isopropanol. The synthesis condition: the initial concentration of TIP = 1.1 mol/L, HOAc/alkoxide molar ratio = 5.5, 60 (C. Scale bar: 200 nm.	91

Figure 5.13. TiO2-1 nano spherical particles calcined at 380 °C: (a) TEM and  (b) HRTEM.	92

Figure 5.14. TEM and HRTEM images: (a) TiO2-11 nanofibers calcined at 380 °C; (b) TEM of TiO2-13 nanofibers calcined at 380 °C; (c) HRTEM of TiO2-13 nanofibers calcined at 380 °C; and (d) TEM of TiO2-18 nanofibers calcined at 380 °C.	93

Figure 5.15. DSC of TiO2-1, -2, -3, -4 aerogels synthesized at 6000 psig and different temperature (a) 40 °C; (b) 50 °C; (c) 60 °C; (d) 70 °C. The initial concentration of TBO: 1.48 mol/L, acetic acid/HOAc: 4.15.	95

Figure 5.16. TGA of as-prepared TiO2-11.	96

Figure 5.17. XRD: amorphous, anatase (a) and rutile (r) phases of the TiO2 mono spherical particles calcined at different temperatures. (A). TiO2-4 synthesized at 70 °C calcined at 300 °C; (B) TiO2-3 synthesized at 60 °C and calcined at 300 °C (B), 380 °C (C), 500 °C (D) and 600 °C (E). The initial concentration of TBO: 1.5 mol/L, acetic acid/HOAc: 4.12, pressure: 6000 psig.	97

Figure 5.18. XRD: nanocrystalline TiO2-11, r: rutile, a: anatase (A) as-prepared TiO2-a aerogel, and calcined at (B) 380 °C, (C) 500 °C (D) 600 °C (E) 800 °C.	99

Figure 5.19. XRD: nanocrystalline TiO2-13, r: rutile, a: anatase (A) calcined at 380 °C, (B) 500 °C (C) 600 °C.	100

Figure 5.20. Powder ATR-FTIR spectra of TiO2-1 nanospherical particles. (A) as-prepared, (B) calcined at 200 °C, (C) calcined at 300 °C, (D) calcined at 400 °C of TiO2-1.	101

Figure 5.21. (a) IR spectrum of TIP. (b) ~ (e) in situ FTIR spectra of polymerization of TIP with acetic acid, at 60 °C and 4500 psig, initial concentration: TIP=1.1 mol/L, HOAc/TIP=5.5 (mol/mol). Reaction time: (b) 10 min; (c) 230 min; (d) 250 min; (e) 4320 min.	103

Figure 5.22. (a) FTIR spectrum of complex 2 synthesized in CO2. The infrared spectrum was recorded on a Bruker Vector 22 FTIR instrument. The crystals were dispersed in a KBr tablet.  (b). In situ FTIR spectrum of polymerization of TIP with acetic acid, at 60 °C and 4500 psig, initial concentration: TIP=1.1 mol/L, HOAc/TIP=3.5 (mol/mol).	104

Figure 5.23. (a) IR spectrum of TBO. (b) to (e) in situ FTIR spectra of polymerization of TBO with acetic acid, at 60 °C and 4500 psig, initial concentration: TBO=1.5 mol/L, HOAc/TBO=5.0 (mol/mol). Reaction time: (b) 10 min; (c) 100 min; (d) 1280 min; (e) 5840 min.	105

Figure 5.24. In situ FTIR spectra of polymerization of TBO with acetic acid, at 60 °C and 4500 psig, initial concentration: TBO=1.1 mol/L, HOAc/TBO=5.5 (mol/mol). Reaction time: (a) 10 min; (b) 100 min; (c) 300 min; (d) 330 min; (e) 5800 min.	106

Figure 5.25. Schematic of the skeletal arrangements of complex 2 (R= Pri) (a) and complex 1 (R= Bun) and 3 (R= Pri)  (b). In the scheme, all acetate groups, some of the oxo bonds, and two bridging OR groups are omitted to make the structure simpler.	107

Figure 5.26. Schematic of nanostructure formation.  Polycondensation of complex 2 or 1 led to formation of either straight or irregular-shape macromolecules. Coacervates and tactoids were formed to lower the energy of the macromolecules in CO2, which in turn resulted in the formation of either fibers or spheres.105	108

Figure 6.1. (a) The homogeneous transparent phase at the initial stage of the reaction; (b) the formation of the opaque white phase; (c) the formation of the transparent gel in the view cell.	116

Figure 6.2. SEM and TEM images.  The translucent monolith of ZrO2-2-400: (a) SEM and (b) TEM. The translucent monolith of ZrO2-2-400: (a) SEM and (b) HRTEM.	120

Figure 6.3. SEM. Precipitate chunks of ZrO2-7.	121

Figure 6.4.  Isotherms of the ZrO2 as-prepared and calcined samples at 500 °C: (a) ZiO2-2; (b) ZrO2-4. See Table 5.1 for the synthesis conditions for ZrO2-2 and -4.	122

Figure 6.5. BJH desorption pore-size-distributions of the as-prepared and calcined at 500 °C: (a) ZrO2-2; (b) ZrO2-4.  See Table 5.1 for the synthesis conditions for ZrO2-2 and -4.	123

Figure 6.6. DSC: (a) as-prepared ZrO2-2, T1: 132 °C; T2: 332 °C; T3: 464 °C; T4: 520 °C; (b) as-prepared ZrO2-4, T5: 328 °C, T6: 467 °C. See Table 5.1 for the synthesis conditions for ZrO2-2 and -4. Inset: TGA of the as-prepared ZrO2-2.	125

Figure 6.7. XRD patterns: (a) the translucent ZrO2-2 calcined at 400 and 500 °C;  (b) the opaque ZrO2-4 calcined at 400 and 500 °C. Note: (t): the tetragonal and/or cubic Zirconium Oxide; (m): the monoclinic Zirconium Oxide.	126

Figure 6.8. ATR-FTIR: ZrO2-2 monolith as-prepared (a) and calcined at (b) 200 °C, (c) 300 °C, (d) 400 °C and (e) 500 °C.	127

Figure 6.9. (a) FTIR spectrum of 70 % zirconium propoxide in propanol; in situ FTIR spectra in CO2:  (b) at the reaction time of 10 min.; (c) 70 min.; (d) 130 min. (e) and 250 min. reaction condition: 40 °C and 5000 psig, initial concentration of ZPO = 1.13 mol/L, HOAc/ZPO = 2.23 (mol/mol).	129

Figure 7.1. Three-dimensional in situ FTIR spectra: 0.088 M TEOS reacting with 0.362M HOAc in CO2 at reaction times of 0-360 minutes and at 50 ºC and 3000 psig.	140

Figure 7.2. In situ FTIR spectra of 0.088 M TEOS reacting with 0.362M HOAc in CO2 at reaction time of 0-360 minutes and at 50 ºC and 3000 psig.	141

Figure 7.3. Comparison of the self-modeling resolved spectra with (a) TEOS and (b) SiO2 aerogel spectra. The spectra of TEOS in (a) and SiO2 in (b) were experimentally collected by means of ATR-FTIR.	143

Figure 7.4. The relative concentration profiles obtained from the self-modeling method. The source IR data was obtained at 50 °C and 3000 psig, and the initial concentrations of TEOS and acetic acid was 0.088 and 0.362 M, respectively.	144

Figure 7.5. Temperature’s effect on the precursor conversion within a reaction time of 0-360 minutes. The initial concentration of TEOS and acetic acid was 0.088 and 0.362 M, respectively, and the pressure was 3000 psig.	145

Figure 7.6. Pressure’s effect on the precursor conversion within a reaction time of 0-360 minutes. The initial concentration of TEOS and acetic acid was 0.088 and 0.362 M, respectively, and the temperature was 50 °C.	145

Figure 7.7.  The three-dimensional in-situ FTIR spectra of 1.10 M TIP reacting with 3.85 M HOAc within a reaction time from 10 to 3720 minutes in CO2. The reaction temperature and pressure were 60 ºC and 4500 psig, respectively.	147

Figure 7.8. In situ FTIR spectra of 1.10 M TIP reacting with 3.85 M HOAc in CO2 within a reaction time from 10 to 3720 minutes, at 60 ºC and 4500 psig. The arrows show the absorbance change trend.	148

Figure 7.9.  FTIR. (a) The black curve is one of the resolved spectra from in situ IR and the curve-fitting results, the residual sum of squares: 4.02E-8; (b) and (c): the spectra of single crystals of 2 and 3, respectively. Note: the black curves = experimental or resolved IR spectra; the pink curve = the fitting curve; blue curves = the individual Gaussian function curves; and the red curve = the residual curve. The number 2 and 3 denote Ti6O6(OPri)6(OAc)6 and Ti6O4(OPri)8(OAc)8, respectively.	149

Figure 7.10.  (a) The other resolved spectrum from the in situ IR spectra, which is attributed to the aerogel product, and (b) TiO2 aerogel spectrum.	150

Figure 7.11. The relative concentration profiles during TIP reacting with HOAc in CO2 within a reaction time from 10 to 3720 minutes, at 4500 psig and 60 ºC; the initial concentration of TIP and HOAc was 1.10 and 3.85 M, respectively.	151

Figure 7.12. The relative concentration profiles during TIP reacting with HOAc in CO2 within a reaction time from 10 to 610 minutes, at 4500 psig and 60 ºC; the initial concentration of TIP and HOAc was 1.10 and 6.05 M, respectively.	152

Figure 7.13.   Three-dimensional in situ FTIR spectra during the direct sol-gel process of ZBO with acetic acid within a reaction time of 10-1330 minutes, at 40 °C and 4500 psig. The initial concentration of ZBO and acetic acid was 0.547 and 1.76 M, respectively.	155

Figure 7.14.  Two-dimensional in situ FTIR spectra during the direct sol-gel processing of ZBO with acetic acid within a reaction time of 10-1330 minutes, at 40 °C and 4500 psig. The initial concentration of ZBO and acetic acid was 0.547 and 1.76 M, respectively. The arrows indicate the absorbance change trend.	156

Figure 7.15.  Two resolved spectra from the in situ IR spectra by means of SIMPLISMA modeling. One spectrum is attributed to the Zr-acetate complex and the other to the ZrO2 aerogel.	157

Figure 7.16.  The relative concentration profiles of Zr-acetate complex and the condensation product during the direct sol-gel processing of ZBO with acetic acid in scCO2 with a reaction time of 10-1330 minutes, at 40 °C and 4500 psig. The initial concentration of ZBO and acetic acid was 0.547 and 1.76 M, respectively.	157

Figure 8.1. In situ IR spectra: (a) 1.3 M TMOS reacting with 5.3 M HOAc in CO2 at a reaction time of 360 minutes, at 50 °C and 4000 psig; (b) 1.10 M TIP reacting with 3.85 M HOAc in CO2 at a reaction time 40 minutes, at 60 °C and 4500 psig; and (c) 0.547 ZBO reacting with 1.76 M HOAc in CO2 at a reaction time of 40 minutes, at 40 °C and 4500 psig.	162

Figure 8.2. Schematic drawing of possible LA-LB interactions between CO2 and (a) the bridging acetate bidentate, (b) the chelating acetate bidentate, and (c) the acetate monodentate.  M: Si, Ti or Zr.	163

Figure 8.3. Schematic drawing of ATR-FTIR analysis. The aerogel powder was pressed against the diamond mirror to obtain higher absorbance peaks.	165

Figure 8.4. The ATR-FTIR spectra of (a) a-TiO2-A, (b) a-TiO2-B and (c) a-ZrO2 before addition of CO2 (black) and at one minute after venting of CO2 (red).	167

Figure 8.5.  The IR spectra and the curve-fitting results of CO2 interacting with (a) a-TiO2-A, the residual sum of squares: 3.86E-3; (b) a-TiO2-B, the residual sum of squares: 4.01E-4; and (c) a-ZrO2, the residual sum of squares: 1.81E-3. Note: the black curves = experimental spectra; the pink curve = the fitting curve; blue curves = the individual Gaussian function curves; and the red curve = the residual curve.	169

Figure 8.6.  Schematic of possible association modes of LA-LB interaction between CO2 and metal bridging acetate. (a) d-p orbital overlap between metal (M) and acetate, and CO2 associates with the π bond either in a vertical or a parallel mode; (b) the partial positive carbon CO2 associates with the lone pairs of oxygen either in T-shape or bended T-shape.	171

Figure 8.7.  The bending and stretching vibrations of a free CO2 molecule.  The two bending vibrations absorb at the same frequency of IR beam due to the symmetry of the CO2 molecule.	171

Figure 8.8.  IR spectra of CO2 impregnated into (a) a-TiO2-A, (b) a-TiO2-B and (c) a-ZrO2 in the ν3 stretching mode region, at one minute after venting of CO2; (d) CO2 impregnated into a-TiO2-A at five minutes after venting of CO2.	172

List of Appendices

Appendix 1. American Chemical Society’s Policy on Theses and Dissertations….…..207

Appendix 2. Copyright Permissions of Acta Crystallography Journals…………….….209

Appendix 3. Physical Properties of the Raw Materials Used in This Thesis…….…….210

Appendix 4. Powder XRD Analysis Conditions……………………………………..…211

Appendix 5. N2 Physisorption Analysis Conditions……………………………………212

Appendix 6. Block Panel of LabView Vis……………………………………………...218

Appendix 7. Instrumentation and Configuration of the Temperature and Pressure Control

………………………………………………………………………………………….219

Appendix 8. Synthesis and Characterization of the Ti-Acetate Single Crystals……….220

Appendix 9. Description of the SIMPLISMA Modeling……………………………….222

Appendix 10. Statistical Results of the SIMPLISMA Modeling……………………….225

Appendix 11. Calculation of Solubility Parameters Using Group Contribution Method

…………………………………………………………………………………………..227

List of Abbreviations, Symbols, Nomenclature

Abbreviations:

Abs: absorbance

ATR-FTIR: attenuate total reflection Fourier transform infrared spectroscopy

BET: Brunauer-Emmett-Teller

DSC: differential scanning calorimeter

FTIR: Fourier transform infrared spectroscopy

HOAc: acetic acid

LA-LB: Lewis acid and Lewis base

NMR: nuclear magnetic resonance

ScCO2: supercritical CO2

ScH2O: supercritical H2O

SEM: scanning electron microscopy

SIMPLISMA: Simple-to-use interactive self-modeling mixture analysis

SMCR: self-modeling curve resolution

TA: titanium alkoxide

TBO: titanium(IV) n-butoxide

TEM: transmission electron microscopy

TEOS: tetraethyl orthosilicate

TMOS: tetramethyl orthosilicate

TGA: thermogravimetric analysis

TIP: titanium(IV) iso-propoxide

TMOS: tetramethyl orthosilicate

XRD: X-ray diffraction

ZBO: zirconium(IV) butoxide

ZPO: zirconium(IV) propoxide

Symbols:

1: Ti6O4(OBun)8(OAc)8

2: Ti6O6(OPri)6(OAc)6

3: Ti6O4(OPri)8(OAc)8

: integrated intensity of rutile

: integrated intensity of anatase

B: pure component matrix

bij: element of pure component matrix

C: concentration coefficient matrix

C0: initial concentration

Ct: concentration at reaction time t

cij: element of concentration coefficient matrix

D: in situ FTIR matrix

dij: element of in situ FTIR matrix

Dpore: adsorption average pore diameter

Dscher: crystallite size

Ecoh: cohesive energy density

Ea: activation energy

k: reaction rate constant

Pc: critical pressure

Pre: reaction pressure

R: universal gas constant

Sbet: Brunauer-Emmett-Teller (BET) surface area

Tc: critical temperature

Tre: reaction temperature

V: molar volume

Vc: critical volume

Vpore: pore volume per gram

: weight fraction of rutile

α: offset for SIMPLISM modeling

β: half-width at half-height of the diffraction peak

δ: solubility parameter

: solubility parameter of supercritical fluid

Δei: energy of vaporization

Δeir: energy of vaporization of repeating unit

: reaction standard enthalpy

(EV: energy change upon isothermal vaporization

(HV: enthalpy change during vaporization

Δυ‡: activation volume

Δυi: mole volume

Δυir: mole volume of repeating unit

θ: half the angle of diffraction

λ: X-ray wavelength

: reduced density of supercritical fluid

: reduced density of liquid at its normal boiling point

# Introduction

## 1.1. Overview

This thesis is focused on developing a new sol-gel route for synthesizing oxide nanomaterials with various morphologies, i.e. nanofibers, nanospheres, and mesoporous architectures in CO2. In the new sol-gel route, carboxylic acids are used for polycondensation of metal alkoxides. Fundamental studies on the synthetic process and resulting materials were carried out using in situ FTIR, N2 physisorption, X-ray diffraction, electron microscopy, and thermal analysis.

In this chapter, the motivation of the research and the potential applications of the synthesized nanomaterials are addressed. Also, the methodologies for synthesizing nanomaterials, especially the sol-gel process and supercritical fluid techniques, are introduced.

## 1.2. Motivation of the Research

The scientific and industrial demand for oxide nanomaterials with desirable morphologies has increased significantly in recent years. As a result, tremendous work has been performed in synthesizing the oxide nanomaterials on both the laboratory and industrial scales.1, 2 Also, concerning human health and the environment, chemical engineers are seeking methodologies for producing nanomaterials in a green and sustainable manner with a low cost.3

The purpose of this research was to develop an inexpensive, environmental friendly, and easy-to-scaleup method for synthesizing oxide nanomaterials with desired morphology, i.e., nanofibers, nanospheres and mesoporous material.

## 1.3. Potential Applications of Oxide Nanomaterials

An oxide is a compound containing oxygen atom(s) and another element. When the other element is electropositive such as a metal atom, the oxides tend to be basic; when the other element is electronegative such as a non-metal atom, the oxides tend to be acidic. Some oxides such as aluminum and zirconium oxides act as both an acid and a base.4

In the oxide family, SiO2, TiO2 and ZrO2 nanoparticles have attracted significant attention in recent years due to their interesting electrical,5 optical,6 magnetic properties and applications for catalysis,7 energy conversion,8 biomedical applications,9 functionalized hybrid materials,10 and nanocomposites.11, 12

Specifically, because of the high-temperature stability, biocompatibility, and metal-oxide-semiconductive properties, SiO2 nanomaterials have many potential applications. For instance, SiO2 nanomaterials can be used as catalyst supports where a metal such as Pt is combined onto SiO2,13, 14 as inorganic fillers for SiO2/polymer nanocomposites where the SiO2 strengthens the polymer composites,15, 16 as nanosized biosensors where SiO2 core-Au shell nanoparticles can be tested at visible wavelength,17, 18 and as a drug capsule where the bioactive molecules are encapsulated in the SiO2 particles.19

Because of its semiconductivity, photoelectrical and photochemical activity under UV light and opacity under X-rays,20 TiO2 nanomaterials can be used as dye-sensitized solar cells (DSSC)21, 22 and photoelectrochemical cells (PEC),23 photocatalysts, chemical sensors,24 self-cleaning coating,25 and TiO2/polymer nanocomposites.16, 26-28

Porous and particulate ZrO2 has outstanding electrical, chemical and mechanical properties.29 Hence it can be used as catalyst supports,30, 31 and as a component of core-shell nanoporous electrodes to prevent recombination of an electron and a hole in dye sensitized solar cells and solid oxide fuel cells (SOFCs).32, 33 ZrO2 is also a very useful ceramic hardening material and is often used as a filler in composite biomaterials for joint prostheses.34

## 1.4. Methodology of Synthesizing Oxide Nanomaterials

Currently, there are many synthetic methods to produce high quality oxides, including sol-gel, hydrothermal or solvothermal, microemulsions, electrospinning, chemical vapor deposition (CVD), thermal decomposition, pulsed laser ablation, templating, and self-assembly techniques.35 However, most of the current methods suffer from environmental pollution and scale-up problems. For example, the conventional sol-gel process and templating methods involve volatile organic compounds (VOCs); hydrothermal or solvothermal methods involve high temperatures in an autoclave that generates corrosion and safety problems; while electrospinning or CVD processes are difficult to scale-up. These methods are briefly outlined below.

Sol-Gel Method. Metal alkoxides or salts are widely used as precursors for synthesizing metal oxides with various morphologies via a sol-gel route. Since the precursors react with water quickly and tend to precipitate, many methods have been used to control the reaction rate in order to obtain desired nanostructures. For instance, TiO2 nanoparticles with a diameter of 4.3 nm were prepared by controlled hydrolysis of titanium alkoxide in reverse micelles with the aid of a surfactant in a hydrocarbon solvent;36 while mesoporous anatase TiO2 nanoparticles with a mean diameter of 25.5 nm and a surface area of 189 m2/g were synthesized recently using the precursor of Ti(SO4)2 and laurylamine hydrochloride;37 TiO2 nanoparticles with a diameter of ca. 14 nm were prepared using a sol-gel process of isopropoxide with the aid of ultrasonication.38 Hansen et al. states that the sol-gel method is becoming the standard method for synthesizing oxide materials in Chemical Reviews, 2004.29

Hydrothermal/Solvothermal. Under subcritical or supercritical water/solvent conditions, TiO2 and ZrO2 nanoparticles have been produced from a variety of precursors. More details about this method are provided in Chapter 2.

Microemulsions. The synthesis of oxides from reverse micelles relies on the precipitation of metal ions in aqueous droplets.39 For example, 20-300 nm TiO2 gels were produced by hydrolysis of tetraisopropyltitanate in sodium bis(2-ethylhexyl)sulfosuccinate (AOT) reverse micelles.40

Electrospinning. This technique involves the use of a high voltage to charge the surface of the metal alkoxide solution that passes through a nozzle (or coaxial capillaries). Using this method, TiO2 and ZrO2 nanofibers and nanotubes have been produced.41-43 However, the resulting one-dimensional materials usually exhibited a diameter in the micron size.

CVD. This method involves the chemical vapor deposition of alkoxides or salts. The particle size was found to be a function of temperature, reaction rate, and concentration of the precursors, and TiO2 particles as small as 2 nm were obtained.44, 45 The advantages of this method include the uniform coating of the nanoparticles or nanofilm, and the disadvantages include the higher temperatures being used and difficulties of scaleup.46

Thermal Decomposition and Pulsed Laser Ablation. Metal alkoxides and salts can be decomposed and nanoparticles formed when high energy from heat or electricity is applied, if the process is well controlled. TiO2 nanoparticles with a diameter less than 30 nm were produced by the thermal decomposition of titanium alkoxide or TiCl4 at 1200 (C.  The particle size was found to be a function of precursor concentration and the flow rate of the precursors.47 Tetragonal ZrO2 particles from 6 to 35 nm were also produced using this method.48 TiO2 nanoparticles with a diameter ranging from 3 to 8 nm were synthesized by pulsed laser ablation of a titanium target immersed in an aqueous solution of surfactant or deionized water.49 However, the drawbacks of these methods are high cost and low yield, and difficulty in controlling the morphology of the particles.29

Templating. A template is a well-defined architecture onto which another material can form a nanostructure. A variety of templates have been studied for synthesizing oxide nanomaterials. For instance, cationic colloidal particles have been used to prepare the hollow TiO2 nanospheres by thermal condensation of the TiO2 shell on the template, followed by calcination to remove the polystyrene core;50 scaffolds of poly (styrene-block-2-vinylpyridiane) diblock copolymers have been used to synthesize highly dense arrays in a regular pattern of TiO2 nanoparticles through a sol-gel process;51 starch gel templates have been used to synthesize meso/macroporous TiO2 monoliths.52 The advantage of this method is that the template allows nanomaterials with a variety of morphologies to be prepared, while the disadvantage is the complicated synthetic procedures and the consumption of the nanotemplates, which need to be removed, normally by calcination.

Direct Sol-gel Process in subcritical CO2. By using a surfactant to disperse water, TiO2 nanoparticles were produced by the hydrolysis and condensation of titanium alkoxides using subcritical CO2 as a solvent.53 More details about this method are described in Chapter 2.

## 1.5. Supercritical Fluids and Supercritical Carbon Dioxide

### 1.5.1. Supercritical Fluids (SCFs)

By definition, a supercritical fluid (SCF) is a single phase when its temperature is above the critical temperature (Tc) and its pressure is above the critical pressure (Pc), as shown in a typical pressure-temperature (P-T) phase diagram (Figure 1.1). In the P-T phase diagram of a pure substance, the phase boundary lines divide the diagram into solid, liquid and gas regions. However, the boundary between the liquid and the gas disappears when the pressure is higher than the critical pressure, and the temperature is higher than the critical temperature.

Figure 1.1. Schematic: the phase diagram of a typical material.

A SCF has a density comparable with a liquid, which enables it to function as a solvent, and a viscosity similar to a gas, which provides superior mass and heat transfer compared with a conventional solvent. Also, due to the zero surface tension, SCFs have been extensively used for supercritical drying to maintain high surface areas of the materials.54 As a result of these favorable properties as a solvent, extensive research and development on SCFs for chemical reactions and extractions have been conducted in recent decades.55-57

By definition, viscosity is a measure of the resistance of a fluid to deform under shear stress.58 Using CO2 as an example, the viscosities and densities of vapor, liquid and supercritical CO2 under selected conditions are listed in Table 1.1.59 From this table, it can be observed that the viscosity and density of supercritical fluid are a function of temperature and pressure. By tuning temperature and/or pressure, a desired physical property of the SCF such as viscosity and density can be achieved.

Table 1.1.  The selected viscosities and densities of CO2 in vapor, liquid and supercritical phases.59, 60

| Temperature (K) | Pressure (psia.) | Phase | Viscosity (10-6 Pa·S) | Density (mol/L) |
| --- | --- | --- | --- | --- |
| 313 | 1000 | Vapor | 19.1 | 4.4 |
| 303 | 3000 | Liquid | 90.5 | 20.4 |
| 323 | 2000 | Supercritical | 52.5 | 15.2 |
| 333 | 2000 | Supercritical | 41.3 | 12.6 |
| 333 | 5000 | Supercritical | 82.8 | 19.5 |

Surface tension is caused by the molecules of the liquid at the surface that are subject to an inward force of molecular attraction.61 The surface tension of the saturated liquid CO2 as a function of pressure/temperature is plotted in Figure 1.2.60, 62 In the saturated liquid region, the surface tension decreases as the pressure/temperature increases. In the supercritical region, the surface tension is zero due to the disappearance of the interface between the liquid and vapor phases.

Figure 1.2.  Surface tension of saturation liquid CO2 vs. pressure.  The data points were labeled with the corresponding saturation temperatures at the specific pressures.  In the supercritical region, the surface tension is zero.60

Different substances have their own critical properties. Table 1.2 shows the Tc, Pc and ρc (the density at the critical point) of selected substances that have been used as SCFs for material processing and chemical reactions.57 Generally speaking, low Tc and Pc of a substance are desirable due to economic issues. Practically, the safety and environmental issues for using a flammable organic compound and the solvent power of the substance have to be considered when one selects a SCF. Among the candidates of SCFs, CO2 is an outstanding one, because of its relative low Tc and Pc, low cost, abundance, and the fact that it is environmentally benign. Usage of scCO2 instead of water or organic solvent can reduce the water pollution and emission of VOCs. The industrial sources of CO2 include the flue gas from power stations, as well as CO2 being a by-product of existing processes such as ethanol, ammonia and hydrogen production.

Table 1.2. Critical properties for selected supercritical fluids in chemical reactions57

### 1.5.2. Particle Formation in SCFs

SCFs offer many opportunities to form particles with improved properties. From the processing aspect, producing particles by SCFs can be classified into several major processes such as gas antisolvent (GAS), rapid expansion of supercritical solution (RESS), precipitation from gas saturated solutions (PGSS), etc.63, 64

RESS Process. In 1984, Krukonis first reported using the RESS process for the preparation of small particles and fibers of polypropylene and soybean lecithin.65 After this report, extensive studies were made on the formation of a variety of materials by means of the RESS process. For example, silica particles with a diameter of 100 ~ 500 nm were prepared by the rapid expansion of supercritical water solution at 470 C.66 It was found that the pre-expansion solution temperature had the most significant impact on product morphology among the RESS parameters, while the polymer-solution concentration had only a minor effect.66, 67 The RESS process can be considered to consist of four steps:

- Preparation of the supercritical solution, typically by dissolution of the solute in the supercritical solvent.

- Setting of the pre-expansion conditions upstream of the expansion device.

- Rapid expansion of the supercritical solution from the pre-expansion conditions to ambient conditions through a device such as a micro-orifice or capillary.

4.   Recovery of the product in an expansion chamber.57

When a SCF containing a dissolved solute goes through a micro-orifice, the density and solvation power of the fluid decreases dramatically in a very short time, resulting in supersaturation and subsequent precipitation of solute particles.57

GAS Process. In the Gas-Antisolvent (GAS) method, the solute is soluble in an organic solvent but insoluble in a SCF. If the SCF is added into the organic solvent, the solubility of the solute decreases, hence causing precipitation. The resulting particle size and size distribution depend on the selection of the solution/antisolvent system, the solution concentration, the relative solution and antisolvent quantities, the rate of the antisolvent addition, and the degree of mixing.68

### 1.5.3. Chemical Reactions in SCFs

The usage of SCFs as an alternative to conventional solvents has been the subject of increasing investigation over the last two decades due to the solvation and transport properties that can be varied appreciably.57 Specifically, CO2 has been used for polymerization,69-73 catalytic oxidation,74 catalytic hydrogenation,75 enzymatic reactions,76 and sol-gel reactions.53, 77-79

Temperature and pressure are fundamental physical properties that affect various thermodynamic and kinetic parameters, especially for chemical reactions carried out in a SCF using a relatively high operating pressure.80 The Arrhenius equation can be used to estimate the temperature effect on the reaction rate constants:

(1.1)

where k = the reaction rate constant, k0 = the frequency factor, Ea = the activation energy in J/mol, R = universal gas constant = 8.314 J/(mol·K), T = temperature in K.

The pressure effect can be evaluated using transition state theory.81, 82 This theory assumes a chemical equilibrium between the reactants and an activated transition state species, with the latter proceeding directly to products. The rate of the chemical reaction is governed by the rate constant k:

A + B ⇌ M‡  products                                                (1.2)

where A and B denote the reactants, M‡ is the transition state complex, and k is the rate constant.

The pressure effect on the reaction rate is given by:

(1.3)

where = bimolecular rate constant (mol/L·min), = M‡ -A-B = activation volume (the difference between the partial molar volume of the transition state species and that of the reactants), i = partial molar volume of component i at reaction conditions, = mixture isothermal compressibility (this term is not included if the rate constant is expressed in a pressure-independent form, such as molar fraction or molarity), R = universal gas constant, and n = the sum of the stoichiometric coefficients of the reactants.83 The partial molar volume, i, and isothermal compressibility of the reaction mixture, , can be estimated from an equation of state.57, 82, 84 According to Equation 1.3, when =0 and  is negative, an increased pressure will result in a higher rate constant.

The density variation in a SCF also influences the chemical potential of solutes and, thus, reaction equilibrium constants.85

The clustering phenomenon is also important for consideration of chemical transformations in SCF media.57 It was widely recognized that the solvent density in the region around a solute molecule will be higher than the bulk density, and this deviation is often 50 to 300 % and influences the kinetics of the reaction.86 For instance, in their study on the pressure’s effect on the esterification of phthalic anhydride in supercritical CO2, Ellington et al. attributed the reaction rate deviation from Equation 1.3 to the clustering effect.87

### 1.5.4. Commercial Implementation of SCFs

Commercial implementation of SCF extraction applications include coffee and tea decaffeination, cholesterol and fat removal from eggs, acetone removal from antibiotics, and organic removal from water.57 The early commercial implementation of SCF technology for conducting chemical reactions include ammonia synthesis (1913), methanol synthesis (1923), oxidation of light alkanes (1920) and the synthesis of low-density polyethylene (1940).55 In 1985, SCF butene was used for 2-butanol production from 1- and 2-butene.57 In 2002, DuPont commercialized the synthesis of fluoropolymers in scCO2.88

### 1.5.5. ScCO2

Of the supercritical fluids, the most exciting potential is provided by the environmentally friendly solvent, supercritical carbon dioxide (scCO2). The utilization of scCO2 as a substitute for conventional organic solvents for the processing of materials has been widely reported.89-92 The reasons are due to scCO2 being non-toxic, non-flammable, inexpensive, naturally abundant, and environmentally benign. With a critical temperature of 31.1 C and a critical pressure of 1070 psig, the critical conditions of scCO2 are easy to be achieved so that a lower capital cost is required for the autoclave materials and a lower operation cost is achieved due to lower energy consumption. The properties of scCO2 can be easily tuned by changes of total pressure and/or temperature, hence changing the solubility of various compounds as desired.93, 94 In addition, removal of scCO2 can be easily achieved by venting, hence no evaporation or drying processes are required. Particularly, supercritical drying extinguishes the liquid surface tension that causes the shrinkage of the solid, hence the microstructure of the aerogel is maintained after the drying process.95 As a result, scCO2 has been widely employed for aerogel processes.96-99 A recent study shows that large pore sizes were obtained when using scCO2 as a solvent for synthesizing mesoporous silica, in which silicon alkoxide was the precursor and a block copolymer was used as the template.100

The first study on homogeneous catalysis in scCO2 started in 1991 when Rathke and Klingler reported their work on hydroformylation of propylene catalyzed by HCo(CO)4 in scCO2.101 The advantages of homogeneous catalysis in scCO2 include higher solubility of the gaseous reactant in the SCF compared to conventional organic solvents,102 higher mass transfer than that of heterogeneous catalysis, and easy ability to scale-up. A major drawback of homogeneous catalysis lies in the difficulty of catalyst recovery and recycling.57

## 1.6. Sol-Gel Synthesis and Aerogel

### 1.6.1. Sol-Gel Technique and Aerogel

A sol is a colloidal suspension of solid particles in a liquid.103 When sols attract each other and stick together in such a way to form a network, a gel is formed. A gel is a substance that contains a continuous solid skeleton enclosing a continuous liquid phase.104 If the smallest dimension of the gel is greater than a few millimeters, the material is called monolith. If gels are in dimension from 1 nm to a few millimeters, it is called particulate gels.105 Drying a gel by evaporation under ambient pressure gives rise to capillary pressure that causes shrinkage of the gel network. The resulting material is called a xerogel that is a dense material and exhibits a low surface area. In contrast, drying the gel under supercritical conditions eliminates the interface between liquid and vapor, so that there is no capillary pressure and relatively little shrinkage; the resulting materials are called aerogels.104, 106 Recently, materials dried by freeze-drying produce materials initially known as cryogels, now also termed aerogels.95 Aerogels are extremely porous, low-density materials with a larger surface area than the xerogels. A typical aerogel comprises both meso- and micro-pores and exhibits a large surface area of hundreds of square meters per gram. They have extremely low thermal conductivities and fascinating acoustic properties due to their porous structure.107 The first gel derived from a metal alkoxide was synthesized by Ebelmen, in 1846,108 while the first aerogel was prepared by Kistler, who invented the supercritical drying method in 1932, which solved the shrinkage problem during gel drying.103, 109 Aerogels can be used for advanced applications including electrochemical devices, thin coatings, composite biomaterials, catalysts, ceramics, and heat and electric insulation devices.110-113 This is because the aerogels have unique morphological and chemical properties which originate from the preparation methods and operational parameters such as the type of alkoxide, the H2O/alkoxide ratio, the catalyst used for hydrolysis and condensation, the calcination temperature, and the SCF used for drying.113

### 1.6.2. Conventional Method of Aerogel Synthesis

The conventional method for producing aerogels by the wet sol-gel route was developed after Kistlers pioneering work. This method involves hydrolysis of the metal alkoxide with water and a catalyst, i.e. an acid or a base, condensation into macromolecules, forming a colloidal sol and three-dimensional network wet gel, solvent exchange to remove water by alcohol, then drying the wet gel into an aerogel using a supercritical fluid (Figure 1.3).114 The mechanism of hydrolysis and condensation of transition metal alkoxides is relatively well-understood.115

Figure 1.3. Flow chart of conventional sol-gel route.

Hydrolysis and condensation of metal alkoxide precursors.

When a metal alkoxide reacts with water, nucleophilic substitutions occur as shown in Figure 1.4:104 For the coordinatively saturated metals such as the metal alkoxides, hydrolysis and condensation both occur by nucleophilic substitution (SN) mechanisms, in which coordination and proton transfer are involved and followed by removal of either alcohol or water.

Figure 1.4. Mechanisms of hydrolysis and condensation of metal alkoxides.105

### 1.6.3. Direct Synthesis of Aerogel via a Sol-Gel Route in SCFs

A modified non-aqueous sol-gel route, was first reported by Loy et al. in 1997, in which the direct synthesis of SiO2 aerogel monolith in CO2 was studied by using formic acid as the polycondensation agent.116 The direct synthesis of silica spherical particles in micron-size and nanofibers in supercritical acetone was reported by M. Moner-Girona et al. in 2003.78 The new method simplified the aerogel process by completing both the reaction process and the drying process in one step. The success of this work on the direct sol-gel process in SCFs shed light and inspired this research.

# Direct Sol-Gel Process in SCF: A Review

## 2.1. Overview

“The 1980s were the decade of extraction, the 1990s have been the decade of materials, and the start of the next century will be the decade of reactions.”

------ Michel Perrut, in 199794

Since the discovery of supercritical drying by Kistle,109 the combination of sol-gel processing and supercritical fluid (SCF) techniques provides significant potential for material science and nanotechnology.

The conventional method of synthesizing inorganic aerogels comprises a wet sol-gel process, in which alkoxides are hydrolyzed and condensed into a wet network, followed by SCF drying in order to maintain the micro-architecture. The inorganic aerogels exhibit microporous and mesoporous structures and significantly higher surface area. Their applications include catalysis, acoustic and thermal insulation, optics, and electrics. The conventional sol-gel method for aerogel synthesis has been well reviewed by Gesser et al. in 1989 and Pierre et al. in 2002.54, 113

In the last decade, a new approach for synthesizing oxides directly in SCFs has been developed, and nanoarchitectures with a variety of morphologies, i.e., aerogel monolith, films, monolayer, nanospheres, and pillared structure, have been prepared.

In the present review, the direct sol-gel process in SCFs designates a one-pot synthesis for inorganic materials through either hydrolysis-condensation or polycondensation of alkoxides or salts in subcritical or supercritical fluids.

## 2.2. Supercritical and Subcritical Water or Alcohol

The high temperature SCF processing of inorganic materials is attractive for materials engineering, as: (1) a variety of morphologies are obtained that are difficult to be synthesized with alternative methods; (2) the high surface area and the microstructures are maintained due to the low interfacial tension of the SCF; (3) the crystalline phases are obtained immediately after the high temperature SCF process, and there is no need to recover the solid from solution and post-annealing; and (4) the process is easily adaptable to continuous production.94, 117

The experimental setup of the SCF continuous system for synthesizing oxide nanoparticles includes: a high pressure pump for pumping the fluid into the reactor, a regulating valve for maintaining the pressure, and the high-pressure reactor.118

The first direct sol-gel process of alkoxides in the high-temperature SCF was studied by Pommier et al. in 1992. After that, many crystalline nanoparticles have been synthesized. As an example, 20 ~ 60 nm TiO2 anatase nanoparticles were prepared from titanium isopropoxide (TIP).117 By using IR analysis, a kinetics study was conducted. The reaction was assumed to be a hydrolytic decomposition, rather than a pure thermal decomposition, followed by a polymerization-polycondensation and precipitation of the solid. Interestingly, it was found that the temperature and pressure had no significant effect on the particle size of TiO2.118 In other research, anatase TiO2 was deposited on the substrate surface and inside the pores of commercial -Al2O3 by hydrolytic decomposition of titanium isopropoxide in supercritical isopropanol. Various experimental parameters, i.e. temperatures, precursor concentration, water-to-alkoxide ratio, solution flow rate, and deposition time, were studied by Brasseur-Tilmant.119

Using the same technique, Znaidi et al. prepared submicron MgO powders with a surface area of 210 ~ 280 m2/g from magnesium isopropoxide or magnesium acetate at approximately 200 C in liquid alcohol or supercritical alcohol-CO2 mixtures.120, 121 The mechanism of the sol-gel process in the SCF comprises hydrolysis and polycondensation:

-Mg-OR + H2O ⇌ -Mg-OH + ROH                                   (2.1)

-Mg-OH + RO-Mg- ⇌ -Mg-O-Mg- + ROH                            (2.2)

-Mg-OH + HO-Mg- ⇌ -Mg-O-Mg- + H2O                            (2.3)

While the sol-gel reactions of magnesium alkoxide in the SCF were the same as those in the conventional solvent, Znaidi et al. also proposed the scheme of formation of the polycondensates from MgL2 (L= acac or acetate):

MgL2 + ROH ⇌ [MgL(OR)(ROH)]n + nLH                               (2.4)

[MgL(OR)(ROH)]n + ROH ⇌ [MgL(OR)x(ROH)4-x]n + nLH               (2.5)

The resulting polycondensates were thermally decomposed into cubic MgO with a diameter less than 100 nm at a higher temperature of 450 (C.121

Znaidi et al. also synthesized BaTiO3 powders with a particle size of ca. 10 nm in a semi-continuous process under subcritical and supercritical isopropanol.  There were two steps involved: (1) the hydrolysis of the alkoxide BaTi(O-iC3H7)6 in isopropanol at temperatures 100  200 C in a tubular flow reactor;  and (2) a thermal treatment of the formed solids at a higher temperature than 235 C.122

In 1997, Hu et al. prepared hydrous zirconia nanoparticles via hydrolysis and controlled hydrothermal condensation of zirconyl inorganic salts, ZrOCl2 and ZrO(NO3)2 in aqueous solution.  The hydrous zirconium oxide particles were porous, cube-shaped aggregates of small crystallites (< 5 nm).  The nucleation and nanoparticle growth were monitored with a dynamic laser light-scattering spectrophotometer.123

From 1999 to 2000, Zeng et al. prepared Pb-zirconate-titanate (PZT), Pb(Zr0.52Ti0.48)O3,  and barium titanate (BaTiO3) thin films on Si substrates using a sol-gel-hydrothermal technique which involved a combination of a conventional sol-gel process and a hydrothermal method. At a low processing temperature of 100 200 C, the dense and pinhole-free PZT films in single perovskite phase and polycrystalline BaTiO3 were observed using atomic force microscopy (AFM).124-126

In 2000, Shen et al. prepared ZrO2 particles with a diameter of ca. 15 nm by hydrothermal processing of zirconium oxychloride octahydrate (ZrOCl2(8H2O) at 150 C. The clear solution containing ZrO2 sol was spin-coated onto a silicon wafer or glass substrate to form a ZrO2 thin film. The multilayer films were characterized with FTIR, AFM and a laser damage test.127, 128 In the same year, Zhao et al. prepared nanocrystalline zirconia sols (4 nm) with a metastable cubic phase from diglycol-modified zirconium propoxide via the alcohol thermal process.  The chelating bonding of diglycol with zirconium was found to be important in obtaining stable zirconia sols, and the formation of cubic ZrO2 crystals was found due to the template of diglycol and the high alignment of solute oligomers through condensation.  The ZrO2 gel generated from the sols exhibited a mesoporous structure with a pore size of 2.5-3.8 nm and Brunauer-Emmett-Teller surface area of 130-266 m2/g.129

In 2002, Hayashi et al. prepared TiO2 powders with mesoporous structure under various subcritical and supercritical water conditions using titanium isopropoxide (TIP) as a starting material. The synthesized TiO2 powders were used for photocatalytic hydrogen evolution in an aqueous methanol suspension.  Activities per unit surface area were found to be higher from the TiO2 synthesized under supercritical water conditions than those synthesized under subcritical water conditions. This phenomenon was explained by the higher crystallinity of the TiO2 powders under supercritical water conditions.130 In the same year, Yang et al. prepared anatase and rutile TiO2 nanoparticles by means of a hydrothermal treatment of tetrabutylammonium hydroxide-peptized and HNO3-peptized sols at 240°C.131

In 2003, Parvulescu et al. prepared mixed vanadia-titania-silica catalysts (3 or 6 wt% V2O5, and 16-34 wt% TiO2) in one pot by both sol-gel and hydrothermal methods in the presence of different surfactants, i.e., cetyltrimethylammonium bromide (CTMABr) or octadecyl-trimethylammonium bromide (ODCABr).  Tetraethylorthosilicate (TEOS) was used as the precursor for silica, titanium isopropoxide (TIP) for titania, and vanadyl sulfate for vanadia.  The resulting materials were characterized by N2 adsorption and desorption curves at 77 K, Raman spectroscopy, XRD, XPS, TEM, NH3-DRIFTS, and H2-TPR.132

In 2004, Tai et al. prepared ZrO2 nanospherical particles using thermal hydrolysis of zirconyl nitrate solution at a temperature at 95 °C. Hydrolysis of ZrO2 salt was confined in the droplets of the water/CTAB/hexanol reverse microemulsion. The particle shape and size distribution varied greatly with both the temperature and composition. However, calcination at 600 °C was required to obtain the tetragonal phase, and the size distribution of the particles was rather large.133

In 2005, Corradi et al. prepared TiO2 nanospheres with a diameter of ca.10 nm and crystal grains (100 by 50 nm) using microwave hydrothermal treatment of TiOCl2 solution. An enhanced powder crystallinity and decreased processing time was achieved.134 Kang et al. synthesized TiO2 and Bi/TiO2 particles with particle size below 25 nm using a solvothermal method, in which isopropoxide was mixed with ethanol in an autoclave and heated to 200 °C for 10 hours. The resulting materials were characterized with XRD, SEM, UV-visible spectrometry, and the plasma-photocatalytic activity for acetaldehyde was tested.135

## 2.3. Direct Sol-Gel Process in CO2

A direct sol-gel process for synthesizing oxide nanomaterials in scCO2 or subcritical CO2 is a promising technique, because of its environmental benignness, and low temperature. There are three approaches for the direct sol-gel process in CO2: (1) using a surfactant to stabilize the dispersion of water in CO2, in which the water droplets react with the alkoxide to start the sol-gel reactions; (2) alkoxides reacting with water without surfactants; and (3) using carboxylic acid instead of water to initialize the polycondensation of the alkoxides to form macromolecules.

### 2.3.1. Surfactant-Assisted Hydrolysis

In 1996, Tadros et al. reported the formation of TiO2 nanoparticles in scCO2 by hydrolysis and condensation of titanium alkoxide. Before addition of CO2, the alkoxide and water + anionic fluorinated surfactant, [F(CF2CF2)zCH2CH2O]xP(O)(ONH4)y (where x = 1 or 2, y = 2 or 1, z = 1 – 7), were put in two vials that were located in an autoclave. The surfactant was able to stabilize the tiny water droplets in scCO2 at 45 (C and 1400 psig, and spherical particles of titanium dioxide with low anatase crystallinity were formed.136

In 2003, Stallings et al. performed a more systematic study on the direct sol-gel process of titanium isopropoxide (TIP) in scCO2 by using the same anionic fluorinated surfactant used by Tadros et al.  TIP was injected into water-in-CO2 dispersions using a HPLC pump. Spherical titania particles with a broad particle size distribution (20-800 nm) were obtained. The surface area of the as-prepared material, 100 ~ 500 m2/g, was attributed to the internal porosity of the spherical titania particles, as evidenced by scanning transmission electron microscopy (STEM).  After calcination, the surface area of the as-prepared titania powder at 300 °C in air decreased from ca. 300 to 65 m2/g and increased the mean cylindrical pore diameter from 2.6 to 4.9 nm.97

In 2003, Hong et al. prepared TiO2 nanospherical particles by the direct sol-gel processing of titanium isopropoxide (TIP) in water-in-carbon dioxide microemulsion using ammonium carboxylate perfluoropolyether (PFPE-NH4) as a surfactant. A narrow distribution of particle sizes was observed. The crystallinity and crystallite size of nanoparticles produced increased with an increase of molar ratio of water to surfactant (W0). Room temperature and a pressure of 4000 psig was used.137

Keith Johnson’s group also produced TiO2 spherical particles by the direct sol-gel process of TIP with water in CO2 at 25 °C and 4000 psig in the presence of surfactants, PFPE-NH4 and poly (dimethyl amino ethyl methacrylate-block-1H,1H,2H,2H-perfluorooctyl methacrylate). The particle size was also found to be a function of the molar ratio of water to surfactant headgroup (W0), and the precursor concentration and TIP injection rate as well. The hydrodynamic diameters of the hydrated micelles and particles were characterized using a dynamic light scattering (DLS) measurement, and the larger size of the TiO2 particles compared to the micelles was attributed to surfactant reorganization. As the surfactant remained attached to the particles, coalescence of the particles was prevented.53

### 2.3.2. Hydrolysis without Surfactant

In 2003, Reverchon et al. prepared amorphous titanium hydroxide nanoparticles on the pilot scale in scCO2 without the assistance of surfactant. The process was based on the reaction:

Ti(OCH3H7)4 + 4H2O ⇌ Ti(OH)4 + 4C3H7OH                           (2.6)

The reaction was carried out in an autoclave, which had three inlets and one outlet. The inlets were connected with a CO2 supply, a CO2-TIP contactor, a CO2-water contactor, while the outlet led to a liquid separation tank. Since the solubility of water in scCO2 is as low as 0.16% (w/w), while that of TIP is 2% (w/w) at 2200 psig and 40 °C, the flow rates of the CO2-TIP and CO2-water were 9 and 20 kg/h, respectively, to ensure enough water was available for the hydrolysis. The residence time was 180 seconds, which led to complete conversion. The formed particles were separated with the liquid in a downstream separator. The synthesized Ti(OH)4 particles were amorphous and had a narrow particle size distribution.138

In 2004, Yoda et al. synthesized titania-pillared clay, montmorillonite (MNT) in scCO2. This scheme consists of two steps: (1) ion exchange of interlayer cation by hydrophobic cation, using alkyltrimethylammonium cation in aqueous solution, and (2) the intercalation of a metal alkoxide dissolved in scCO2 followed by hydrolysis with adsorbed water present in the interlayer space. Nano-sized anatase crystal structure was observed in the calcined samples. The titania-pillared clay sample showed potential as a catalytic adsorbent for toxic volatile organic compounds in air.139

In 2005, Sun et al. grafted mono and bi layers of TiO2 on mesoporous SiO2 molecular sieve SBA-15 via a surface sol-gel process in scCO2. The process involved grafting of TIP onto the surface of the molecular sieve, extraction of extra TIP, followed by hydrolysis of the impregnated TIP with an excess amount of water and calcination. The XPS results confirmed the formation of Ti-O-Si and Ti-O-Ti bonds. The TiO2 grafted SiO2 molecular sieve has potential for photocatalysis and as a catalyst support.140, 141

In 2006, Jensen et al. prepared anatase titania at a temperature as low as 100 °C in scCO2 by a “seed enhanced crystallization (SSEC) process”. A crystallinity as high as ca. 60% was obtained without downstream calcination. Polypropylene, ceramics, metal fibers and wool fibers were used as seeding materials. To prevent the premixing of the reactants before addition of CO2, TIP and water were injected in the upper third and lower third, respectively, of the seeding material that was loaded into an autoclave. After addition of CO2, the reactants were able to mix and the sol-gel reaction started. The authors claimed a mechanism that water dispersed into CO2 and reacted with TIP sitting on the surface of the seeding material, and the seeding material acted as heterogeneous seeds for the nuclei formation and facilitated the formation of crystalline nuclei. The results were encouraging, however, the proposed mechanism is suspect. As the solubility of TIP is much higher that that of water in scCO2, it is unlikely that water will be “mechanically dispersed with scCO2” while TIP was “homogeneously dispersed” by the seeding material rather than CO2.142 Recently, Jensen et al. studied the growing of TiO2 particles with reaction time using in situ small-angle X ray scattering (SAXS) and wide-angle scattering (WAXS),143 and it was found that the sol-gel process in scCO2 was faster than in the organic solvent.

Recently, Cabanas et al. synthesized highly porous SiO2 aerogels in scCO2 using polystyrene latex particles decorated with methacrylic acid. TEOS or TMOS were used as a precursor reacting with water.144, 145

### 2.3.3. Carboxylic Acids as Polycondensation Agents

In 1997, Loy et al. prepared a silica aerogel monolith for the first time by polymerization of silicon alkoxide, tetramethyl orthosilicate (TMOS), with formic acid in CO2 at 40 °C and 6000 psig.77 The results showed that the sol-gel polymerization could be conducted directly in CO2 as solvent by using formic acid as the condensation agent/co-solvent. The resulting materials exhibited a highly porous architecture with both meso- and macropores. Following this idea, Moner-Girona et al. prepared silica aerogel micro-particles by using formic acid as a polycondensation agent in CO2.78

## 2.4. Summary

The direct sol-gel process in SCFs simplifies the conventional aerogel preparation by using a one-pot synthesis. The crystalline formation in the high temperature autoclave makes it possible to skip the downstream calcination process. Furthermore, the direct sol-gel process in SCFs promises a new route for synthesizing inorganic and hybrid materials with exciting morphologies, such as nanoparticles, films, and mesoporous and pillared materials.

For synthesis of inorganic materials, scCO2 is a promising solvent due to its low critical temperature, and relatively low equipment cost. Supercritical water is also very attractive due to the direct formation of the crystalline phases. Its drawbacks include high operation temperature and corrosion of the autoclave materials. The supercritical alcohols suffer from safety issues, and very strict safety systems are required in the area in which the reactor is located.

# Materials and Methods

## 3.1. Outline

In this chapter, the experimental setup used for sol-gel synthesis and characterization methods used throughout this thesis are described.

The synthesis of the nanomaterials was carried out either in a high-pressure view cell reactor or an autoclave. The high-pressure reactors were connected with CO2 and other liquid supplies, along with having temperature and pressure controllers, and in situ spectroscopy characterization equipment.

Characterization methods of the synthesized materials include: in situ attenuate total reflection-Fourier transform infrared spectroscopy (ATR-FTIR), powder ATR-FTIR, differential scanning calorimeter (DSC), thermogravimetric analysis (TGA), N2 physisorption, X-ray diffraction (XRD), scanning electron microscopy (SEM), transmission electron microscopy (TEM), high-resolution TEM (HRTEM), and scanning transmission electron microscopy (STEM).

## 3. 2. Synthesis Setup

For synthesizing a small amount of material, the experiments were carried out in 10 mL or 25 mL view cells made of stainless steel. For larger scale synthesis and in situ analysis, a 100 mL stainless steel autoclave equipped with ATR-FTIR spectrometry was used.

### 3.2.1. View Cell, Pump, Valves and Connections

View cell. Equipped with sapphire windows, the view cell is ideal for observation of phase equilibrium, particle formation and small-scale material synthesis in SCFs, especially for scCO2.146-148

The body of the view cell is made of stainless steel (Figure 3.1). There are 4 holes with threads on the wall. The big hole is for a pressure transducer, and the three small holes are for a thermocouple, inlet and outlet connections, respectively. The two openings are sealed using a Teflon™ O ring, sapphire window, copper washer and a stainless steel fastening part, respectively.

Figure 3.1. The view cell.

Pump. Syringe pumps (ISCO 100 or 260D) were used for pumping CO2 or other liquids into the reactors. There are two modes for pumping operation using the syringe pumps: constant pressure and constant flow. Generally, when CO2 was added into the reactor to initialize the reaction, the constant pressure mode was used; when using CO2 to extract the liquid in the reactor after the reaction, the constant flow mode was used. The operation of the syringe pump was performed through LabView VI control or using the electronic controller provided by ISCO.

Valves, Tube and Connections. The valves and connections for the high-pressure reactors were provided by HIP. The specifications of the parts are:

Taper seal needle valves: 15-11 AF1 (1/16” tube), 15-11 AF2 (1/8” tube, straight), 15-12 AF2 (1/8” tube, angle).

Glands: 15-2 AM1 (1/16” tube), 15-2 AM2 (1/8” tube).

Sleeves: 15-2 A1 (1/16” tube), 15-2 A2 (1/16” tube).

Ball check valves: 15-41 AF1  (1/16” tube), 15-41 AF2  (1/8” tube)

### 3.2.2. View cell with LabView VI control

A 10 or 25 ml stainless steel view cell was connected with a syringe pump (ISCO 100 DM) for pumping CO2 from a dip tube. The check valve next to the pumps was used to prevent possible back flow from the view cell. Temperature in the view cell was measured and controlled by means of a T-type thermocouple, a heating tape (Omega SRT051-040, 0.5×4 FT) and a temperature controller (Fuji PXZ-4). The pressure was controlled by means of a pressure transducer (Omega PX302-10KGV) and a control valve (Badger-78S), which were connected to a network interface (FieldPoint, National Instruments). The network interface communicated with a computer by means of LabView software (Figure 3.2).

Figure 3.2. Schematic of experimental setup: (A) computer with LabView Virtual Instrument, (B) FieldPoint by National Instruments, (C) temperature controller, (D) thermocouple, (E) pressure transducer (F) stainless steel view cell equipped with sapphire windows, (G) pneumatic control valve, (H) needle valve, (I) check valve, (J) syringe pump, (K) CO2 cylinder.

### 3.2.3. Instrumentation

The syringe pump was controlled either by a local controller provided by ISCO or by a computer. A 9 pin 232 serial port and a driver were used for computer control. The driver for pump control was provided by ISCO.

The pneumatic control valve was controlled using the computer with “Pressure Control VI (Visual Instrument)” designed by the author. The front panel is shown in Figure 3.3, the block panel is provided in Appendix 6, and the software is provided in the attached CD. On the Front Panel, the pressure setpoint can be adjusted by clicking on the arrow buttons either before or during running the virtual instrument (VI). The real pressure is indicated by means of the blue level in the cylinder, the blue dots in the window, or numerically above the window. The real-time status of the pneumatic valve is indicated by means of the round indicator above the valve. The default PID Tuning Parameters were: Prop Band = 40 %, Reset Time = 0.08 min, Deriv Time = 0.02 min.

Figure 3.3. The Front Panel of Pressure Control. A: switch for automatic or manual control; B: pressure cylinder indicator; C: pneumatic valve open-close indicator; D: pneumatic valve; E: read error out; F: write error out; G: pressure setpoint; H: setpoint and real pressure indicator; I: PID tuning parameters; J: stop button.

The block diagram of pressure control was designed by using LabView 7.0 of National Instruments (Appendix 6). The analog input signals provided by FieldPoint FP-TP-10 channel 2 was translated from mV into pressure unit (psig) and displayed. The signal in engineering units was also transferred to percentage, and then sent to the PID subVI, together with the pressure setpoint. The output of the PID subVI was transferred from percentage into engineering units (mA), and then converted into dynamic data, which was sent to the pneumatic valve via FieldPoint FP-TP-10 channel 1. The instrumentation and configuration are summarized in Appendix 7.

### 3.2.4. Temperature Controller

In order to control the temperature of the view cells, a Fuji PXW-4 temperature controller and heating tape (Omega SRT051-040, 0.5×4 FT) were used.

### 3.2.5. Reactor Equipped with In situ FTIR

Figure 3.4 shows the schematic of the experimental reactor used in this research. Carbon dioxide and precursor were pumped using syringe pumps (ISCO 260D). All feed lines have check-valves to prevent backflow and rupture disks (HIP) for safety in case of over pressurization. The reactor is a 100-mL stainless steel stirred autoclave (Parr Instruments) with a turbine impeller to provide mixing of ingredients. The reactor is heated by a heating mantle, and has an installed pressure transducer (Ashcroft K25F) and a thermo well containing a thermocouple (Parr-A472E2). The reactor temperature was controlled using a digital controller (Parr 4842).

Figure 3.4. Schematic of experimental setup: autoclave with online FTIR and GC-MS. (A) computer; (B) FTIR; (C) temperature and RPM controller with pressure display; (D) 100 ml autoclave equipped with diamond IR probe; (E) needle valves; (F) check valves; (G) syringe pump; (H) container for carboxylic acid; (I) CO2 cylinder.

Collection Vessel for RESS Process.

During the RESS process, particles were sprayed through a variable-volume nozzle (HIP) into a closed stainless steel chamber (home made, Figure 3.5) with a heating jacket (Glas-Col, 102A, 300W) to collect particles sprayed at a constant depressurizing rate. The inlet of the particle collection device was connected to the stirred reactor and the outlet went through a filter (HIP) and was vented to a high velocity fume hood.

Figure 3.5. Schematic of particle collection vessel for the RESS process.

## 3.3. Synthesis Procedures

Synthesis of SiO2, TiO2 and ZrO2 aerogels. The experimental procedures for synthesizing SiO2 TiO2 and ZrO2 included addition of a carboxylic acid and an alkoxide into the reactor (a view cell or an autoclave), followed by addition of CO2 to a desired temperature and pressure. In the case of synthesis of SiO2 nanoparticles, two methods have been used: (1) quick depressurizing with the particles being collected directly in the autoclave, and (2) using the RESS process, in which the SCF was passed through a nozzle and the particles were generated in the collection vessel as described in Figure 3.5. In the case of synthesizing TiO2 and ZrO2 monolithic aerogels, typically 2-3 days were allowed for aging after the gel was formed. After CO2 extraction and venting, the resulting aerogels were subject to further drying and calcination in air. More details of the synthetic procedures for SiO2, TiO2 and ZrO2 are described in Chapter 4, 5 and 6, respectively. The synthetic procedures for Ti-acetate single crystals are provided in Appendix 8.

## 3. 4. Characterization Methods

### 3.4.1. Online FTIR

IR spectrometry is a type of absorption spectrometry that uses the infrared region of the electromagnetic spectrum, at which frequency chemical bonds vibrate in either a stretching or bending mode. The absorption frequency is determined by the molecular structure. FTIR is an improved technique to make the IR measurements easier and faster, in which the IR beam is guided through an interferometer. A FTIR spectrum is obtained from performing a mathematical Fourier Transform on the interferegram.

Recent literature has shown that ATR-FTIR spectroscopy is a powerful tool for in situ measurement of concentration, solubility, and supersaturation in crystallization processes for the chemical and pharmaceutical industries.149, 150 ATR spectroscopy uses the phenomenon of total internal reflection. In this technique, the radiation beam is directed onto an angled crystal and reflected within the crystal until it emerges from the other “end”, where it is collected. The depth of penetration, as the beam of radiation penetrates a fraction of a wavelength beyond the reflecting surface, distinctively produces: (1) little to no disturbing interference from the solid particles already present in the solution, or generated by crystallization, and (2) a less intense solvent contribution to the overall infrared spectrum so the solvent spectra can be easily subtracted from the sample spectrum. These characteristics of a small depth of penetration with no sensitivity to solid particles constitute the technical motivation for the employment of ATR-FTIR technology as an online monitoring tool for supercritical crystallization and chemical reactions. Figure 3.6 shows a schematic of the ATR-probe cell used in this thesis. In the ReactIR-4000 main box, there are instrument computer boards, a laser power supply, an IR source, and a detector. A mirrored optical conduit with 25 mm interior diameter is used to transmit the light between the IR source/detector and the diamond probe, which is located at the bottom of the reactor. The diamond probe, with a commercial name DicompTM composition probe, is robust and pressure-rated to 5000 psig (Figure 3.7).

Figure 3.6. Schematic of the reactor with the ATR-FTIR probe assembly.

Figure 3.7. Schematic of the DicompTM probe.  Infrared radiation is reflected into the chemically resistant ATR disk that is in contact with the reaction mixture.  The drawing is adapted from ASI.

Beer-Lambert law: The Beer-Lambert law is an empirical relationship that relates the absorption of light to the properties of the material through which the light is traveling.

A = α×l×c                                                             (3.1)

where, A is the absorbance, α is the absorption coefficient, l is the light path length, and c is the concentration of absorbing species in the solution.151

### 3.4.2. Electron Microscopy

Electron microscopes, e.g., TEM and SEM, are instruments that use a beam of electrons to examine solid materials and provide the surface and internal imaging on a nanometer scale. Since their commercialization, TEM and SEM have made crucial contributions to the science and engineering of microelectronic devices, and made them indispensable tools for nanomaterials research.152

TEM. More than 70 years ago, Knoll and Ruska invented the TEM to overcome the limitations of the light microscope.152 However, the TEM had not been used for material studies until 40 years ago, when the thin-foil preparation technique was developed. More improvements of the TEM technique in the 1990s provided 0.1 nm of resolution,153 which made TEM an indispensable analysis technique for studying materials in the micron or nano size region.

When incident electrons interact with a specimen, what could be generated are X-ray, cathode luminescence and six type of electrons: (1) transmission, (2) back-scattered, (3) reflected, (4) secondary, (5) Auger and (6) trapped electrons (Figure 3.8).154 The transmission and scattered electrons are collected for TEM imaging.

Figure 3.8. Schematic: interactions of a specimen with incident electrons (redrawn from Ref. 154).

TEM is the only technique allowing a 3D observation and quantitative characterization of most kinds of lattice defects. Its high spatial resolution for orientation determination and high resolution of TEM images can be advantageous over SEM for nanomaterial analysis.155

A TEM such as Philips CM10 has a resolution of 0.5 nm, while a high resolution TEM (HRTEM), e.g., JOEL 2010, is capable of a spatial resolution of 0.194 nm and can provide images with 1024(1024 pixel resolution by using a multiscan digital camera. The diffraction patterns of HRTEM images are also very useful for studying the nanocrystalline phases of metals and nanoceramics.

SEM. Following the invention of the TEM, Knoll went on to develop the first SEM.152 Even though the SEM was invented after the TEM, the maximum resolution of SEM is never higher than that of the TEM.

In the SEM, a very fine beam of electrons with energies up to several tens keV is focused on the surface of the specimen and scanned across it in a parallel pattern. The intensity of emission of secondary and backscattered electrons is very sensitive to the angle at which the electron beam strikes the surface of the sample.  The emitted electron current is collected and amplified. The magnification produced by SEM is the ratio between the dimension of the final image display and the field scanning on the specimen. Usually, the magnification range of SEM is between 10 to 222,000 times, and the resolution is between 4 to 10 nm. The advantages of SEM include that a relatively large sample can be examined, while TEM can only examine the nanoparticles or thin layers with a thickness in nano size.

It should be mentioned that the specimen might be damaged by the electron-beam sputtering, and focusing for a long time on a small spot of the specimen should be avoided.156

Both TEM and SEM were widely used in this thesis for studying the nanostructures of metal and oxide nanomaterials.

### 3.4.3. Crystals and Powder X-Ray Diffraction

By definition, a crystal is a solid in which the constituent atoms, molecules, or ions are packed in a regularly ordered, repeating pattern extending in all three spatial dimensions. An amorphous material does not have the ordered repeating pattern; however, it may change into a crystalline material upon heat treatment. For instance, when amorphous TiO2 was heated up to 400 °C, either a rutile or an anatase crystalline phase can be formed depending on the particle size.157

Single Crystal. In a single crystal, all atoms in the crystal are related either through translational symmetry or point symmetry.

Polycrystalline Materials. Polycrystalline materials are made up of a great number of tiny ((m or nm) single crystals.

Unit cell, Tetragonal and Monoclinic

By definition, a unit cell is the smallest repeat unit of a crystal structure, in 3D, which shows the full symmetry of the structure. The unit cell is a box with three sides (a, b, c) and three angles (α, β, γ) (Figure 3.9).

Figure 3.9. Schematic of a unit cell of crystals.158

There are seven unit cell shapes: cubic, tetragonal, orthorhombic, monoclinic, triclinic, hexagonal and rhombohedral.

Tetragonal: a = b ≠ c, α = β = γ = 90°

Monoclinic: a ≠ b ≠ c, α = γ = 90°, β ≠ 90°

The perpendicular distance between pairs of adjacent planes in the crystal is the d-spacing.

For orthogonal crystal systems, i.e., α = β = γ = 90°:

(3.2)

Where, d is d-spacing; a, b, c are sides of the unit cell; h, k, and l are Miller indices, which are used to describe lattice planes and directions in a crystal. Table 3.1159 shows the crystallographic data of the rutile and anatase TiO2.

Table 3.1. Crystallographic data for rutile and anatase.

| Substance | Structure Type | Lattice Parameters (nm) | Space Group |
| --- | --- | --- | --- |
| Rutile | Tetragonal | a = b = 4.593 c = 2.959 | P42/mnm |
| Anatase | Tetragonal | a = b = 3.758 c = 9.514 | I 42/amd |

Powder X-ray Diffraction (XRD) is one of the primary techniques used to characterize solid-state materials such as metal oxides. Powder XRD can provide information about the crystalline structure in a sample even when the crystallite size is too small for single crystal x-ray diffraction.

Bragg’s Law

The X-ray diffraction of a crystal can be formulated by means of Bragg’s law (Figure 3.10):

(3.3)

where d is d-spacing,  is the incident angle, n is the layer of planes, and is the wave length of the X-rays.160

Figure 3.10. Schematic of X-ray reflection on the crystal planes.

### 3.4.4. N2 Adsorption/Desorption

N2 adsorption/desorption (physisorption) is an important method for characterization of solid-state materials to determine the surface area and pore structure.

BET Surface Area. When N2 molecules are introduced into a vacuumed system filled with the solid-state sample, the N2 molecules tend to form a thin layer that covers the entire surface of the solid. Using the Brunauer, Emmett and Teller (BET) theory, one can calculate the sample's surface area by means of multiplying the number of monolayer N2 molecules required to cover the solid surface by the cross-sectional area of the N2 molecule.

The BET equation is written as:

(3.4)

where, P and P0 are the equilibrium and the saturation pressures of adsorbates at the temperature of adsorption, υ is the adsorbed gas quantity (for example, in volume units), and υm is the monolayer adsorbed gas quantity, c is the BET constant and can be expressed as:

c = exp                                                       (3.5)

where E1 is the heat of adsorption of the first layer, and EL the heat for liquefaction.

Equation 3.4 is an adsorption isotherm and can be plotted as a straight line, called a BET plot, with P/v(P0-P) on the ordinate and P/P0 on the abscissa according to experimental results. The value of the slope and the y-intercept of the line are used to calculate the monolayer adsorbed gas quantity, vm, and the BET constant, c, respectively.161 An example of a BET plot of N2 adsorption in silica gel at 91 K is shown in Figure 3.11, from which vm and the BET constant c can be determined as 116.2 ml/g and 80.6, respectively.161

Figure 3.11.  BET plot of N2 adsorption on silica gel at 91 K. The data was obtained from Ref. 161

A total surface area (Stotal) and a specific surface area (S) can be calculated as:

(3.6)

(3.7)

where, Stotal = total surface area, N = Avogadro’s number, s = adsorption cross section, M = molecule weight of adsorbate, S = specific surface area, and a = weight of sample solid.

BJH Pore-Size Distribution and Pore Volume. According to IUPAC’s definition, the microporous, mesoporous and macroporous materials exhibit pore diameters of less than 2 nm, in the range of 2-50 nm and 50 nm, respectively.162

Addition of more N2 molecules beyond a monolayer of N2 on the surface leads to the formation of multiple layers and capillary condensation. The capillary condensation is believed to be proportional to the equilibrium gas pressure and the size of the pores inside the solid. The Barrett, Joyner and Halenda (BJH) computational method allows the determination of pore sizes from equilibrium gas pressures. The BJH method for calculation of pore size distribution is based on a model of the adsorbent exhibiting cylindrical pores.163 During desorption, a pore loses its condensed liquid adsorbates, known as the core of the pore, at a particular relative pressure related to the core radius by the Kelvin equation (Equation 3.8). After the core evaporated, a layer of adsorbate remains on the wall of the pore. The thickness of this layer can be calculated for a particular relative pressure from a thickness equation. Using this approach, the pore size distribution and pore volume of solid with various pore sizes can be determined.163

(3.8)

where, σ is the surface tension of liquid nitrogen, V is the liquid molar volume of nitrogen, rk is radius of capillary in cm, T is the absolute temperature in K, and 8.316(107 is the gas constant in ergs per degree.

Hysteresis Loops. After generation of adsorption isotherm and fulfillment of saturation, one can also generate desorption isotherms by withdrawing a known amount of gas from the system in steps. Adsorption and desorption isotherms rarely overlay each other. The resulting hysteresis leads to isotherm shapes that can be mechanistically related to those expected from particular pore shapes. Figure 3.12 shows the classification of hysteresis loops denoted as H1, H2, H3 and H4 by IUPAC. Type H1 and H2 loops were obtained from agglomerated spherical particles and corpuscular systems, respectively, while type H3 and H4 were obtained from slit-shaped pores or plate-like particles.164

Figure 3.12. Classification of hysteresis loops as recommended by the IUPAC.164

It is widely recognized that two mechanisms contribute to the sorption hysteresis that is observed in experimental measurements on mesoporous solids.165 The first mechanism, the single-pore mechanism, is purely thermodynamic in origin and does not relate to the interconnectivity of the pores. In the case of adsorption, the gas phase includes the adsorbed film on the pore wall at a certain pressure P*. However, it is possible for a metastable gas phase to persist beyond P* during the adsorption process, thus a higher pressure is required to reach the adsorbed volume. Similarly, a metastable liquid phase may persist below P* during desorption, thus a lower pressure is required to reach the desorbed volume.165 Due to the existence of the metastable gas or liquid, the adsorption and desorption curves cannot overlay one another, and hysteresis loops are generated. The second hysteresis mechanism is a result of the interconnectivity of the pores. During the desorption process, nitrogen can vaporize only if the pore is in direct contact with the vapor phase. If the pore is not at the surface of the adsorbent particle, nitrogen can only vaporize if an adjacent pore contains vapor.165 The more the pores connect, the smaller the hysteresis loops, and vise versa.

The relationship between the morphology of the pores and the hysteresis profile has been studied using computational simulations.166-168 Although gas adsorption techniques and the data analysis methods appear to be well established, it is still difficult to evaluate the pore structures accurately, due to the surface heterogeneity and structural heterogeneity of the solid materials.169

### 3.4.5. Thermal Analysis

Thermal analysis is an important technique for the characterization of solid-state materials, as it provides information on the physical and chemical changes involving endothermic and exothermic processes, temperatures for phase transitions, melting points and crystallization, and the weight loss when the temperature is increased.

Differential Scanning Calorimetry (DSC). DSC is a thermal analysis technique that is used to measure the heat flows associated with transitions in materials as a function of time or temperature. Such measurements provide qualitative and quantitative information about physical and chemical changes that involve endothermic processes such as melting, and exothermic processes such as crystallization, or changes in heat capacity such as at the glass transition temperature (Figure 3.13).170 DSC can determine the glass transition temperature of polymers and the phase transition temperatures of solids. This makes DSC an indispensable technique for characterization of polymer and oxide materials.

Figure 3.13. A schematic DSC curve demonstrating the appearance of glass transition, crystallization and melting.

Thermogravimetric Analysis (TGA). TGA measures any changes of the sample weight with increasing temperature. It can determine: (1) moisture/liquid content and the presence of volatile species, (2) decomposition temperatures, and (3) the rate of degradation. TGA is widely used for characterization of solid materials including polymer, organic, inorganic and composite materials. Especially, TGA can be used to determine the percentage of inorganic fillers in inorganic/polymer composites.

# Synthesis and Characterization of Silica Aerogel Particles

In this chapter, the synthesis of silica nano spherical particles by a direct sol-gel process in scCO2 is described. Part of this chapter is reproduced from the published article by the author: Synthesis and Formation of Silica Aerogel Particles By a Novel Sol-Gel Route in Supercritical Carbon Dioxide,171 with permission from the Journal of Physical Chemistry B, 108 (32), 11886-11892, Copyright [2004] American Chemical Society.

A new approach for synthesizing SiO2 nanoparticles was carried out in CO2 by polycondensation of silicon alkoxides with carboxylic acids at 40-70 °C and 1300-3000 psig. After formation of SiO2 colloidal particles in the high-pressure vessel, CO2 was vented quickly before gelation, resulting in formation of submicron SiO2 particles in the vessel. By using a nozzle, the supercritical fluid was sprayed into a collection vessel, and SiO2 nanoparticles with a diameter of about 100 nm were prepared.

## 4.1. Introduction

Because SiO2 has high-temperature stability, biocompatibility, and insulating properties, SiO2 aerogel particles have many potential applications, e.g. catalyst matrixes, chromatography resins, and precursors for ceramic powders for biomaterials.112, 172-174 An aerogel is a gel that has a lower density than the fully condensed form of the material forming it. Aerogels are typically produced by replacing the liquid of a gel by air or another gas without allowing complete collapse of the structure.175 Early work led to aerogels through the use of supercritical fluids to extract liquid, and it led to the hypothesis that the gel structure itself can be preserved in the supercritical drying process.109 SiO2 aerogels are conventionally prepared by hydrolyzing and condensing silicon alkoxides in water and/or organic solvents under ambient pressure with an inorganic acid or base as catalyst, gelating for a long time, then drying in scCO2.115, 176 A route of SiO2 aerogel particle synthesis was previously developed using formic acid to react with tetramethyl orthosilicate (TMOS) or tetraethyl orthosilicate (TEOS) in a supercritical fluid. The first monolithic SiO2 aerogel was synthesized by employing this methodology in 1997,177 and M. Moner-Girona et al.178 in 2003 who obtained micron-size spheres and fibers in supercritical acetone, but found it difficult to have separated particles in scCO2 because of agglomeration. Advantages of this route include a shorter time for gel aging, obtaining a dry product directly after CO2 venting, and the ability of the size and morphology of the SiO2 aerogel to be tailored by modifying the temperature, pressure, relative amounts of reactants, and supercritical fluid venting rate. However, the mechanism and kinetics of the reactions are not well understood.

Recent literature has shown that attenuated total reflection Fourier transform infrared (ATR-FTIR) spectroscopy is technically feasible for in situ measurement of concentration, solubility, and supersaturation in crystallization processes for the chemical and pharmaceutical industries.149, 150 The goal of the present work was: (1) to study the particle formation by means of two techniques of (a) destabilizing the sol-gel solution by pressure reduction and (b) the RESS process; (2) to investigate the technical potential and efficacy of ATR-FTIR spectroscopy for the in situ monitoring of solute concentration during the modified aerogel procedure in scCO2; and (3) to study the kinetics of the sol-gel reactions by using in situ FTIR results.

## 4.2. Experimental Details

Materials. Reagent-grade tetraethyl orthosilicate (TEOS), tetramethyl orthosilicate (TMOS), acetone (HPLC grade), acetic, benzoic acid, and chloroacetic acid were obtained from the Aldrich Chemical Co. (Ontario, Canada), and used without further purification. Formic acid (Aldrich, reagent grade) was further dehydrated by refluxing with phthalic anhydride (Sigma-Aldrich, 99% reagent grade) for 6h and then distilling. Instrument-grade carbon dioxide (99.99%) was obtained from BOC Canada and further purified by passage through columns containing molecular sieves (Aldrich) and copper (II) oxide supported on alumina (Aldrich) to remove excess water and oxygen, respectively. Purified water was produced by using a Barnstead Easypure LFsystem.

Experimental Setup.

The experimental setup was described in detail in Chapter 3. The polycondensation was carried out in both the view cells (Figure 3.2) and the reactor connected with the in situ FTIR (Figure 3.4).

Polymerization Procedure. To determine the activity of the various acids (acetic, formic, benzoic, and chloroacetic) for catalyzing the condensation reaction, 20-mL of acetone was added to all acids to aid in dissolution (benzoic and chloroacetic acid were not soluble in scCO2 without this cosolvent). The acid, cosolvent, and orthosilicate precursor were added to the autoclave before heating and addition of carbon dioxide. In the second group of experiments, the 0.176 M acid (acetic or formic) was added to the autoclave before heating and addition of carbon dioxide to the desired pressure. Then 0.044 M TEOS (or TMOS) was pumped in with a separate syringe pump. FTIR spectra were obtained in situ. After the reactions were complete, excess carboxylic acid was washed with fresh scCO2 at a fixed flow rate (≈2 ml/min). The results provided were the mean of three separate experiments (n=3), and the error bars represent the standard deviation.

Particle Formation and Collection Techniques. Two techniques for particle formation were employed. One was direct formation of particles in the stirred reactor during depressurization with a fixed CO2 venting rate. For the other one, the RESS process was used, where particles were sprayed through a variable-volume nozzle into a closed stainless steel chamber with heating jacket to collect particles sprayed at a constant depressurizing rate.

Online Characterizations. In situ FTIR monitoring of solution concentration in the stirred autoclave was performed using a high-pressure diamond immersion probe (Sentinel-ASI Applied Systems). The probe is attached to an ATR-FTIR spectrophotometer (ASI Applied Systems ReactIR 4000), connected to a microcomputer, supported by ReactIR software (ASI) (see Figure 3.7).

Product Characterization Techniques. Scanning electron microscopy (SEM) measurements were used to determine the size and morphology of particles. These measurements were made at either Surface Science Western on a Hitachi S-4500 FE instrument using an accelerating voltage of 5kV, or at the UWO Photonics and Nanotechnology Laboratory using a LEO 1530 Field Emission Scanning Electron Microscope. Solid aerogel powders were characterized by means of a Bruker Vector 22 FTIR instrument using a MIRacle Single Reflection HATR (Pike Technologies).

## 4.3. Results and Discussion

### 4.3.1. In situ FTIR Analysis of the Sol-gel Reactions.

Figure 4.1 provides a series of traces for a typical experiment in CO2 taken at fixed time intervals, from the in situ ATR-FTIR analysis of the condensation of TEOS using acetic acid. Analysis of the spectra shows that the absorptions at 1066, 923, and 796 cm-1 correspond to the stretching frequency of the Si-O-Si bond from the product,170, 179 whose absorbance increases as the reaction proceeds. The produced SiO2 aerogel powder was further analyzed by a separate offline FTIR instrument, which is designed for measuring solid materials. Figure 4.2 shows the results of this analysis, which confirm the peaks at 1066, 923, and 796 cm-1 in Figure 4.1 belong to the aerogel product, although a slight peak shift can be observed. The in situ FTIR analysis showed that the product peaks were found to increase during the course of the polymerization and then would remain constant if the reaction approached equilibrium, or the saturated concentration of polycondensate was reached. This reaction was repeated in an agitated view-cell reactor, and the solution remained clear during the course of the condensation reaction. As the condensation product is most likely polydisperse with a broad range of molecular weights, it is not possible to directly determine concentration of the molecules by FTIR, only of the actual bond concentration. Analysis of the FTIR spectrum also shows a product peak at 3344 cm-1, which increases during the course of the reaction from the production of the condensate molecule. The condensate molecule is a mixture of H2O and CH3CH2OH. Both the alcohol and water will merge into an indistinguishable broad peak in this range. More detailed in situ IR studies of the sol-gel process will be discussed in Chapter 7.

Figure 4.1. ATR-FTIR plot of the progress of an aerogel reaction in CO2, where the lines are experimental data: 4.4 mmol TEOS + 22 mmol HOAc + 4.4 mmol H2O at 3000 psig and 60 C from 1 to 7 h at 1-h intervals.

Figure 4.2. FTIR spectrum of the SiO2 aerogel powder, there are three obvious absorptions (1065, 928 and 797cm-1) in the range between 4000 and 600 cm-1 (The small absorptions at 3294 and 1709 cm-1 are due to water and acetic acid residue respectively).

### 4.3.2. Activity of Various Acids

To compare the relative activity of the various acids studied in the condensation of the orthosilicates, the main absorbance from the oxo bond at ~1065 cm-1 was plotted versus reaction time (see Figure 4.3). The results showed that among the four acids, benzoic and chloroacetic acid were the most active in promoting conversion to product. However, several problems make these acids poor candidates for the polymerization agent. First, as we will see later, slower condensation of orthosilicates is preferred to form discrete particles. Second, as both of these acids are solid at room temperature, and as they have poor solubility in CO2, this makes separation from the final product difficult. Both anhydrous acetic and formic acids were less active than the other two acids.

Figure 4.3. Effect of acid type on TEOS condensation activity in CO2. The points are experimental data from the ATR-FTIR absorbance at 1066 cm-1 (n = 3). The experimental conditions are 60 °C and 3000 psig, 0.044 M TEOS, 0.176 M acid, and 2.75 M acetone.

Figure 4.4 shows that production of the condensation product could rise remarkably by addition of (a) a small amount of water (TEOS: H2O = 1 ~ 2) or (b) more acid. NMR studies in aqueous sol-gel polymerizations show similar accelerations with increased concentrations of water.180 However, too much water was found to make the reaction rate too high, causing precipitation and agglomeration of aerogel particles. Also, too much acid is not economically feasible and causes downstream separation problems.

Figure 4.4. Effect of water and acid concentration on TEOS condensation activity in CO2. The points are experimental data from the ATR-FTIR absorbance at 1066 cm-1 (n = 3). Series 1 (♦) : 0.088 M TEOS + 0.352 M HOAc; Series 2 (■): 0.088 M TEOS + 0.352 M HOAc + 0.088 M H2O; Series 3 (▲): 0.088 M TEOS + 0.704 M HOAc. The experimental conditions are 50 °C and 3000 psig.

### 4.3.3. Effect of Temperature and Pressure

Figure 4.5 shows that higher temperatures resulted in significantly higher polycondensation rates. The rate of condensation clearly increases with temperature, indicating the dominating reaction of the sol-gel process is either an irreversible reaction or an endothermal reversible reaction.181 Figure 4.6 shows an interesting effect from experiments varying the reactor pressure. Increasing the reactor CO2 pressure caused lower initial reaction rates, but led to higher final concentrations of the product. The behavior of the curve at 1300 psig was probably due to the lower solubility of the colloidal particles when the pressure was low, which resulted in a lower absorbance of the oxo bond in the CO2 phase.

It should be noticed that the absorbance of the oxo bond peak around 1066 cm-1 is close to the TEOS peaks at 1085 and 1108 peaks, and they may overlapping with one another. This will be further discussed in Chapter 7.

Figure 4.5. Effect of temperature on TEOS condensation activity in CO2. The points are experimental data from the ATR-FTIR absorbance at 1066 cm-1 (n = 3). The experimental conditions are 3000 psig, 0.088 M TEOS, and 0.352 M acetic acid.

Figure 4.6. Effect of pressure on TEOS condensation activity in CO2. The points are experimental data from the ATR-FTIR absorbance at 1066 cm-1 (n = 3). The experimental conditions are 50 °C, 0.088 M TEOS, and 0.352 M acetic acid.

### 4.3.4. Experimental Phase Behavior

Using the view-cell system for the experimental conditions studied, it was found that TMOS, TEOS, acetone, acetic acid, and formic acid were miscible with CO2. Benzoic and chloroacetic acid had poor solubility, but were soluble in CO2 with added acetone cosolvent. When the FTIR experimental conditions were further examined by means of the view cell reactor, it was found that precipitates appeared spontaneously after the silicon alkoxide and 96% formic acid (≈ 4% water) were pressurized with CO2 and heated. Figure 4.7a shows an example of the typical agglomerated micron size spheres that were produced. The situation could be improved by adding excess formic acid as cosolvent in CO2, and by decreasing the concentration of reactants (Figure 4.7b), but precipitation of the products was still inevitable. However, when using anhydrous acetic or formic acid and small amounts of water (water/TEOS = less than 2/1), the fluid remained clear, indicating that the products remained in solution.

Figure 4.7. SEM of SiO2 aerogel powder. The experimental conditions are: (a) 1.1 mmol TEOS + 7.7 mmol 96% HCOOH in the 25-mL view cell, at 40 °C and 2000 psig; (b) 0.176 mmol TEOS + 2.64 mmol 96% HCOOH in the 25-mL view cell, at 40 °C and 2000 psig.

### 4.3.5. Particle Formation

Particles were formed either by depressurizing the reactor vessel or expanding the particles using a modified RESS process, into a heated collection chamber. When depressurizing the reactor vessel, particles would form at pressures of approximately 900 ~1000 psig. Results from the view cell observation and SEM showed that separated micro-spheres were formed when the pressure dropped to about 900 ~1000 psig. When using the modified RESS process, the particle size was found to decrease with increasing rate of depressurization and the particles were significantly smaller than those formed from depressurizing the reactor vessel. Generally, a higher venting rate made smaller particles with narrower distributions and lower levels of agglomeration. The particles gathered in the autoclave, spheres in the range between submicron and several microns in diameter (Figure 4.8a), were larger than those formed in the device outside the autoclave by the RESS process (with approximate diameters of 100 nm) (Figure 4.8b).

Figure 4.8. SEM of SiO2 aerogel powder: (a) collected from the high pressure mixer upon decompression. The experimental conditions are 0.044 M TEOS + 0.176 M HOAc, at 60 °C and 3000 psig; (b) collected using the Rapid Expansion of Supercritical Solutions (RESS) process. The experimental conditions are 0.044 M TEOS + 0.176 M HOAc, at 60 °C and 6000 psig.

## 4.4. Conclusions

This study of the particle formation process for aerogels in CO2 demonstrated that in situ ATR-FTIR spectroscopy is a valuable technique for studying this high-pressure process. Both anhydrous formic and acetic acid were found to be mild and controllable agents for sol-gel route preparation of SiO2 aerogel particles in CO2. By modifying the ratio of silicon alkoxide, acetic acid, and water, the polymerization rate is tunable and precipitation can be prevented, and therefore agglomeration minimized. Increasing the reaction temperature led to higher rates of reaction and increasing the pressure decreased the rate of reaction. Submicron particle sizes were obtained when the sol-gel solution was destabilized by pressure reduction. Particles as small as 100 nm were formed using the RESS process.

# Synthesis and Characterization of Titania Nanofibers and Nanospheres

This chapter is reproduced from a letter and an article by the author: Formation of Titania Nanofibers: A Direct Sol-Gel Route in Supercritical CO2, and FTIR Study on the Formation of TiO2 Nanostructures in Supercritical CO2, with permission from Langmuir, 21 (14) 6150-6153, and the Journal of Physical Chemistry B, 110 (33), 16212-16218, respectively, Copyright [2005-6] American Chemical Society.

This chapter describes a new method to synthesize titania aerogel composed of nanofibers or nanospheres via a sol-gel route in CO2. The aerogel was formed by polycondensation of titanium alkoxides using acetic acid as the polymerization agent in CO2 at 40-70 °C and 2500-8000 psig. The TiO2 morphology was characterized by means of SEM and HRTEM. Depending on experimental conditions, TiO2 anatase nanospheres with a diameter of 20 nm, or TiO2 anatase/rutile nanofibers with a diameter of 10 to 100 nm were obtained. N2 physisorption and powder XRD showed that the nanofibers exhibited high surface areas up to 400 m2/g, and anatase and/or rutile nanocrystallites were formed after calcination.

It was found that fiber formation was enhanced by a higher HOAc/Ti ratio, and the use of the titanium isopropoxide (TIP) precursor. The mechanism of the microstructure formation was studied using in situ FTIR analysis in CO2. The FTIR results indicated that the formation of nanofibers was favored by a titanium hexamer that leads to one-dimensional condensation, while nanospheres were favored by a hexamer that permits three-dimension condensation.

## 5.1. Introduction

### 5.1.1. Applications of TiO2 Aerogel and TiO2 Nanomaterials

TiO2 aerogel is a material with significant potential for many applications. As examples, it can be used as a ceramic material,182 an opacifier in dental filler,183, 184 a bone filler,185 a construction ceramic in nanofiltration membranes,186  an anion- and cation-exchange packing material for ion chromatography,187 a catalyst support for oxides and group VIII metals,20, 188-190 a photocatalyst,25, 191-195 a semiconductor for dye-sensitized solar cells (DSSCs) and other applications.196-202 Particularly, TiO2 has been of great interest for energy conversion and photocatalysis since the discovery of its ability for photoelectrolyzing water to produce hydrogen.203 Many efforts were focused on decreasing the band gap energy of TiO2 (3.2 eV) into the sunlight spectrum (0.5 ~2.9 eV) by synthesizing new nanoarchitectures and transition-metal-doped, oxide-coated or nitrogen-doped TiO2.204-207 TiO2 and hybrid TiO2 nanoarchitectures have been extensively prepared by using hydrolytic208, 209 or nonhydrolytic210, 211 sol-gel routes.

### 5.1.2. TiO2 Synthesis Method

The formation of mesoporous materials as thin films, fibers, spheres or monoliths is of great interest with regard to various applications.212 Titania materials with a variety of morphologies have been reported. Mesoporous powder or film was synthesized via a templating route213-216 or a non-templating route;217 nano-aerogel particles were obtained by stabilizing with surfactants;53 micron size TiO2 fibers were manufactured using electrostatic deposition;218 hollow fibers were produced by electrospinning two immiscible liquids through a coaxial, two-capillary spinneret;219 TiO2 pillared clay structure was developed using scCO2;139 unsupported large-area membranes were also fabricated.220 However, the formation of sol-gel-derived pure TiO2 monolith is rarely reported.221 The reason is that pure TiO2 aerogel is extremely brittle and fluffy. This makes it unsuitable for catalyst supports.95, 222 To solve this problem, TiO2 was either grafted onto other oxides, i.e., SiO2 or Al2O3, to form a composite monolith,223 or was mixed with water into a paste, extruded and calcined to form a hardened extruded catalyst support.224 Suh et al. believed that the brittleness of TiO2 aerogel was due to the fast hydrolysis of titanium precursor and the destabilization of the alcogel.225

The conventional sol-gel route of TiO2 synthesis involves wet-chemistry: dissolving of titanium alkoxide in alcohol and a stabilization agent, controlled hydrolysis of the metal alkoxide with a limited amount of water and a catalyst, i.e. an acid or a base, condensation into polymers, forming colloidal particles sol and three-dimension network wet gel, aging, extraction of alcohol by supercritical fluid, and calcination.226

Since titanium alkoxides are very active with water and tend to form precipitate, they were modified by acetic acid before addition of water to control the reaction rate in the conventional sol-gel route.227, 228 It was believed that a coordination bond was formed between the titanium and the acetate group, so as to decrease the hydrolysis activity.

### 5.1.3. Ti-Carboxylate Complex

Ti(VI) is known to be able to form acetate complexes. In the complex, the acetate can potentially coordinate with the metal as a chelating, bridging bidentate or monodentate (Figure 5.1 a, b, and c respectively).229 FTIR is an established technique for analyzing the complexes of metal carboxylate species.230 During in situ FTIR interpretation, we took many benefits from the reports of the synthesis and analysis of Ti-carboxylate complexes in conventional media using single-crystal XRD and IR techniques. Nakamoto and Deacon et al. summarized the IR studies of a variety of metal-acetate complexes having known X-ray crystal structures.229, 230 Figure 5.1 d and e show two examples of titanium hexamer complex structures determined by single crystal XRD.231 The bridging acetate exhibited peaks at 1600, 1580, 1555 and 1445 cm-1 from rutilane shape Ti6O4(OBun)8(OAc)8 1,232 and at 1603 and 1548 cm-1 from hexaprismane shape Ti6O6(OPri)6(OAc)6 2.233 By reacting titanium isopropoxide with a lower amount of acetic acid (with the molar ratio of HOAc/alkoxide = 1.33:1) in CO2, an additional two crystals were also synthesized: 2 and rutilane shape Ti6O4(OPri)8(OAc)8 3.234 The single crystal 2 exhibited peaks of bridging acetate at 1604, 1543 and 1458 cm-1, and 3 showed peaks at 1581, 1560, 1452 and 1410 cm-1. The IR results of the crystals, as summarized in Table 5.1, are important for understanding the formation of TiO2 nanoarchitecture as described later.

Figure 5.1. Reported structures of TA oligomers with acetate ligands: (a) chelating bidentate; (b) bridging bidentate; (c) monodentate; (d) Ti6O4(OBun)8(OAc)8, rutilane shape; (e) Ti6O6(OPri)6(OAc)6, hexaprismane shape.   (a) ~ (c), Ref.229; (d) and (e) images were modified from Ref.231. The black balls stand for Carbon, the red ones stand for Oxygen, Titanium is in the middle of the octahedrons.

Table 5.1. IR absorption peaks corresponding to COO-1 stretching vibration in various acetates.

| Ti-acetate coordination | νsym(COO) cm-1 | νasym(COO) cm-1 | Ref. |
| --- | --- | --- | --- |
| 1, Ti6O4(OBun)8(OAc)8, rutilane shape | 1445 | 1600, 1580, 1555 | 232 |
| 2. Ti6O6(OPri)6(OAc)6, hexaprismane shape |  | 1603, 1548 | 233 |
|  | 1458 | 1604, 1543 | 234 |
| 3. Ti6O4(OPri)8(OAc)8, rutilane shape | 1452, 1410 | 1581, 1560 | 234 |

## 5.2. Experimental Details

### 5.2.1. Materials

Reagent grade 97% titanium (IV) butoxide (TBO), 97% titanium (IV) isopropoxide (TIP), 99.7% acetic acid, from the Aldrich Chemical Company, were used without further purification. Instrument grade carbon dioxide (99.99%) was obtained from BOC Canada.

### 5.2.2. Experimental Setup

The synthesis of titania nanomaterials was carried out in the 25 mL or 10 mL view cell, or in the 100 mL autoclave equipped with in situ FTIR, as described in Chapter 3.

### 5.2.3. Preparation of TiO2 Nanoparticles

In a typical experiment, titanium alkoxide (TA) was quickly placed in the view cell, followed by addition of acetic acid and CO2 up to the desired temperature and pressure. A magnetic stirrer system was used for mixing the reaction mixture. An amber transparent homogeneous phase was formed at the specified temperature and pressure (Figure 5.2a). The fluid in the view cell became semi-transparent and turned to dark red (Figure 5.2b) after stirring the reaction mixture from several hours to several days, just before gelation into a white gel. After at least 72 hours of aging, a few venting droplets were placed in a test tube, followed by addition of water and nitric acid. If there was no precipitate formed, this indicated the complete polymerization of TA. In order to remove the unreacted acetic acid and condensation byproducts, i.e. alcohol, ester and water from the gel formed in the view cell, a CO2 wash was conducted. To prevent collapse of the gel network, both the CO2 wash and CO2 venting were conducted carefully in a controlled manner by means of the pneumatic control valve that was fine tuned by the LabView virtual instrument. During the CO2 wash, the syringe pump was operated in a constant flow manner at a rate of 0.5 ml/min until the pump was empty. The pressure of the view cell was maintained at ≈ 6500 psig. When the pump was empty, the pneumatic valve would shut off automatically. The pump was refilled and pressurized to 6500 psig and operated with constant-flow mode again. After the supercritical drying process was finished, CO2 was released gradually by decreasing the pressure in a controlled manner.

Figure 5.2. Photographs following the reaction in the view cell: (a) start of the reaction; (b) the moment directly proceeding gel-formation.

The prepared TiO2 aerogel was further dried at 120 (C under a vacuum of 508 mmHg for 24 hours, then calcined in air at the desired temperature for 2 hours with a ceramic crucible in a programmable furnace (Thermolyne 1500). The heating rate for each calcination temperature was 10 (C per minute to the set point. The holding time was 2 hours, and the cooling rate to room temperature was 0.5 (C per minute.

### 5.2.4. Characterization

FTIR. In situ FTIR monitoring of solution concentration in the stirred autoclave was performed using a high-pressure diamond immersion probe (Sentinel-ASI Applied Systems). The probe is attached to an ATR-FTIR spectrometer (ASI Applied System ReactIR 4000), connected to a computer, supported by ReactIR software (ASI). The spectra were collected automatically within the reaction time with specified intervals.

Solid TiO2 aerogel powder was characterized by means of a Bruker Vector 22 FTIR instrument using a MIRacle Single Reflection HATR (Pike Technologies). The samples were finely ground before FTIR examination.

Thermal analysis. DSC and TGA analysis were performed on a Mettler Toledo DSC822e and TGA/SDTA851e, respectively, at a heating rate of 10 (C/min in nitrogen.

XRD. Powder XRD was performed either on Bruker D8 Discover Diffractometer with GADDS employing CuKα radiation or on Rigaku-Geigerflex CN2029 employing CuKα1 + Kα2 radiation with a power of 40kV×35mA for the crystalline analysis. The samples were finely ground and spread on a glass substrate.

N2 physisorption. Brunauer-Emmett-Teller (BET) surface area, pore size and distribution were obtained on Micromeritics ASAP 2010 at 77 K. Prior to the N2 physisorption, a sample was crushed into small pieces (without grinding) and degassed at 200 (C under vacuum.

SEM. SEM micrographs were recorded using either a LEO 1530 or Hitachi S-4500 FE. The samples were crushed (without grinding) and spread on a carbon substrate without gold coating unless specified.

TEM. TEM images and electron diffraction patterns were measured using either a JEOL 2010 operated at 200 kV or Philips CM 10 at 80 kV. The specimens were previously finely ground and then dispersed in distilled water with the help of ultrasonic vibration. A drop of water with dispersed TiO2 powder was placed on a copper grid covered with Formvar® or carbon and dried in the air.

## 5.3. Results and Discussion

# Either a white opaque monolith with low density (Figure 5.3a) or cracked translucent monoliths with higher density (Figure 5.3b) were formed in the view cell after CO2 venting. The SEM showed that the low-density monolith was composed of nanofiber clusters and the high-density monoliths were composed of nano-spherical particles as described in the SEM result section. Both the low-density monolith and the high-density monolith were easy to be ground into separate fine particles in micron size.

Figure 5.3. Photographs: (a) the low-density monolith, and (b) the cracked high-density monoliths.

# A conversion of 98% was obtained when the reaction was complete based on the amount of starting TA and the weight of calcined TiO2 at 500 °C. Determined by the monolith volume and weight, the typical aerogel apparent densities were approximately 0.13 and 0.20 g/cm3 for the ‘low-density’ monolith and ‘high-density’ monolith, respectively. There were two factors that affected the density. First, a higher initial concentration of the alkoxide was used for synthesizing the high-density monolith than that used for the low-density one. Second, upon scCO2 extraction and drying, the low-density monolith did not shrink, while the high-density monolith shrank noticeably. This can be explained by the microstructure of the aerogels. As described later, the low-density monoliths were composed of randomly-oriented nanofibers and bundles, which were hard to shrink upon drying; while the high-density monoliths were comprised of nanospherical particles, which were easier to shrink by decreasing the interstitial space when the gel was dried. Both the low-density and higher-density monoliths were fragile and easy to be crushed into a fine white powder.

### 5.3.1. N2 Adsorption/Desorption

The N2 adsorption/desorption technique was employed to study the surface area and the pore structure. The average BET surface area, the single point adsorption total pore volume per gram, and the adsorption average pore diameter (4V/A by BET) of the aerogels formed under different synthesis conditions are summarized in Table 5.2.

Table 5.2. Results of the reaction of TBO with acetic acid in CO2.

| Sample | Precursor | Co a (mol/L) | HOAc/TA b | Tre c | Pre d | Tcalc e | Sbet f | Dpore g | VPore h | Microstructure | Morphology |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | (mol/mol) | ((C) | (psig) | ((C) | (m2/g) | (nm) | (cm3/g) |  |  |
| TiO2-1 | TBO i | 1.5 | 4.2 | 40 | 6000 | N/A | 484 | 6.3 | 0.76 | 20nm spheres | High-density Monolith |
|  |  |  |  |  |  | 380 | 123 | 14.3 | 0.44 |  |  |
|  |  |  |  |  |  | 500 | 74 | 14.5 | 0.27 |  |  |
|  |  |  |  |  |  | 600 | 62 | 14.7 | 0.22 |  |  |
| TiO2-2 | TBO | 1.5 | 4.2 | 50 | 6000 | N/A | 458 | 7.2 | 0.74 |  |  |
|  |  |  |  |  |  | 380 | 114 | 14.6 | 0.42 |  |  |
| TiO2-3 | TBO | 1.5 | 4.2 | 60 | 6000 | N/A | 511 | 9.6 | 1.22 |  |  |
|  |  |  |  |  |  | 300 | 309 | 10.4 | 0.8 |  |  |
|  |  |  |  |  |  | 380 | 135 | 20.9 | 0.7 |  |  |
| TiO2-4 | TBO | 1.5 | 4.2 | 70 | 6000 | N/A | 285 | 8.3 | 0.59 |  |  |
|  |  |  |  |  |  | 300 | 241 | 9.2 | 0.55 |  |  |
|  |  |  |  |  |  | 380 | 101 | 11.6 | 0.3 |  |  |
| TiO2-5 | TBO | 1.5 | 4.2 | 60 | 4000 | N/A | 642 | 6.6 | 1.1 |  |  |
|  |  |  |  |  |  | 380 | 102 | 10.0 | 0.25 |  |  |
| TiO2-6 | TBO | 1.5 | 4.2 | 60 | 5000 | N/A | 416 | 6.1 | 0.64 |  |  |
|  |  |  |  |  |  | 380 | 135 | 12.4 | 0.42 |  |  |
| TiO2-7 | TBO | 1.5 | 4.2 | 60 | 7000 | N/A | 327 | 2.3 | 0.45 |  |  |
|  |  |  |  |  |  | 380 | 191 | 10.3 | 0.49 |  |  |
| TiO2-8 | TBO | 1.1 | 4.0 | 40 | 6000 | N/A | 228 | 2.0 | 0.12 |  |  |
|  |  |  |  |  |  | 380 | 39 | 4.5 | 0.044 |  |  |
| TiO2-9 | TBO | 1.1 | 4.5 | 40 | 6000 | N/A | 590 | 2.98 | 0.44 |  |  |
|  |  |  |  |  |  | 380 | 144 | 5.22 | 0.19 |  |  |
| TiO2-10 | TBO | 1.1 | 5.0 | 40 | 6000 | N/A | 404 | 2.3 | 0.23 | 1(m rods | Powder |
|  |  |  |  |  |  | 380 | 68 | 4.5 | 0.076 |  |  |
| Sample | Precursor | Co a (mol/L) | HOAc/TA b | Tre c | Pre d | Tcalc e | Sbet f | Dpore g | VPore h | Microstructure | Morphology |
|  |  |  | (mol/mol) | ((C) | (psig) | ((C) | (m2/g) | (nm) | (cm3/g) |  |  |
| TiO2-11 | TBO | 1.1 | 5.5 | 40 | 6000 | N/A | 380 | 3.7 | 0.35 | 80nm fibers | Low-density Monolith |
|  |  |  |  |  |  | 380 | 105 | 8.7 | 0.23 |  |  |
|  |  |  |  |  |  | 500 | 83 | 11.1 | 0.19 |  |  |
|  |  |  |  |  |  | 600 | 61 | 13.2 | 0.14 |  |  |
| TiO2-12 | TIP j | 1.5 | 4.2 | 40 | 6000 | N/A | 436 | 5.8 | 0.63 | 10nm fibers |  |
|  |  |  |  |  |  | 380 | 176 | 9.6 | 0.42 |  |  |
| TiO2-13 | TIP | 1.5 | 4.2 | 60 | 6000 | N/A | 415 | 3.8 | 0.39 |  |  |
|  |  |  |  |  |  | 380 | 185 | 8.8 | 0.35 |  |  |
|  |  |  |  |  |  | 500 | 77 | 11.3 | 0.22 |  |  |
|  |  |  |  |  |  | 600 | 65 | 14 | 0.15 |  |  |
| TiO2-14 | TIP | 1.5 | 4.2 | 70 | 6000 | N/A | 383 | 2.7 | 0.26 |  |  |
|  |  |  |  |  |  | 380 | 109 | 6.2 | 0.17 |  |  |
| TiO2-15 | TIP | 1.5 | 4.2 | 60 | 4000 | N/A | 387 | 5.3 | 0.52 |  |  |
|  |  |  |  |  |  | 380 | 232 | 7.4 | 0.43 |  |  |
| TiO2-16 | TIP | 1.5 | 3.0 | 60 | 6000 | N/A | - | - | - | Curled 10 nm fibers |  |
|  |  |  |  |  |  | 380 | 192 | 4.8 | 0.23 |  |  |
| TiO2-17 | TIP | 1.5 | 3.5 | 60 | 6000 | N/A | - | - | - |  |  |
|  |  |  |  |  |  | 380 | 164 | 7.5 | 0.31 |  |  |
| TiO2-18 | TIP | 1.1 | 5.5 | 60 | 6000 | N/A | - | - | - | Straight 40nm fibers |  |
|  |  |  |  |  |  | 380 | 133 | 8.0 | 0.27 |  |  |
| TiO2-19 | TIP | 1.1 | 5.5 | 60 | 4000 | N/A | - | - | - |  |  |
|  |  |  |  |  |  | 380 | 281 | 5.7 | 0.4 |  |  |
| Note: a: concentration of titanium alkoxide; b: molar ratio of acetic acid over the alkoxide; c: reaction temperature; d: reaction pressure; e: calcination temperature; f: BET surface area; g: adsorption average pore diameter (4V/A by BET); h: single point adsorption total pore volume per gram; i: titanium butoxide; j: titanium isopropoxide. |

The as-prepared aerogels (TiO2-1 to –15), which were amorphous as described later, exhibited a high BET surface area of 228 ~ 642 m2/g. After calcination at 380 (C for two hours in air, the surface area of the aerogels decreased to 101 ~ 281 m2/g, except TiO2-8 and –10 which are 39 and 68 m2/g, respectively. The surface areas of TiO2-1, -11 and –12 dropped into 74 ~ 83 m2/g after calcination at 500 (C and into 61 ~ 65 m2/g after calcination at 600 (C. The quick decrease of the surface area is due to the fusion of the solid face and losing of the micropores during heat treatment, as shown later in the isotherm curves.

The pore diameters of the as-prepared materials were in the range of 2.0 ~ 9.6 nm, and increased to 4.5 ~20.9 nm after heat treatment at 380 (C. The pore volumes of the as-prepared materials were in the range of 0.12 ~ 1.22 cm3/g, and dropped to 0.044 ~ 0.8 cm3/g after calcination at 380 (C.

The resulting TiO2 exhibited a Type IV adsorption isotherm (see Figure 5.4), indicating the existence of mesopores.164 The high-density monoliths exhibited H3 hysteresis loops, indicating the existence of agglomerated spherical particles.164 Figure 5.4 shows the isotherms of the TiO2-1 samples without and with calcination at different temperatures. The hysteresis loop (a) from 0.45 to 0.80 P/P0 is likely due to the mesopores inside the particles, and the loop from 0.8 to 1.00 P/P0 is assigned to the interstitial porosity due to the agglomeration of the nanoparticles.164 From the as-prepared isotherm, it seems that the mesopores inside the particles made a significant contribution. When curve (a) and (b) are compared, it is observed that the hysteresis loop between 0.4 and 0.7 disappeared after heat treatment at 380 (C. This indicates that the hysteresis loop contributed by the mesopores disappeared after calcination at 500 and 600 (C, the loop less than 0.80 P/P0 disappeared, indicating further loss of the mesopores inside the nanoparticles. The isotherm plots of the TiO2 aerogels, before and after calcination at different temperatures, showed that the H3 hysteresis loop moved to a higher relative pressure with increased calcination temperature, indicating a larger average pore size was generated.

Figure 5.4. Isotherms of TiO2-1 high-density monolith: (a) as-prepared and calcined at (b) 380 °C, (c) 500 °C, and (d) 600 °C.

The low-density monoliths also exhibited H3 hysteresis loops. Figure 5.5 shows the isotherms of TiO2-13 samples without and with calcination at different temperatures. Again, the H3 hysteresis loop from 0.2 to 0.8 P/P0 is due to the mesopores inside the particles (fibers in this case), and the loop from 0.8 to 1 P/P0 is assigned to the interstitial porosity due to the agglomeration of the nanofibers. Like Figure 5.4, after heat treatment at 380 and 500 (C, the hysteresis loop became narrow; after calcination at 600 (C, the loop at less than 0.80 P/P0 disappeared, indicating loss of the mesopores inside the nanoparticles.

Figure 5.5. Isotherm: TiO2-13 low-density monolith. (a) as-prepared and calcined at (b) 380 °C, (c) 500 °C, and (d) 600 °C.

### 5.3.2. SEM

The microstructure of the TiO2 aerogels was carefully examined by means of SEM. The morphology and the size of the nanoparticles were summarized in Table 5.2. The high-density monoliths were found to be composed of nanospherical particles with a diameter of 20 ~ 30 nm, while the low-density monolith was composed of nanofibers with a diameter of 10 ~ 80 nm and a length in the micron range. While the ratio of HOAc/alkoxide has a significant effect on the morphology and size of the aerogel particles, the reaction temperature and pressure show a rather insignificant effect.

The reaction temperature’s effect on the morphology of the aerogel was studied by varying the temperature from 40 to 70 (C, while maintaining the pressure at 6000 psig, the initial concentration of TBO at 1.5 mol/L, and HOAc/alkoxide ratio at 4.2, as shown in Table 5.2 TiO2-1~4. In this temperature range, high-density monoliths composed of spherical particles with a diameter of ca. 20 nm were obtained. The results show that temperature has no obvious effect on the morphology and the size of the aerogel. This is also true when using TIP as the precursor. TiO2-12~14 were prepared at the temperature range of 40 ~ 70 (C, while the other synthesis parameters remained constant, and low-density monoliths composed of fibers with a diameter of 10 nm were obtained.

The reaction pressure’s effect on the morphology of the aerogel was studied by varying the pressure from 4000 to 7000 psig, while keeping the temperature at 60 (C, the initial concentration of TBO at 1.5 mol/L, and HOAc/alkoxide ratio as 4.2, as shown in Table 5.2 TiO2-5~7. In this pressure range, the high-density monoliths composed of spherical particles with a diameter of ca. 20 nm were obtained. When using TIP as the precursor, the pressure was varied from 4000 to 6000 psig while the other synthesis conditions remained constant, no change of the morphology and size was observed, as shown by TiO2-18~19 in Table 5.2.

The ratio of acetic acid/titanium alkoxide has a significant effect on the morphology of the resulting aerogels. Keeping the initial TBO concentration at 1.1 mol/L, the temperature at 40 (C and the pressure at 6000 psig, and varying the HOAc/alkoxide ratio at 4.0, 4.5, 5.0 and 5.5 (mol/mol) resulted in formation of 20 nm spheres, 20 nm spheres, 1 (m rods and 80 nm fibers, respectively (see TiO2-8 ~11 in Table 5.2). When using TIP as the precursor, and the HOAc/alkoxide ratio was varied from 3.0 to 5.5 while the other synthesis conditions remained constant, curled 10 nm fibers and straight 40 nm fibers were obtained (see TiO2-16~18 in Table 5.2). The mechanism of nanostructure formation will be discussed in section 5.3.7.

TiO2 Spheres. Both the as-prepared and the calcined high-density TiO2 monoliths were examined by SEM, and were found to be composed of agglomerated spherical particles. At low magnification, the surface of the high-density monoliths looks rough, even though it looks very smooth by eye. Figure 5.6a shows the surface of a small piece of high-density monolith under a magnification of 4.86 K. At a higher magnification of 67 K, however, it can be observed that the high-density monoliths, either the as-prepared or the calcined TiO2, were composed of fused nano spherical particles, which have an identical diameter of about 25 nm (Figure 5.6b). Here we can also observe the interstitial space between the particles. This agrees with the N2 physisorption isotherms, as described earlier. Also, the nanoparticles seem to be loosely attached, which explains why the monolith can be easily crushed and ground into a fine powder. The powder can be dispersed in anhydrous organic solvents with ultrasonic, so that separate TiO2 nano spherical particles can be obtained.

Figure 5.6. SEM: (a) TiO2-1 monolith at low magnification, and (b) at high magnification. The sample was calcined at 500 °C. The arrows indicate where the mesopores are present.

TiO2 Nanofibers.

Contrasting to the microstructure of the high-density monolith, the low-density monolith is composed of nanofiber clusters. Figure 5.7 reveals the microstructures of the as-prepared TiO2-11 by increased magnification. At low magnification, the monolith looks very porous (Figure 5.7a). At high magnification, the nanofibers with a diameter less than 100 nm are loosely contacted with each other. If the synthesis process was well controlled, especially with caution taken during the CO2 extraction and venting steps, the low-density monoliths exhibited a well-defined nanofiber structure under the SEM.

Figure 5.7. SEM of as-prepared TiO2-11 monolith at increasing magnification: (a) 50 times; (b) 100 times; (c) 1,000 times and (d) 10,000 times. The arrow indicates where the macropores are present.

SEM images showed that the nanofibers did not break, even after heat treatment at 800 °C for 2 hours. After heat treatment in the temperature range from 300 to 800 °C, no obvious morphology change can be observed by using SEM at low magnification. Under high magnification, however, the calcined TiO2 nanofibers were composed of connected beads, which is different from the relatively smooth surface of the as-prepared TiO2 nanofibers (Figure 5.8a and b). It should be noted that the nanofibers described above were synthesized from TBO. By using TIP instead of TBO as the polymerization precursor, TiO2 nanofibers with a smaller diameter were obtained. Under a low magnification, the aerogel looks like coral (Figure 5.8c). Under a higher magnification, very fine fibers can be observed (Figure 5.8d). The fine fibers form clusters and the clusters are connected with each other to form the monolith. The mechanism of the morphology change will be discussed in section 5.3.6.

Figure 5.8. SEM: (a) as-prepared TiO2-11; (b) TiO2-11 calcined at 380 °C (the sample was coated with gold to prevent charging); (c) TiO2-13 nanofiber clusters under a low magnification; and (d) TiO2-13 nanofiber clusters under a high magnification.

It was found that the HOAc/TIP ratio has an effect on the morphology and diameter of the nanofibers. An increasing HOAc/TIP ratio resulted in formation of straight fibers with a larger diameter of 40 nm (Figure 5.9a). A decreasing HOAc/TIP ratio resulted in formation of curled fibers with a smaller diameter (Figure 5.9b).

Figure 5.9. SEM: (a) TiO2-18 nanofibers with a diameter of 40 nm, calcined at 380 °C; (b) TiO2-17 curled nanofibers, calcined at 380 °C.

TiO2 Rods. The aerogel derived from TBO (TiO2-10) was composed of rods with a diameter of about 1 μm (Figure 5.10a). The surface of the rods is revealed under a higher magnification (Figure 5.10b). It appears that the nanospheres were fused together forming the rods.

Figure 5.10. SEM. The TiO2-10 rods calcined at 380 °C: (a) at a low magnification, and (b) at a high magnification.

As described earlier in the experimental section, complete condensation, so-called aging, is required to achieve desired microstructure. If the condensation is not complete, unreacted titanium alkoxide will be removed while venting CO2, and a mixture of fiber-like bundles and chunks will be produced (Figure 5.11).

Figure 5.11. SEM. The result of scCO2 drying before the complete condensation.

In order to study the effect of CO2 on the formation of the microstructures, the synthesis was also carried out under similar conditions using isopropanol as solvent, instead of CO2, and a sheet-like structure was obtained without scCO2 drying (Figure 5.12). This result shows that CO2 takes a critical role in the formation of nanofibers.

Figure 5.12. TiO2 synthesized in isopropanol. The synthesis condition: the initial concentration of TIP = 1.1 mol/L, HOAc/alkoxide molar ratio = 5.5, 60 (C. Scale bar: 200 nm.

### 5.3.3. TEM

Different from SEM images that “scan” the specimen and only provide surface information of the nanomaterials, TEM images can provide more details about the microstructure underneath the surface, and as important, the crystal information.

Figure 5.13 shows the TEM image of TiO2-1 calcined at 380 °C at a low magnification. Both the crystalline and amorphous phases can be observed. HRTEM of the sample provides the reflection pattern of the crystalline phase (Figure 5.20). The d-spacing of 0.35 nm indicates that the (101) lattice plane of anatase is present.235

Figure 5.13. TiO2-1 nano spherical particles calcined at 380 °C: (a) TEM and  (b) HRTEM.

Figure 5.14a shows the TiO2 nanofibers with a diameter of 80 nm, which were calcined at 380 °C. The connection between beads can be clearly observed. Figure 5.14b shows the TEM of TiO2 nanofibers with a diameter of 10 nm, in which, connected beads can also be observed. Figure 5.14c shows the HRTEM of the TiO2 nanofibers with a diameter of 10 nm, in which the reflection pattern of anatase can again be observed. Figure 5.14d shows the TEM image of the straight fiber with a diameter of 40 nm. Different from Figure 5.21 ~ 5.23, the fibers are straight and they are not composed of beads. Furthermore, the white spots in the fiber show the presence of mesopores.

Figure 5.14. TEM and HRTEM images: (a) TiO2-11 nanofibers calcined at 380 °C; (b) TEM of TiO2-13 nanofibers calcined at 380 °C; (c) HRTEM of TiO2-13 nanofibers calcined at 380 °C; and (d) TEM of TiO2-18 nanofibers calcined at 380 °C.

### 5.3.4. Thermal Analysis

DSC. The DSC analysis on the TiO2 synthesized under different reaction temperatures showed that the reaction temperature had an effect on the aerogel thermal properties. The TiO2 synthesized under a temperature range of 40 ~70 ºC, while other synthesis parameters remained constant, were characterized with DSC. Figure 5.15 shows the thermal behavior of fresh titania aerogels of TiO2-1, -2, -3 and –4, prepared with the initial TBO concentration = 1.5 mol/L, HOAc/alkoxide = 4.2 (mol/mol) at 6000 psig. The endothermal peaks at 100 and 350 °C are due to the evaporation of the organic liquid trapped in the pores and decomposition of the organic groups, respectively. The exothermal peaks are due to the formation of the crystalline phases. The DSC curves at the temperature range of 300 ~ 370 °C are quite complicated due to the formation of the crystalline phase and the quick decomposition at the temperature range, as described later.

Figure 5.15. DSC of TiO2-1, -2, -3, -4 aerogels synthesized at 6000 psig and different temperature (a) 40 °C; (b) 50 °C; (c) 60 °C; (d) 70 °C. The initial concentration of TBO: 1.48 mol/L, acetic acid/HOAc: 4.15.

From this figure, it is observed that, at 300 °C, the aerogels synthesized at 70 °C (curve d) released more energy compared with those synthesized at lower temperatures, suggesting the formation of more crystallites. The powder XRD results support the DSC results. While the TiO2-1, -2 and –3 remained amorphous after calcination at 300 °C, TiO2-4 exhibited the anatase phase after heat treatment at 300 °C. This result suggests that a lower calcination temperature could be used to obtain the TiO2 crystalline phase, by means of using a higher reaction temperature.

As described by Jensen, research was carried out to synthesize TiO2 crystals at low temperature, which simplified the synthesis process and required less energy.142

Although calcination is still necessary for crystallization of the TiO2 spheres and fibers, it is encouraging to see that the calcination temperature could be decreased significantly when the reaction temperature was raised.

TGA.

When the temperature increases, the weight loss of the as-prepared titania aerogel provides information about evaporation of the moisture and decomposition of the aerogel that contains organic groups. A typical TGA result is shown in Figure 5.16. The TGA curve can be divided into 5 sections. From 25 to 90 °C, the curve was flat, indicating no significant organic solvents in the sample. In the temperature region of 90 ~190 °C, a small slope of weight loss is shown, probably due to evaporation of the entrapped water and acetic acid, and decomposition of some organic groups such as the ending alkoxide groups that are easy to be removed. The slope becomes larger in the temperature range of 190 ~ 310 °C and reached its maximum at 310 ~ 370 °C, probably due to the decomposition of acetate bidentate groups. It becomes flat again after the temperature is over 400 °C. The TGA result agrees with the DSC observations.

Figure 5.16. TGA of as-prepared TiO2-11.

### 5.3.5. XRD

The wide-angle powder XRD results showed that the crystalline phase in the TiO2 is particle-size dependent. A larger nanoparticle size facilitated the formation of rutile nanocrystallites, while a smaller nanoparticle size favored the formation of anatase phase. Figure 5.17 shows the XRD patterns of the TiO2 nano spherical particles (with a diameter of 20 ~30 nm) that were synthesized at 60 or 70 °C and calcined at temperature of 300, 380, 500 and 600 °C.

Figure 5.17. XRD: amorphous, anatase (a) and rutile (r) phases of the TiO2 mono spherical particles calcined at different temperatures. (A). TiO2-4 synthesized at 70 °C calcined at 300 °C; (B) TiO2-3 synthesized at 60 °C and calcined at 300 °C (B), 380 °C (C), 500 °C (D) and 600 °C (E). The initial concentration of TBO: 1.5 mol/L, acetic acid/HOAc: 4.12, pressure: 6000 psig.

A pure anatase phase could be observed from the TiO2 calcined at 380 and 500 °C. From the sample calcined at 600 °C (Figure 5.17), besides 93.8 % of anatase, 6.2 % of rutile could be observed. The percentage of the crystalline phase was based on Zhang and Banfield’s correlation:157

(5.1)

where  represents the weight fraction of rutile, is the integrated peak intensity of rutile peak at 27.5 (2-theta), and  is the integrated intensity of anatase at 25.3 (2-theta).

The results show that anatase was the main crystalline phase at a relatively low calcination temperature (380-600 °C), even though rutile is more thermodynamically stable under ambient pressure compared with anatase and brookite. This might be explained by Zhang et al.’s study that anatase becomes more stable when the nanoparticles are smaller than 14 nm.236, 237

No obvious peaks could be observed from the TiO2-3 synthesized at 60 °C and calcined at 300 °C (Figure 5.17 curve B). However, anatase phase is observed from the sample TiO2-4 synthesized at 70 °C and calcined at 300 °C (Figure 5.17, curve A). This agrees with the DSC results that higher reaction temperatures resulted in lower calcination temperatures for crystallite formation.

The XRD patterns of the as-prepared and calcined TiO2-11 nanofibers with an average diameter of 80 nm are presented in Figure 5.18. No crystalline phase could be observed from the as-prepared TiO2 aerogel. Rutile phase was obtained after calcination at 380 °C. Polycrystalline phases, rutile and anatase with a ratio of 5.3: 94.7, were obtained after calcination at 500 (C. The only crystalline phase observed was anatase after calcination at 600 (C. However, the anatase phase transferred back into the rutile phase after calcination at 800 (C. The formation of rutile at 380 (C is due both to the larger size of the nanofibers (80 nm) and the fact that the rutile phase is more thermodynamically stable.

Figure 5.18. XRD: nanocrystalline TiO2-11, r: rutile, a: anatase (A) as-prepared TiO2-a aerogel, and calcined at (B) 380 °C, (C) 500 °C (D) 600 °C (E) 800 °C.

The TiO2-13 nanofibers with a diameter of around 10 nm were also examined by XRD (Figure 5.19). Similar to the nano spherical particles of 20-30 nm, lower calcination temperature, i.e., 380 (C, resulted in anatase. When the calcination temperature was 600 (C, rutile was formed with a relative percentage of 56 %.

Figure 5.19. XRD: nanocrystalline TiO2-13, r: rutile, a: anatase (A) calcined at 380 °C, (B) 500 °C (C) 600 °C.

### 5.3.6. Spheres or Fibers?

ATR-FTIR Measurements

Powder ATR-FTIR spectra of the resulting nanospherical powder (TIO2-1) in Figure 5.20 shows the IR spectra of both the as-prepared (spectrum a) and calcined TiO2 nano spherical particles of TiO2-1 (b-d). The peaks at 1546, 1447 and 1410 cm-1 in Figure 20a are due to a Titanium-acetate complex.238 The small peak at 1343 cm-1 is contributed by the CH3 group.232 Besides the titanium-acetate absorbance, there are also small peaks at 1132, 1117 and 1022 cm-1 corresponding to Ti-O-C, and the ending and bridging butoxyl groups, respectively. The oxo bonds can be observed by the presence of wide bands below 800 cm-1. With increasing calcination temperature (Figure 20a to d), the bidentate acetates, and the ending and bridging butoxyl groups were gradually removed, similar to the TGA observation. At 400 °C (Figure 20d), only the oxo bands can be observed. In addition, with increased calcination temperature, the oxo bands shifted to a smaller wave number, as a possible result of the removal of adjacent organic groups from the oxo-bond network.

Figure 5.20. Powder ATR-FTIR spectra of TiO2-1 nanospherical particles. (A) as-prepared, (B) calcined at 200 °C, (C) calcined at 300 °C, (D) calcined at 400 °C of TiO2-1.

In order to investigate the polycondensation reaction process of the two precursors (TIP and TBO) in CO2, in situ FTIR was also utilized. Formation of the Ti-acetate complex, and polycondensation products along with consuming of acetic acid and titanium alkoxide, were observed. Selected IR spectra during the sol-gel process using TIP as the metal alkoxide in CO2, with experimental conditions of TiO2-19, are presented in Figure 5.21. Straight TiO2 fibers with a diameter of 40 nm were produced afterwards. The curve (a) was the spectrum of TIP, and spectra (b) to (e) were taken at a reaction time from 10 to 4320 minutes. Acetic acid consumption can be conveniently observed from the decreasing peak at 1715 cm-1, while the consumption of TIP alkoxide precursor can only be observed from the peak at 860 cm-1, as the other strong peaks of TIP from 950 to 1120 cm-1 are in the fingerprint region of acetic acid, isopropanol and propyl acetate, hence being obscured. At the reaction time of 10 minutes, which is at the initial stage of the polycondensation reaction (spectrum b), the presence of peaks at 1596, 1557 and 1447 cm-1 provided evidence for the formation of the hexaprismane shape Ti6O6(OPri)6(OAc)6 complex 2, (see Table 5.1). After the reaction time of 4320 minutes, the peaks from the complex shifted to lower wave numbers at 1549, 1445 and 1397 cm-1, likely due to the OCO angle change of the bridging acetate, during further condensation of the hexamer. The gradual increasing of the peaks in the region below 800 cm-1 in spectra (b) ~ (e) indicates the formation of oxo bonds.

Figure 5.21. (a) IR spectrum of TIP. (b) ~ (e) in situ FTIR spectra of polymerization of TIP with acetic acid, at 60 °C and 4500 psig, initial concentration: TIP=1.1 mol/L, HOAc/TIP=5.5 (mol/mol). Reaction time: (b) 10 min; (c) 230 min; (d) 250 min; (e) 4320 min.

To further examine the role of hexamer formation in fiber growth, Figure 5.22 compares the powder FTIR spectrum of complex 2 previously synthesized in CO2 (molar ratio of HOAc/alkoxide = 1.33:1 and isolated as a crystal) to the in situ FTIR spectrum at 10 minutes polycondensation time using TIP alkoxide with a HOAc/TIP ratio of 3.5. Comparing the peaks in Figure 5.32 at 1604, 1543 and 1458 of the Ti6O6(OPri)6(OAc)6 complex, the peaks at 1603 1543 and 1448 cm-1 of the self-assembling fiber are very close, providing further evidence for the formation of this hexamer in the early stages of the self-assembly process. Curled TiO2 fibers with a diameter of 10 nm were produced under these lower HOAc/TIP ratio conditions.

Figure 5.22. (a) FTIR spectrum of complex 2 synthesized in CO2. The infrared spectrum was recorded on a Bruker Vector 22 FTIR instrument. The crystals were dispersed in a KBr tablet.  (b). In situ FTIR spectrum of polymerization of TIP with acetic acid, at 60 °C and 4500 psig, initial concentration: TIP=1.1 mol/L, HOAc/TIP=3.5 (mol/mol).

The polymerization of TBO by acetic acid in CO2 under conditions leading to sphere formation was also examined by in situ FTIR (Figure 5.23). At the reaction time of 10 minutes, the peaks at 1580~1600, 1560 and 1449 cm-1 were observed.  These absorption peaks are similar to those of the previously reported rutilane shape complex Ti6O4(OBun)8(OAc)8 (1 in Table 5.2). After the reaction time of 100 minutes, the peaks from the complex moved to 1547, 1457 and 1420 cm-1 due to further condensation. A large amount of butyl acetate was also produced according to the presence of the peaks at 1243 cm-1, 1368 and 1742 cm-1, due to the higher initial TBO concentration. Figure 5.24 shows the in situ FTIR during the polymerization of TBO by acetic acid in CO2 under conditions leading to fiber formation. At the reaction time of 10 minutes, there were three Ti-acetate bidentate peaks at 1565, 1447 and 1418 cm-1 (Figure 5.24a), which is different from Figure 5.23b, indicating another type of complex being produced. Variation of acid ratio to alkoxide is known to give different hexamer structures.231

Figure 5.23. (a) IR spectrum of TBO. (b) to (e) in situ FTIR spectra of polymerization of TBO with acetic acid, at 60 °C and 4500 psig, initial concentration: TBO=1.5 mol/L, HOAc/TBO=5.0 (mol/mol). Reaction time: (b) 10 min; (c) 100 min; (d) 1280 min; (e) 5840 min.

Figure 5.24. In situ FTIR spectra of polymerization of TBO with acetic acid, at 60 °C and 4500 psig, initial concentration: TBO=1.1 mol/L, HOAc/TBO=5.5 (mol/mol). Reaction time: (a) 10 min; (b) 100 min; (c) 300 min; (d) 330 min; (e) 5800 min.

Additionally, it is noticeable that lower peaks at 700 ~ 800 cm-1 in Figure 5.23e are lower than those in Figure 5.21e and 5.24e, suggesting less oxo bond being formed during formation of spherical colloidal particles than that of the fibrous equivalent.

Formation Scheme of TiO2 Fibers and Spheres

In order to consider how these FTIR results can shed light on the reaction pathways during polycondensation to nanostructures in CO2, we will consider both the cases where nanofiber formation is favored, and where nanosphere formation is favored. As described above for nanofiber formation using TIP alkoxide, our in situ FTIR results provided evidence for the formation of the titanium-acetate complex 2 at the initial stage of the reaction.  The schematic of the skeletal arrangement of this hexamer is redrawn (omitting the bridging acetate, etc.) for clearer observation (Figure 5.25a). In the structure, all six OPri groups are vertical, with three upward and another three downward. The condensation of this structure can only take place either above or underneath the ending OPri. In other words, one-dimensional condensation is favored with this hexamer, leading to step-growth of straight polymers.

In the case of spherical nanoparticles formed from TBO alkoxide, the in situ IR results provided evidence for the formation of complex 1 at the initial stage of the reaction. The schematic of the skeletal arrangement of this hexamer is shown in Figure 5.25b, in which there are six ending OBun groups, two upward, two downward, one to the left and one to the right. This structure would easily permit the formation of polycondensate chains with branches. This branching facilitates three-dimensional growth and subsequent formation of spheres.

Figure 5.25. Schematic of the skeletal arrangements of complex 2 (R= Pri) (a) and complex 1 (R= Bun) and 3 (R= Pri)  (b). In the scheme, all acetate groups, some of the oxo bonds, and two bridging OR groups are omitted to make the structure simpler.

The evolution of the macromolecules into nanofibers or nanospheres can be explained by aggregation of rigid colloidal particles as described by Brinker.105 When the straight polymers grow long enough, the solubility decreases and small spherical concentrated regions, called coacervates, are formed to decrease the interfacial energy (Figure 5.26). The arrangement of the macromolecules in the coacervates results in elliptical tactoids, in which the straight polymers are organized due to the interaction among the straight macromolecules. The macromolecules end up with a rigid fiber structure (crystalloid) as observed by electron microscopy.

Figure 5.26. Schematic of nanostructure formation.  Polycondensation of complex 2 or 1 led to formation of either straight or irregular-shape macromolecules. Coacervates and tactoids were formed to lower the energy of the macromolecules in CO2, which in turn resulted in the formation of either fibers or spheres.105

As described earlier, both the HOAc/Ti ratio and the alkoxide structure are the primary factors determining whether fibers or spheres are formed. In the case of TBO as a precursor, formation of spherical particles at low acid ratios (e.g. HOAc/TA= 4) was explained due to the skeletal structure of complex 1; however, formation of nanofibers from TBO at higher acid ratios (e.g. 5.5) is more difficult to explain due to the lack of IR and XRD crystal data. For the TIP alkoxide system, increased HOAc/TIP ratios resulted in the formation of fibers with a larger diameter and more straight morphology.  This may be due to the presence of a small amount of complex 3 with 2, which was previously identified in our XRD studies. Similar to complex 1, complex 3 will facilitate 3-dimensional condensation as shown schematically in Figure 5.25. This has the potential to act as a cross-linking agent among the straight macromolecules, which could make the fiber thicker and stronger upon heat-treatment.

### 5.3.7. CO2’s Effect on the formation of TiO2 Microstructures

The zero interfacial tension of scCO2 maintained the nanostructures and a high surface area of the resulting materials. The acetate group in the complex also likely plays a role in the colloidal stabilization by enhanced solubility of the macromolecules in CO2, analogous to that observed with Beckman surfactants239 or Wallen sugars.240 As well, hydrogen bonding between individual acetic acid molecules241, 242 will slow down the condensation process, facilitating nanofiber formation and minimizing precipitate formation. Further studies on CO2’s effect on the sol-gel process will be described in Chapter 8.

## 5.4. Conclusion.

As described in the introduction, the reaction between TBO and acetic acid is rather mild, such that these two ingredients could be placed together in the view cell before addition of CO2. It was found that the morphology of the TiO2 aerogel formed in CO2 depends on the starting concentration of the precursor and the molar ratio of acetic acid and TA, while temperature and pressure had little effect. Very low concentration of the precursor facilitates the formation of precipitate. When the concentrations of TBO and acetic acid were as low as 0.031mol/L and 0.26 mol/L, respectively, a precipitate with a surface area as low as 5 m2/g was formed. Very high molar ratios of the acid to the alkoxide and high temperature also facilitate formation of the precipitates. If the concentrations of TBO and acetic acid were 1.10 mol/L and 5.50 mol/L, respectively, the gel time was less than two days under the specified conditions, and mesoporous fiber clusters were obtained. When concentrations of TBO and acetic acid are 1.48 mol/L and 6.12 mol/L, respectively, the gel time is much longer (3-4 days) and TiO2 aerogel monolith was produced.

Comparing with TBO, TIP is much more active with acetic acid. The gelation time was shorter and only a fragile monolith was obtained (as described in Table 5.2), even with a temperature as low as 40 °C.

Different from the conventional sol-gel process, from which the TiO2 aerogel monolith is difficult to be prepared due to the rapid hydrolysis reaction,20 the modified non-aqueous sol-gel method makes it feasible to form a TiO2 monolith. The morphology and the pore size of the aerogel could be tailored by changing the concentration of the starting materials. Aerogels with a higher surface area and crystalline phases could be obtained by increasing the process temperature.

# Synthesis and Characterization of ZrO2 Nanoarchitectures

This chapter is reproduced from the published article by the author: Direct Synthesis of Zirconia Aerogel Nanoarchitecture in ScCO2, with permission from Langmuir, 22 (9), 4390-4396, Copyright [2006] American Chemical Society.

Similar to the approach of synthesizing titania, ZrO2 nanomaterials were synthesized at 40-50 °C and 6000 psig. Either a translucent or opaque monolith was obtained. The resulting materials were characterized by electron microscopy, X-ray diffraction, thermal analysis, N2 physisorption and infrared spectroscopy analysis. The electron microscopy results showed that the translucent monolithic ZrO2 exhibited a well-defined mesoporous structure, while the opaque monolith formed using added alcohol as a co-solvent was composed of loosely compacted nanospherical particles with a diameter of ca. 20 nm. After calcination at 400 and 500 (C, X-ray diffraction results indicated that the ZrO2 exhibited tetragonal and/or monoclinic phases. In situ infrared spectrum results showed the formation of Zr-acetate coordinate complex at the initial stage of the polycondensation, followed by further condensation of the complex into macromolecules.

## 6.1. Introduction

Porous zirconia (ZrO2) is an insulation material that has both acidic and basic properties that are desirable for several current applications of interest, including catalyst supports30, 31 and electrodes in dye sensitized solar cells32 and solid oxide fuel cells.33 For catalyst supports, CuO/ZrO2 was used for synthesis of methanol from hydrogen and carbon dioxide,243, 244 Pt/ZrO2 was studied for hydrogenation of formate species,245 and noble-metal/ZrO2 was chosen for NOx removal.246 Zirconia is also a very useful ceramic hardening material, and is often used as a component in composite biomaterials for joint prostheses.34 Due to the interest in zirconia’s unusual properties and wide-spread applications, well-defined mesoporous ZrO2 has been prepared by several techniques including templating213, 247 and evaporation-induced self-assembly (EISA) methods.248 Sol-gel processing followed by supercritical fluid drying has also been used to synthesize ZrO2 aerogels.  This technique normally provides a very porous material with irregular patterned mesopores having a large pore-size-distribution.95, 104 Recently, a well-developed mesoporous structure in the ZrO2 aerogel was reported having a large surface area by calcination in flowing helium at 300 °C and then in flowing oxygen at 500 °C.249

Like several other materials, zirconia nanoparticles are of significant current interest in preparing piezoelectric, electro-optic, dielectric and nanocomposite materials,250-252 and hybrid materials for solid oxide fuel cells.253 Sub-micron and nano spherical particles of ZrO2 have been prepared by several methods including a sol-gel technique utilizing hydroxypropyl cellulose as a polymeric steric stabilizer254 and miniemulsification of molten salts.255 Using a so-called flame spray pyrolysis (ESP) method, spraying of combustible droplets into a CH4/O2 flame, formed ZrO2 particles with a diameter ranging from 6 to 90 nm.48, 256 Thermal decomposition of ZrO(OH)2·xH2O polymer precursor generated ZrO2 particles as small as 12 nm.257 A biosynthesis process using the fungus Fusarium oxysporum developed ZrO2 particles less than 10 nm.219

This research was motivated by usage of the green solvent, scCO2, and developing a new synthesis method for ZrO2 that allows for material properties appropriate for catalyst preparation, inorganic/organic hybrid nanomaterials, and porous ceramics for biocomposites. The properties of the resulting material that were of interest for these applications were studied, including morphology, particle size, crystal structure, and mesoporous structure.

## 6.2. Experimental Details

Materials. Reagent grade 70% Zirconium (IV) Propoxide (ZPO) in 1-propanol, 80% Zirconium (IV) Butoxide (ZBO) in 1-butanol, 99.5% 1-butanol, and 99.7% acetic acid (HOAc), from the Aldrich Chemical Company, were used without further purification. Instrument grade carbon dioxide (99.99%) was obtained from BOC Canada.

For synthesis, a 10 ml stainless steel view cell was connected to a syringe pump (ISCO 100 DM) for pumping CO2. Temperature and pressure in the view cell were measured and controlled by means of a temperature controller (Fuji), a pressure transducer (Omega) and a control valve (Badger), which communicated with a computer through a network interface (National Instruments). The details of the experimental setup were previously provided in Chapter 3.

Preparation of ZrO2. In a typical experiment, zirconium alkoxide (ZPO or ZBO) was placed in the view-cell reactor, followed by addition of acetic acid and CO2 up to a temperature of 40 ºC and a pressure of 6000 psig, which is above the supercritical condition of CO2 (Tc =31 ºC, Pc =1070 psig). The amount of zirconium alkoxide and acetic acid added to the view-cell ranged from 5.47 to 11.3 mmol and from 17.6 to 35.1 mmol, respectively (see Table 5.1). A magnetic stirrer was used for mixing the reaction mixture to reach a homogeneous transparent phase. To ensure complete condensation of the precursor, a few drops of the reaction mixture were vented into water, where a white precipitate indicated that further reaction time was required. Normally, several days of aging was required for complete reaction, which is further studied in Chapter 7. In order to remove the unreacted acetic acid and condensate, i.e. alcohol and ester from the gel formed in the view cell, a scCO2 washing step was conducted. After aging, the formed gel was washed continuously using scCO2 at a rate of approximately 0.5 ml/min, followed by controlled venting at 0.5 ml/min to prevent collapse of the solid network. The transparent gel gradually became translucent during the scCO2 washing and venting steps. The as-prepared ZrO2 was then calcined using a heating rate for each calcination temperature of 10(C per minute, to set-point.  The holding time was 2 hours, and the cooling rate to room temperature was 0.5(C per minute.

Characterization. In situ FTIR was performed on the Sentinel-ASI Applied Systems. Solid ZrO2 aerogel powder was characterized by means of a Bruker Vector 22 ATR-FTIR instrument. DSC and TGA analysis were performed using a Mettler Toledo DSC822e and TGA/SDTA851e, respectively, at a heating rate of 10 (C/min under a nitrogen atmosphere. XRD was conducted utilizing Rigaku-Geigerflex CN2029 employing CuKα1 + Kα2 radiation with a power of 40kVx35mA for the crystalline analysis. BET surface area, and pore size and distribution were obtained using Micromeritics ASAP 2010 at 77 K. Prior to the N2 physisorption, the sample was degassed at 200 (C under vacuum. SEM micrographs were recorded using a LEO 1530 electron microscope without gold coating. TEM images and electron diffraction patterns were obtained using a JEOL 2010f transmission electron microscope. The specimens were ground, and placed on a copper grid covered with holey carbon film.

## 6.3. Results and Discussion.

In this direct sol-gel route in CO2, when mixing the Zr alkoxide and acetic acid, a transparent homogenous phase was initially formed which was either clear or yellow, depending on the starting concentrations of the precursor and acetic acid (Figure 6.1a). After stirring the transparent reaction mixture for several hours, the viscosity of the fluid became large enough to stop the stirrer whirling, and either a white opaque phase or a light yellow transparent homogeneous phase was formed (Figure 6.1b) which through ageing turned into a transparent gel (Figure 6.1c). High conversions were typically obtained using this direct sol-gel synthesis method in CO2, approaching 98% based on the weight of starting zirconium alkoxide and calcined ZrO2 product at 500 °C.

Figure 6.1. (a) The homogeneous transparent phase at the initial stage of the reaction; (b) the formation of the opaque white phase; (c) the formation of the transparent gel in the view cell.

As a precipitate tended to form after mixing acetic acid with zirconium alkoxide in CO2, it was found crucial to select a temperature, pressure and initial concentrations of starting materials to maintain a homogeneous phase before gel formation in order to obtain well-defined nanostructures. A variety of experimental conditions were carried out, and favorable conditions were found using lower temperatures (e.g. 40 (C), higher pressures (e.g. 6000 psig), higher initial zirconium alkoxide concentrations, low acid/alkoxide ratio, usage of ZBO instead of ZPO, and usage of butanol as a cosolvent. The synthesis conditions for the successful and unsuccessful ZrO2 aerogel preparation are summarized in Table 6.1.

Table 6.1. Synthesis conditions of ZrO2 structures in CO2 and characterization results.

| Samples | Precursor | Tre b | Tre c | Co d | HOAc/ZA e | butanol | Tcalc f | Sbet g | Dpore h | VPorei | morphology | microstructure |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | (°C) | (psig) | (mol/L) | (mol/mol) | (ml) | (°C) | (m2/g) | (nm) | (cm3/g) |  |  |
| ZrO2-1-APa | ZPOj | 40 | 6000 | 1.13 | 2.23 | - | - | 257 | 2.9 | 0.19 | translucent monolith | mesoporous |
| ZrO2-1-400 |  |  |  |  |  |  | 400 | 101 | 4.6 | 0.051 |  |  |
| ZrO2-1-500 |  |  |  |  |  |  | 500 | 51 | 7.8 | 0.045 |  |  |
| ZrO2-2-AP | ZBOk | 40 | 6000 | 1.13 | 2.23 | - | - | 257 | 4.5 | 0.29 | translucent monolith | mesoporous |
| ZrO2-2-500 |  |  |  |  |  |  | 500 | 52 | 9.8 | 0.15 |  |  |
| ZrO2-3-AP | ZBO | 40 | 6000 | 1.09 | 3.22 | - | - | 215 | 4.9 | 0.26 | translucent monolith | mesoporous |
| ZrO2-3-500 |  |  |  |  |  |  | 500 | 71 | 7.9 | 0.19 |  |  |
| ZrO2-4-AP | ZBO | 40 | 6000 | 0.547 | 3.22 | 5.5 | - | 361 | 6.0 | 0.54 | opaque monolith | nanospheres |
| ZrO2-4-500 |  |  |  |  |  |  | 500 | 75 | 12.7 | 0.24 |  |  |
| ZrO2-5-AP | ZBO | 40 | 6000 | 0.547 | 3.22 | 5 | - | 397 | 5.7 | 0.57 | opaque monolith | nanospheres |
| ZrO2-5-500 |  |  |  |  |  |  | 500 | 76 | 9.7 | 0.14 |  |  |
| ZrO2-6-AP | ZBO | 40 | 6000 | 0.547 | 3.22 | 4 | - | 399 | 5.3 | 0.53 | opaque monolith | nanospheres |
| ZrO2-6-500 |  |  |  |  |  |  | 500 | 71 | 8.7 | 0.15 |  |  |
| ZrO2-7 | ZBO | 50 | 6000 | 1.13 | 2.23 | - | 400 | 4.9 | - | - | precipitate | chunks |
| ZrO2-8 | ZBO | 40 | 6000 | 1.13 | 3.22 | - | - | - | - | - | precipitate | - |
| ZrO2-9 | ZBO | 40 | 3000 | 1.13 | 2.23 | - | - | - | - | - | precipitate | - |
| ZrO2-10 | ZBO | 40 | 6000 | 0.547 | 2.23 | - | - | - | - | - | precipitate | - |

Note:  a: AP: as-prepared; b: reaction temperature; c: reaction pressure; d: initial concentration of zirconium alkoxide; e: molar ratio of acetic acid over zirconium alkoxide; f: calcination temperature; g: BET surface area; h: adsorption average pore diameter (4V/A by BET); i: single point adsorption total pore volume per gram; j: zirconium propoxide; k: zirconium butoxide.

Although the zirconium alkoxide, acetic acid and CO2 were miscible at the initial stage, two layers were formed after 10~60 minutes of reaction if the synthesis parameters of ZrO2-2 were changed as follows: when the temperature was increased from 40 to 50 °C (ZrO2-7), or the HOAc/ZBO ratio increased from 2.23 to 3.22 (ZrO2-8), or the pressure decreased from 6000 to 3000 psig (ZrO2-9), or decreased initial concentration of ZBO from 1.13 to 0.547 mol/L without butanol as the cosolvent (ZrO2-10). The ZrO2 produced from the lower layer was examined by SEM and N2 physisorption, which showed that the material was badly agglomerated micron-size-spheres and exhibited a low surface area of 4.9 m2/g. Hence, in most experiments, the synthesis parameters were selected at 40 °C and 6000 psig in order to maintain the homogenous phase and the supercritical state.

SEM and TEM. After calcinations, samples ZrO2-1 to ZrO2-3 were found to produce relatively hard translucent monoliths while ZrO2-2 to ZrO2-4 produced fragile opaque monoliths. The microstructure of these materials was examined by means of electron microscopy. The SEM results showed that the translucent monolith samples exhibited a relatively smooth surface (Figure 6.2a), while the TEM results revealed wormlike mesopores on the thin flakes of the specimen (Figure 6.2b).  The SEM (Figure 6.2c) of the fragile opaque monolith showed that it was composed of loosely compacted nanospherical particles with diameters of approximately 20 nm. The HRTEM of this sample showed the size of the crystallites and reflection pattern of the polycrystalline phases (Figure 6.2d). The d-spacings of 0.37 nm and 0.32 nm correspond (011) and (-1 11) planes of monoclinic ZrO2, respectively.258 The crystallite size of ZrO2-4-500 determined by HRTEM was measured to be 10 nm, which is in agreement with the XRD results estimated using Scherrer’s equation (see below). Figure 6.3 shows the lumber-like precipitate of ZrO2-7.

Figure 6.2. SEM and TEM images.  The translucent monolith of ZrO2-2-400: (a) SEM and (b) TEM. The translucent monolith of ZrO2-2-400: (a) SEM and (b) HRTEM.

Figure 6.3. SEM. Precipitate chunks of ZrO2-7.

N2 Physisorption. The N2 physisorption (77K) was employed to study the surface area and pore structure of the aerogel-like materials. For the various synthesis conditions of this study for as-prepared and calcined ZrO2, the average BET surface area, the single point adsorption total pore volume per gram, and the adsorption average pore diameter (4V/A by BET), are summarized in Table 6.1. The surface areas of the as-prepared translucent monoliths (ZrO2-1 to 3) ranged from 215 to 257 m2/g, while when calcined at 500 °C, decreased to 51 ~ 71 m2/g, likely due to the fusion of the solid network.  The surface areas of the opaque monoliths (ZrO2-4 to 6) were as high as 361 ~ 399 m2/g as-prepared, while when calcined at 500 °C also declined into the 71 ~ 75 m2/g range. Several samples were also heat treated in an inert atmosphere using the technique of Suh and Park,249 however, the surface areas were not found to be noticeably higher. Comparing with the literature, the surface areas of the calcined ZrO2 (Table 6.1) were higher than those obtained using the conventional sol-gel process (48-56 m2/g),259 and lower than those obtained by careful control of sol-gel parameters, i.e., between 69 and 134 m2/g by Ward et al.,260 and between 96 and 145 m2/g by Suh et al..249

All the resulting aerogel materials in this study (samples 1-6) exhibited a Type IV isotherm, indicating the existence of mesopores.261 The translucent monoliths (samples 1-3) exhibited H2 hysteresis loops (Figure 6.4a), while the opaque fragile monoliths with nanostructure (samples 4-6) exhibited H3 loops (Figure 6.4b).  After heat treatment for both samples, the isotherms: a) showed lower volume of N2 gas adsorbed per relative pressure indicating lower surface areas, and b) moved to a higher relative pressure region, indicating that larger pore sizes were produced. These isotherms were found to be typical for both sets of samples.

Figure 6.4.  Isotherms of the ZrO2 as-prepared and calcined samples at 500 °C: (a) ZiO2-2; (b) ZrO2-4. See Table 5.1 for the synthesis conditions for ZrO2-2 and -4.

The pore sizes of the experimental samples were in the range of 2.9 ~ 6.0 nm before calcination, and increased to 4.6 ~ 12.7 nm after calcination (Table 6.1) due to the evolution of gas (i.e., CO2 and water vapor) during heat treatment.262 At the same time, the pore volume was 0.19 ~ 0.57 cm3/g before calcination, and was reduced to 0.051 ~ 0.24 cm3/g after calcination, indicating the formation of denser materials. By comparing Figures 6.5a and Figure 6.5b, which show the BJH desorption pore-size distribution, we can see that ZrO2-2 exhibited a smaller pore size and pore-size distribution than ZrO2-4. Careful examination and measurement of the TEM image of ZrO2-2 (Figure 6.2b) shows relatively uniform pores with an approximate accessible diameter of 4.0 nm. This TEM result is similar to the N2 physisorption result (4.8 nm). In the case of ZrO2-4, the pores are formed by the interstitial space between the loose-compact nanoparticles inside the monolith. These pore volumes are larger and more polydisperse than the translucent monolith samples (Figure 6.5b), and can be visualized by electron microscopy in Figure 6.2c.

Figure 6.5. BJH desorption pore-size-distributions of the as-prepared and calcined at 500 °C: (a) ZrO2-2; (b) ZrO2-4.  See Table 5.1 for the synthesis conditions for ZrO2-2 and -4.

DSC. The as-prepared translucent and opaque monoliths were examined by means of DSC, which are shown in Figure 6.6a and b for samples ZrO2-2 and ZrO2-4, respectively. The endothermal peaks in Figure 6.5a for ZrO2-2 are at 132 (T1) and 332 °C (T2), while the ZrO2-4 sample shows a weak peak around 100 °C, and a strong peak at 328 °C (T5).  These peaks correspond to the evaporation of the organic solvent trapped in the pores, and removal of the organic groups from the ZrO2 network, which is also shown by the FTIR and TGA results (see below). The exothermal peaks at 464 (T3, tetragonal) and 520 °C (T4, monoclinic) for ZrO2-2, and at 467 °C (T6, monoclinic) for ZrO2-4, indicate the formation or transformation of the crystalline phases, which were recognized by powder XRD analysis as described later. For ZrO2-2, the slope from 400 to 464 °C indicates the development of crystalline phases, and the inflection point at 445 °C suggests the formation of more than one crystalline phase. In contrast to ZrO2-2, ZrO2-4 is flat near 400 °C, indicating there is no significant formation of crystal structure at this temperature. Interestingly, ZrO2-4 exhibited a very sharp exothermal peak (T6) contrasting to ZrO2-2, suggesting a rapid crystallization of nanoparticles at the specified temperature.

Figure 6.6. DSC: (a) as-prepared ZrO2-2, T1: 132 °C; T2: 332 °C; T3: 464 °C; T4: 520 °C; (b) as-prepared ZrO2-4, T5: 328 °C, T6: 467 °C. See Table 5.1 for the synthesis conditions for ZrO2-2 and -4. Inset: TGA of the as-prepared ZrO2-2.

The TGA result (Figure 6.6 inset) shows two obvious regions when the temperature was increased: the first region started from 80 °C and ended at 260 °C with a relatively small slope; while the second region started at 320 °C and ended at 490 °C with a large slope indicating more weight loss in this region. This agrees with the DSC results.

XRD. The wide-angle powder XRD patterns of translucent ZrO2-2 calcined at 400 and 500 °C are displayed in Figure 6.7a. Mainly tetragonal phase was found present in the sample calcined at 400 °C while the monoclinic baddeleyite became the main phase after calcination at 500 °C. The tetragonal crystallite size of the ZrO2 calcined at 400 °C is 4.1 ± 0.9 nm, while the monoclinic crystallite size of the ZrO2 calcined at 500 °C is 8.2 ± 1.7 nm. The crystallite size was estimated by using Scherrer’s equation:

Dscher = 0.90 λ/(βcos θ)                                                 (6.1)

where, Dscher is the crystallite size, λ the X-ray wave length, θ half the angle of diffraction, and β is the full width at half-height of the diffraction peak, as described in Chapter 3.263 The opaque ZrO2-4 sample consisting of nanospheres, exhibited the similar crystalline phases as the translucent ZrO2-2 when calcined at 500 °C (Figure 6.7b), with a crystallite size of 10.1 ± 2 nm. The main phase in the ZrO2 calcined at 400 °C was amorphous, with a very small amount of tetragonal phase. The XRD results are consistent with the DSC observations. The samples were also examined in the small angle XRD region between 0 and 20 2-theta. No peaks were observed, indicating the mesophases were not in a regular pattern that could be detected using this technique.

Figure 6.7. XRD patterns: (a) the translucent ZrO2-2 calcined at 400 and 500 °C;  (b) the opaque ZrO2-4 calcined at 400 and 500 °C. Note: (t): the tetragonal and/or cubic Zirconium Oxide; (m): the monoclinic Zirconium Oxide.

FTIR. The as-prepared material, as well as the materials after calcination at 200 ~ 500 °C, were examined by means of ATR-FTIR (Figure 6.8). The peak in the 1500-1600 cm-1 spectral range is due to the asymmetric stretch of acetate bidentates, while the peaks in the 1360-1480 cm-1 spectral range are due to the symmetric stretching of acetate bidentates.264 The small peak at 1342 cm-1 is contributed by CH3 group.  The peaks at 1049 and 1026 cm-1 are due to the ending and bridging butoxyl groups, respectively. The spectra show that there were still organic groups after calcination at 300 °C (Spectra c), and the absorbance drops greatly from 300 to 400 °C (Spectra d).  After calcination at 500 °C, essentially no organic groups remain. The absorbance frequencies of Zr-O-Zr oxo bands (lower than 800 cm-1) decreased noticeably with increased calcination temperature, as a possible result of the removal of adjacent organic groups from the oxo-bond network. The powder IR spectra showed a sudden absorbance decrease when the calcination temperature was increased from 300 °C to 400 °C (Spectra c and d in Figure 6.8), which agrees with the TGA observation.

Figure 6.8. ATR-FTIR: ZrO2-2 monolith as-prepared (a) and calcined at (b) 200 °C, (c) 300 °C, (d) 400 °C and (e) 500 °C.

In situ ATR-FTIR was used to monitor the sol-gel process under actual reaction conditions in CO2. Figure 6.9 curve (a) shows the spectrum of ZPO (w/w 70%) dissolved in propanol. The peaks from 1381 to 1458 cm-1 are due to the stretching and vibration of the aliphatic CH2 and CH3 groups, and the peaks from 1015 to 1160 cm-1 are due to the Zr-OPr groups.265 Spectra (b) - (e) were recorded at different reaction times in CO2. The condensation of ZPO can be observed by the decreasing peak at 1134 cm-1, while other Zr-OPr peaks from 1015 to 1104 cm-1 are in the fingerprint range of n-PrOH, hence obscuring analysis. At the reaction time of 10 minutes (Spectra b), the quick formation of the peaks at 1600, 1567, 1544, 1478, and 1455 cm-1 indicates the formation of a Zr-alkoxo-acetate coordination compounds. Gradual formation of ester during polycondensation can be observed from the peaks at 1239 and 1744 cm-1 due to the reaction of acetic acid and 2-propanol into ester and water (Figure 6.9 b ~ e). At the same time, obvious movement of the acetate bidentate peaks (at the range 1455 ~ 1600 cm-1) can be observed, due to the OCO bond angle and length change during condensation.230 The chemical reactions between zirconium alkoxide and acetic acid will be discussed in Chapter 7.

Figure 6.9. (a) FTIR spectrum of 70 % zirconium propoxide in propanol; in situ FTIR spectra in CO2:  (b) at the reaction time of 10 min.; (c) 70 min.; (d) 130 min. (e) and 250 min. reaction condition: 40 °C and 5000 psig, initial concentration of ZPO = 1.13 mol/L, HOAc/ZPO = 2.23 (mol/mol).

In order to examine the role of CO2 in the sol-gel process, the reaction of zirconium alkoxide with acetic acid was also conducted in butanol, instead of in CO2, under similar synthesis conditions. No gel was formed at 40 (C when ZBO = 1.13 mol/L and the HOAc/ZBO ratio = 2.23. When ZBO = 0.547 mol/L and HOAc/ZBO = 3.22, gel was formed and subsequently dried using scCO2.  However, a relatively low surface area of 35 m2/g was obtained before calcination, and SEM analysis did not show any nanostructure. In addition, increased gel shrinkage was observed providing a very dense material compared to the zirconia synthesized in CO2. Hence, the results show that CO2 played an important role in the nanostructure formation and mesoporous structure. The zero interfacial tension of scCO2 maintained the nanostructures and a high surface area of the resulting materials.113 Acetic acid is known to decrease the hydrolysis rate of metal alkoxides in water by coordination of the acetate group to the metal ions, hence slowing down the sol-gel process, and preventing precipitate formation for TiO2 and ZrO2 aerogels.227, 266 Also, according to Yamamoto et al. and Han et al., there is significant hydrogen bonding between acetic acid molecules in scCO2,241, 242 which will similarly slow down the sol-gel process, hence likely facilitating the formation of uniform nanostructures. The acetate group in the complex also likely plays a role in the colloidal stabilization by enhanced solubility of the polycondensates in scCO2, analogous to that observed with Beckman surfactants or Wallen sugars.239, 240 Further studies on CO2’s effect on the sol-gel process will be described in Chapter 8.

The results in this chapter showed that acetic acid was an excellent reaction agent for producing nanoparticles and mesoporous monolith of ZrO2 in CO2. This research and our former synthesis of TiO2 nanofibers and nanospheres show the promise of this technique for synthesizing nanomaterials, compared to the more challenging conventional aerogel process.

## 6.4. Conclusion

The zirconia nanomaterials were synthesized for the first time by a one-step sol-gel route in CO2 using zirconium alkoxides and acetic acid. Both mesoporous monolith and nanoparticles were produced. The as-prepared materials exhibited a high surface area (up to 399 m2/g) and porosity, while the calcined materials demonstrated tetragonal and/or monoclinic nanocrystallites. The mesoporous monoliths exhibited H2 hysteresis loops from N2 physisorption, while the nanospheres exhibited H3 loops. DSC analysis showed that the nanoparticles gave a very sharp exothermal peak.  In situ FTIR was found to be a valuable technique for studying the morphology evolution of the polycondensation reaction. The success in synthesizing ZrO2 nanostructures within the present study, along with our former research on SiO2 and TiO2, shows the promise of using CO2 for producing metal oxide nanomaterials. The low surface tension during scCO2 drying allows the formation of mesoporous oxides that have potential application as porous ceramics for SOFC.

# Kinetics Study on Direct Sol-Gel Reactions in CO2 by Using In Situ ATR-FTIR Spectrometry

In this chapter, a chemometric method is used to extract pure-component spectra and the concentration profiles from the in situ ATR-FTIR spectra, which were obtained during the sol-gel process of TEOS, TIP and ZBO with acetic acid in CO2. The precursor conversions and the metal complex concentration profiles under different synthesis conditions are discussed.

## 7.1. Introduction

In previous chapters, synthesis of SiO2, TiO2 and ZrO2 nanomaterials in CO2 were described; however, the kinetics were not discussed. A kinetics study requires rather detailed knowledge of the chemical reactions, e.g. the step-by-step reaction scheme, and the concentration profiles of reactants, intermediates and/or products. By mixing TEOS with acetic acid without a solvent, the possible sol-gel reaction steps have been proposed by Sharp using NMR results:267

Substitution:

≡SiOR + HOAc ⇌ ≡SiOAc + ROH                                     (7.1)

Esterification:

HOAc + ROH ⇌ AcOR + H2O                                     (7.2)

Hydrolysis:

≡SiOR + H2O ⇌ ≡SiOH + ROH                                    (7.3)

Condensation:

≡SiOH + ≡SiOH ⇌ ≡SiOSi≡ + H2O                                 (7.4)

Condensation:

≡SiOH + ≡SiOR ⇌ ≡SiOSi≡ + ROH                               (7.5)

Condensation:

≡SiOH + ≡SiOAc ⇌ ≡SiOSi≡ + HOAc                           (7.6)

Carboxylation:

≡SiOH + HOAc ⇌ ≡SiOAc + H2O                              (7.7)

The chemistry of titanium alkoxides reacting with acetic acid in conventional solvents is also reasonably well understood. Doeuff et al. explained the formation of the Ti hexamer complex through modification, esterification, hydrolysis and condensation.232 The reactions can be generally written as:

Modification:

Ti(OR)4 + HOAc → Ti6(OAc)m(OR)n + ROH                               (7.8)

Esterification:

ROH + HOAc ⇌ ROAc + H2O                                       (7.9)

Hydrolysis:

Ti6(OAc)m(OR)n + H2O → Ti6(OAc)m(OR)n-x(OH)x + ROH              (7.10)

Oxolation:

Ti6(OAc)m(OR)n-x(OH)x → Ti6Ox(OAc)m(OR)n-2x + ROH                 (7.11)

Where, Ti6Ox(OAc)m(OR)n-2x is the hexamer complex.

Zirconium alkoxide reacting with carboxylic acid has also been studied in conventional solvents and the products were characterized by single crystal XRD.268-270 According to the scheme provided by Kickelbick,268 the reaction pathways can be written as:

Modification:

Zr(OR)4 + HOAc → Zrm(OR)4m-n(OAc)n + ROH                          (7.12)

Esterification:

HOAc + ROH ⇌ ROAc + H2O                                     (7.13)

Hydrolysis:

Zrm(OR)4m-n(OAc)n + H2O → Zrm(OR)4m-n-x(OAc)n(OH)x + ROH         (7.14)

Oxolation:

Zrm(OR)4m-n-x(OAc)n(OH)x → ZrmOx(OR)4m-n-2x(OAc)n + ROH             (7.15)

Further condensation

ZrmOx(OR)4m-n-2x(OAc)n → macromolecules                             (7.16)

It is noted that water is required for the sol-gel processes. At the initial stage of the reaction, water was generated only through the esterification reaction. With the reactions proceeding, water can also be generated from condensation.

To date, no kinetics study on the reactions between the alkoxides and acetic acid has been reported. For a detailed kinetics study, the concentration profiles of the reactants or products are indispensable. On-line monitoring of a chemical process using vibrational spectrometry, e.g. in situ ATR-FTIR or Raman, is of increasing importance due to the real time analysis of the components in the reactor. However, the collected spectra are often complicated by peak overlapping, and hence cannot be directly analyzed using a conventional peak height or peak area measurement. For instance, the previous in situ ATR-FTIR spectrometry results in Chapters 4-6 have shown that the significant peaks of the precursors are overlapped severely with those of the products.

In order to calculate the component concentrations from the complicated spectra, mathematical and statistical methods, known as chemometrics, have been used.271 There are two categories of chemometric methods for resolving the spectrometry data: i.e. calibration and self-modeling curve resolution (SMCR). The least squares regression method has also been extensively used in the calibration methods.151, 271 However, in situations when there is an unknown component, or the pure component spectrum for the reference component is not available, the calibration methods cannot resolve the mixture spectra.272 In these situations, e.g. the sol-gel process for SiO2 TiO2 and ZrO2, the SMCR methods are attractive.

The SMCR method uses chemometrics to extract a set of concentration profiles and spectra of pure components from a set of mixture spectra, e.g. in situ IR spectra, without any prior knowledge about the system.273, 274 The first SMCR method was proposed by Wallace in 1960.275 A simple-to-use interactive self-modeling mixture analysis (termed SIMPLISMA), was proposed by Windig of the Eastman Kodak Company in 1991.272, 276 The SIMPLISMA technique has been an effective SMCR method for data analysis in various chemical processes using UV, IR, Raman and NMR spectrometry.277-285

To describe the chemometric SIMPLISMA technique, consider a reaction system with n components, in which a set of IR spectra collected at different reaction times can be written as a matrix, D. As D is a function of the concentration and the absorbance (Bpure) of each component, it can be expressed as:

D = C ×B                                                      (7.17)

where D is the known rw matrix transformed from a set of in situ IR spectra, C is the to-be-determined rn matrix representing concentration coefficients, B is the to-be-determined nw matrix representing n pure component spectra, r is the number of spectra, and w is the index of wavenumbers.286

In the IR spectra, the absorbance will change at certain wavenumbers due to the reaction proceeding. The SIMPLISMA method tries to find the highest absorbance standard deviation from the mean value in the IR spectra. The “purity”, qj, is calculated as:

(7.18)

where, μj is the mean value of absorbance at wavenumber j, σj is the standard deviation at wavenumber j, and α is an empirical parameter called offset, which is added to the mean value in order to suppress the noise in the region where the absorbance is close to zero. Typical values for α range from 1-5 % of the maximum μj for the conventional method; for the second-derivative method as described later, however, α is normally selected as 20 %.276, 287

A pure variable is defined as the wavenumber where only one component contributes to the absorbance. The first ‘pure variable’ is selected as the wavenumber that has the highest qj value. Then other pure variables are selected, which are independent of the first variable. The absorbances of the pure variables from all components in matrix D are used to calculate matrix C using the linear correlation of the Beer-Lambert law described in Chapter 3. With the known matrices D and C, Matrix B can be calculated using a least-squares regression method.272, 276, 286

In the second-derivative method, the calculated matrix B was used to recalculate a new C denoted as C’ using a least square approximation. Thus the matrix C’ provides the second-derivative concentrations. Consequently, the second-derivative pure component spectra B’ can be obtained using matrices D and C’. It was found that the second-derivative method was effective when the conventional pure-variable approach could not give satisfactory results.276, 287 It should be noted that SIMPLISMA cannot calculate the absolute concentrations of the components. In the case when quantitative solution is necessary, an independent calibration of the system should be performed for every component of interest. The advantages of SIMPLISMA modeling include: knowledge about the pure component spectra are not required, the purity and resolved spectra are visualized, and the overlapped IR peaks can be resolved.272 More details about SIMPLISMA modeling are described in Appendix 9.

In this chapter, the SIMPLISMA method is used for modeling the in situ IR spectra collected during the direct sol-gel process in CO2, and the resulting concentration-time curves are discussed. In addition, a curve-fitting method was also used to study the in situ IR spectra. The curve-fitting procedure consists of modeling an experimental spectrum using a sum of Gauss peak functions with a least residual sum of squares. The residual sum of squares refers to the residual sum of squared differences between the calculated spectrum and the original experimental data.

## 7.2. Experimental

In Situ IR Collection. The experiments were carried out in the 100 mL autoclave equipped with ATR-FTIR, as described in Figure 3.5 of Chapter 3. In the case of SiO2 aerogel synthesis, the temperature and pressure were controlled in the range of 40 – 60 °C and 1300 – 3000 psig, respectively, and the initial concentrations of TEOS and acetic acid were 0.088 M and 0.352 M, respectively. In the case of TiO2 aerogel synthesis, the temperature and pressure were at 60 °C and 4500 psig, respectively, and the initial concentrations of TIP and acetic acid were 1.10 M and 3.85 M (or 6.05 M), respectively. In the case of ZrO2 aerogel synthesis, the temperature and pressure were at 40 °C and 4500 psig, respectively, and the initial concentrations of ZBO and acetic acid were 0.547 and 1.76 M, respectively. In situ FTIR spectra were collected automatically using the ASI Applied System ReactIR 4000, at fixed intervals from 600 to 4000 cm-1 with a resolution of 2 cm-1.

Modeling. The curve fitting and SIMPLISMA modeling were carried out using the ACD UVIR Processor Version 8.0 software (ACD Inc., Toronto, Ontario). The Gaussian peak profile was used for curve fitting, and the limit of the half-peak width was set at 150 cm-1 for a better curve fit. The input spectra were not smoothed or pre-processed other than the declared cut-off of the inactive region. During SIMPLISMA modeling, the offset α was set as a default at 20 %.

## 7.3. Results and Discussion

### 7.3.1. Conversion of TEOS

Figure 7.1 shows the three-dimensional in situ FTIR spectra collected during TEOS reacting with acetic acid in CO2, which shows a gradual growth of the water peak at 3343 cm-1 and oxo bond peak at ~ 1066 cm-1 during the reaction times of 0-360 minutes.

Figure 7.1. Three-dimensional in situ FTIR spectra: 0.088 M TEOS reacting with 0.362M HOAc in CO2 at reaction times of 0-360 minutes and at 50 ºC and 3000 psig.

Self-Modeling. In order to decrease the interference from other components, a region of the spectra in Figure 7.1 was selected where the interested component exhibits significant peaks. In the case of TEOS and SiO2, the most significant peaks of Si-OEt are in the region of 750 -1250 cm-1. This spectral region is now ready for the self-modeling process (Figure 7.2).

Figure 7.2. In situ FTIR spectra of 0.088 M TEOS reacting with 0.362M HOAc in CO2 at reaction time of 0-360 minutes and at 50 ºC and 3000 psig.

Using the conventional SIMPLISMA, without second-derivative processing, no reasonable result was obtained, indicating that the pure variables do not exist for all components. By using the second-derivative, however, the SIMPLISMA process generated two resolved pure-component spectra and the concentration profiles (the statistics of the modeling is provided in Appendix 10). The resolved pure-component spectra match those of TEOS and SiO2 (Figure 7.3 a and b), indicating that the self-modeling was successful. The resulting relative concentration profiles of TEOS and SiO2 are shown in Figure 7.4. From this figure, it can be noticed that after a reaction time of 280 minutes, the Si-OEt bond concentration remained constant, while the product’s concentration still increased. As described in the introduction section, the Si-OEt bond converts into Si-acetate and Si-OH intermediates (Reactions 7.1 and 7.3) or directly converts into oxo bond (Reaction 7.5) during the polycondensation process. The intermediates can still produce oxo bond when the Si-OEt concentration becomes very low and maintains constant, typical of a condensation type polymerization.

Figure 7.3. Comparison of the self-modeling resolved spectra with (a) TEOS and (b) SiO2 aerogel spectra. The spectra of TEOS in (a) and SiO2 in (b) were experimentally collected by means of ATR-FTIR.

Figure 7.4. The relative concentration profiles obtained from the self-modeling method. The source IR data was obtained at 50 °C and 3000 psig, and the initial concentrations of TEOS and acetic acid was 0.088 and 0.362 M, respectively.

By applying the self-modeling method to the IR spectra that were collected at different reaction temperatures and pressures, the Si-OEt concentration profiles were obtained. The resulting Si-OEt concentration profiles were subsequently transferred into the conversion profiles versus the reaction time (Figures 7.5 – 7.6). It should be noted that the absolute concentration of Si-OEt is not necessary for calculation of the Si-OEt conversion. At a reaction time of zero, the relative concentration of Si-OEt is at a maximum. The Si-OEt conversion at the reaction time t can be calculated using Equation 7.19.

Conversion = (C0  - Ct)/C0                                         (7.19)

where, C0 and Ct are the relative concentrations of Si-OEt when the reaction time is zero and t, respectively.

Figure 7.5. Temperature’s effect on the precursor conversion within a reaction time of 0-360 minutes. The initial concentration of TEOS and acetic acid was 0.088 and 0.362 M, respectively, and the pressure was 3000 psig.

Figure 7.6. Pressure’s effect on the precursor conversion within a reaction time of 0-360 minutes. The initial concentration of TEOS and acetic acid was 0.088 and 0.362 M, respectively, and the temperature was 50 °C.

From the conversion-time curves in Figures 7.5-7.6, some conclusions can be made: the 100 % conversion of Si-OEt was never reached before a reaction time of 360 minutes under the given synthesis conditions, which is similar to the conventional sol-gel process where water was used as a reaction agent and an alcohol as a solvent;105 the reaction was favored by the higher reaction temperature and the lower reaction pressure. The temperature’s effect on the conversion indicates that the main reaction for Si-OEt consumption (the forward reactions in Equations 7.1, 7.3, and 7.5) is either an irreversible reaction or an endothermal reversible-reaction according to the Arrhenius equation (Equation 1.1), where a higher temperature results in a higher conversion. However, the pressure’s effect is difficult to be explained using transition state theory (Equation 1.2) without knowledge of which step is dominating the consumption of Si-OEt.83, 288 Although the effect of temperature and pressure on the oxo bond formation has been studied in Chapter 4, the results in Figure 4.5 and 6 may be complicated due to the overlapping of the IR peaks, as described earlier; on the other hand, the conversion of TEOS in Figures 7.5-7.6 are more reliable, because these results are based on the pure component concentrations.

It should be pointed out that these results were obtained at a relatively low initial concentration of TEOS, when there was no precipitate formed in the view cell, which was crucial to produce SiO2 nanoparticles.171 The low concentration resulted in a low absorbance and consequently a higher error for the calculated results.

### 7.3.2. Concentration Profiles of Ti-Acetate and TiO2 Aerogels

Figure 7.7 shows the three-dimensional in situ FTIR spectra during polycondensation of TIP with acetic acid at the reaction time of 10–3720 minutes. It can be observed that the product peaks experienced a sudden increase, which was due to the condensation kinetics, as will be explained further later. Figure 7.8 shows the two-dimensional spectra in the region of 600-1880 cm-1, in which a sudden increase of the product peaks can again be observed. The self-modeling was first carried out in the region of 800 – 1400 cm-1 where TIP exhibits significant peaks, and no spectrum of TIP was resolved from the mixture spectra. This indicates that the substitution of TIP with acetate was fast, and free TIP disappeared in a reaction time of less than 10 minutes, as the first spectrum was collected at 10 minutes.

Figure 7.7.  The three-dimensional in-situ FTIR spectra of 1.10 M TIP reacting with 3.85 M HOAc within a reaction time from 10 to 3720 minutes in CO2. The reaction temperature and pressure were 60 ºC and 4500 psig, respectively.

Figure 7.8. In situ FTIR spectra of 1.10 M TIP reacting with 3.85 M HOAc in CO2 within a reaction time from 10 to 3720 minutes, at 60 ºC and 4500 psig. The arrows show the absorbance change trend.

Due to the high initial concentrations of TIP and HOAc, the in situ IR spectra in Figure 7.8 show strong peaks of Ti-acetate bidentates in the region of 1400–1650 cm-1, where the self-modeling was carried out and two resolved spectra (Figure 7.9-7.10) and the concentration profiles (Figure 7.11) were obtained. Figure 7.9a (the black curve) shows one of the resolved spectra and the curve-fitting results. In this figure, the deconvoluted peaks are labeled as 2 or 3, which match the spectra of Ti6O6(OPri)6(OAc)6 (2) and Ti6O4(OPri)8(OAc)8 (3) in Figure 7.9b and c, respectively. This result indicates that mixed hexamers were formed during the sol-gel process. The formation of 2 or 3 hexamers from TIP and acetic acid in CO2 has been described in Chapter 5. The second resolved spectrum is close to that of the TiO2 aerogel (Figure 7.10), but the resolved peaks in the range of 1350-1600 cm-1 are wider than the aerogel peaks. The peak broadening in the resolved spectrum is probably due to the Lewis acid-Lewis base interaction between the acetate and the Lewis acids (e.g., acetic acid, isopropanol and CO2),289, 290 which are more fully described in Chapter 8. Saturation of the IR probe may also contribute to the peak broadening, as the peak absorbance was very high (Figure 7.8).

Figure 7.9.  FTIR. (a) The black curve is one of the resolved spectra from in situ IR and the curve-fitting results, the residual sum of squares: 4.02E-8; (b) and (c): the spectra of single crystals of 2 and 3, respectively. Note: the black curves = experimental or resolved IR spectra; the pink curve = the fitting curve; blue curves = the individual Gaussian function curves; and the red curve = the residual curve. The number 2 and 3 denote Ti6O6(OPri)6(OAc)6 and Ti6O4(OPri)8(OAc)8, respectively.

Figure 7.10.  (a) The other resolved spectrum from the in situ IR spectra, which is attributed to the aerogel product, and (b) TiO2 aerogel spectrum.

# The relative concentration profiles of the hexamer mixture and the TiO2 aerogel are shown in Figure 7.11. In the initial stage of the reaction, the hexamer concentration increased until the maximum was reached and then decreased gradually; after a critical point at 1800 minutes, a significant reduction in the concentration occurred at the reaction time of 1800–2040 minutes, followed by gradual decreasing. The product concentration experienced the identical, but opposite trend.

Figure 7.11. The relative concentration profiles during TIP reacting with HOAc in CO2 within a reaction time from 10 to 3720 minutes, at 4500 psig and 60 ºC; the initial concentration of TIP and HOAc was 1.10 and 3.85 M, respectively.

# Similar concentration profiles can be observed in Figure 7.12 where a higher acid/TIP ratio was applied, and the difference between Figure 7.12 and 7.11 is a shorter time for the sudden concentration change. In this case, the critical point was at a reaction time of 230 minutes, likely due to the higher acid/alkoxide ratio increasing the rate of reactions.

Figure 7.12. The relative concentration profiles during TIP reacting with HOAc in CO2 within a reaction time from 10 to 610 minutes, at 4500 psig and 60 ºC; the initial concentration of TIP and HOAc was 1.10 and 6.05 M, respectively.

# According to Figures 7.11 and 7.12, the formation of the product was accompanied with the consumption of the hexamers.

The phenomenon of a sudden change of concentration profiles was consistent with the phase observations obtained using the view cell reactor. The phase change can be described as four separate stages: (1) the initial phase was transparent with a light amber color during the first few hours to more than one day depending on the synthesis conditions; (2) the solution became red and translucent likely due to the growing and agglomeration of the colloidal particles,291 with this stage being relatively short, i.e. from 40 minutes to two hours; (3) it became opaque with white particles appearing, and the stirrer bar being still movable; and (4) the stirrer bar becoming immobile. The stages 1 to 4 correspond to the formation of hexamers, colloidal particles, larger particles and gel, respectively, which agrees with the in situ IR observations. According to the concentration profiles, the colloidal particle formation stage was abrupt, which likely happened in stage (2).

As the condensation of the metal complexes (in this case they are a mixture of complexes 2 and 3) can only take place on the OR group, the reactions for formation of the macromolecules can be written as:

Hydrolysis:

MxOy(OAc)z(OR)n+ H2O → MxOy(OAc)z (OR)n-1(OH) + ROH         (7.20)

Condensation 1:

MxOy(OAc)z (OR)n-1(OH) + MxOy(OAc)z(OR)n → M2xO2y+1(OAc)z(OR)2n-2 + ROH

(7.21)

Condensation 2:

2 MxOy(OAc)z (OR)n-1(OH) → M2xO2y+1(OAc)z(OR)2n-2 + H2O          (7.22)

Water is known to react with titanium alkoxides very quickly to form titanium oxide.292 From Equations 7.20-7.22, it can be anticipated that the process will be dominated by the reactions that generate water, since water was absent at the initial stages of the process. A hydroxylated metal complex MxOy(OAc)z(OR)n-1(OH) can react with either a nonhydroxylated MxOy(OAc)z(OR)n or another hydroxylated complex. Two cases will be discussed, as described below.

Case 1: if the nonhydroxylated complexes are more active, Condensation 1 (7.21) is close to or faster than condensation 2 (7.22). In this case, at the initial stage of the reaction when the concentration of the hydroxylated metal complexes is still low, they will have a higher possibility to react with the nonhydroxylated complexes, which generates alcohol. The alcohol slowly reacts with acetic acid and generates both water and an ester, and the water reacts with another nonhydroxylated complex. In this case, the kinetics is controlled by the slow esterification reaction that generates water, and a gradual reaction process can be anticipated.

Case 2: if the nonhydroxylated complexes are inactive, Condensation 1 (7.21) is much slower than condensation 2 (7.22). In this case, at the initial stage when the concentration of the hydroxylated metal complexes is still low, they do not have many possibilities to react with one another. Thus, a very slow start of the reactions can be expected. However, after a certain reaction time when the concentration of the hydroxylated complexes reaches a certain level, they are able to react with one another significantly and generate a large amount of water. Subsequently, the water will react quickly with more nonhydroxylated complexes and accelerate the reaction, leading to the concentration profiles shown in Figures 7.11 and 7.12, which are similar to self-catalysis reaction profiles described in the literature.293

Based on the above discussion, it can be rationalized that, during hydrolysis and condensation of the Ti complexes 2 and 3 into the colloidal particles, Condensation 1 should be much slower than Condensation 2.

### 7.3.3. Concentration Profiles of Zr-Acetate and ZrO2 Aerogels

Similar to the sol-gel chemistry of titanium alkoxides, when zirconium alkoxides react with acetic acid, they form zirconium acetate complex structures, in which there is unreacted ending alkoxide groups (-OR). Then, the alkoxide group is hydrolyzed and condensated with other metal-OH or metal-OR to form oxo bond, as shown in Equations 7.20-7.22.

# The three-dimensional in situ FTIR spectra collected during ZBO reaction with acetic acid in CO2 are shown in Figure 7.13, from which a gradual increase of water and product peaks can be observed. Figure 7.14 shows the two-dimensional spectra in the region 1300-1650 cm-1, where a gradual formation of product peaks can be observed.

Figure 7.13.   Three-dimensional in situ FTIR spectra during the direct sol-gel process of ZBO with acetic acid within a reaction time of 10-1330 minutes, at 40 °C and 4500 psig. The initial concentration of ZBO and acetic acid was 0.547 and 1.76 M, respectively.

Figure 7.14.  Two-dimensional in situ FTIR spectra during the direct sol-gel processing of ZBO with acetic acid within a reaction time of 10-1330 minutes, at 40 °C and 4500 psig. The initial concentration of ZBO and acetic acid was 0.547 and 1.76 M, respectively. The arrows indicate the absorbance change trend.

# Using the SIMPLISMA technique, similar to the cases of TIP as described earlier, no spectrum of ZBO was resolved from the mixture spectra in the region of 800 – 1300 cm-1 where ZBO exhibits significant peaks. This indicates the substitution of ZBO with acetate was also very fast. In the region of 1300–1650 cm-1, both the resolved component spectra and the concentration profiles were obtained (Figures 7.15 and 7.16).

Figure 7.15.  Two resolved spectra from the in situ IR spectra by means of SIMPLISMA modeling. One spectrum is attributed to the Zr-acetate complex and the other to the ZrO2 aerogel.

Figure 7.16.  The relative concentration profiles of Zr-acetate complex and the condensation product during the direct sol-gel processing of ZBO with acetic acid in scCO2 with a reaction time of 10-1330 minutes, at 40 °C and 4500 psig. The initial concentration of ZBO and acetic acid was 0.547 and 1.76 M, respectively.

# From the concentration profiles, one can see that the consumption of the Zr-acetate complex and formation of product were gradual, which was different from the case of TIP reacting with acetic acid. The kinetics of the process can be explained by case 1 (described above), where Condensation 1 is close to or faster than Condensation 2. The different kinetics between the Ti complexes and the Zr complexes can be explained by the different activity of the metal complexes. As described in Chapter 5 and 6, when the acid/Ti alkoxide ratio was 5.5, well-defined nanostructures were synthesized; on the other hand, when the acid/Zr alkoxide ratio was above 3.22, precipitate was produced. This indicates that both the Zr alkoxides and complexes are more active than the Ti alkoxides and complexes. As discussed earlier, the more active the complexes, the more likely the kinetics are similar to Case 1, i.e. controlled by the esterification reaction.

## 7.4. Conclusion

The in situ ATR-FTIR spectrometry was analyzed using the curve fitting and the self-modeling method, and the concentration profiles during the direct sol-gel process in CO2 were obtained. The resulting relative concentration profiles of the precursors, complex structures and products are of importance for understanding the direct sol-gel process in CO2. According to the calculated concentration profiles, the activities of TEOS, TIP and ZBO precursors with acetic acid were significantly different. For instance, the reactivity of TEOS was much lower than that of TIP and ZBO. Less than 100 % conversion from TEOS to SiO2 was obtained in 360 minutes at 60 °C. On the other hand, the Ti and Zr complexes were formed in 10 minutes at 60 and 40 °C, respectively, indicating that these precursors were more reactive. Additionally, the condensation kinetics of the Ti and Zr complexes was different: the consumption of the former was abrupt after a critical point, and that of the latter was gradual through the sol-gel process. The different kinetics can be explained by the activity of the complexes and the competition of the two condensation reactions.

# Stabilization of the Colloidal Particles in CO2

In this chapter, the interaction between CO2 and the colloidal particles is studied using both the approaches of ATR-FTIR spectrometry and solubility parameter methods based on Fedors’ equations. The study results show that the acetate group is CO2-philic and the SiO2, TiO2 and ZrO2 colloidal particles containing an acetate group can be stabilized in CO2.

## 8.1. Introduction

Due to the lack of polarity and dipole moment, scCO2 or subcritical CO2 is a poor solvent for most polar solutes and macromolecules. However, CO2 has a large quadrupole moment and a polar C=O bond, making a variety of materials soluble in scCO2.294 The interaction between CO2 and small molecules or polymers has been studied by ab initio calculations295, 296 and FTIR spectroscopy.289, 297, 298 CO2 may behave as both an electron acceptor and donor.290, 296 For example, the interaction of CO2 and the carbonyl functional group has been found to consist of a Lewis acid and Lewis base attraction (LA-LB) between the partial positive carbon of CO2 and the lone pairs of the carbonyl oxygen.289 As well, the C-H(((O hydrogen bond between CO2 and the LB site has been attributed to the high solubility of polymers with a carbonyl moiety in CO2.290

Understanding the nature of the interactions between colloidal particles and CO2 is of importance to design and synthesize well-defined oxide nanoarchitectures during the sol-gel process in scCO2 and subcritical CO2. During the synthesis of SiO2, TiO2 and ZrO2 nanoarchitectures in CO2 in the earlier part of this work, in situ FTIR spectra were used to study the mechanism and kinetics of the sol-gel processes. Figure 8.1 shows the in situ FTIR spectra during the alkoxides reacting with acetic acid, in which the absorbance peaks in the region of 1400-1600 cm-1 indicate the formation of M-acetate bidentates (M= Si, Ti, and Zr).229 Similar to the carbonyl group, the acetate bridging and chelating bidentate group may donate electrons to CO2 and result in LA-LB interactions (Figure 8.2). Because of the high intensity of bulk CO2 and interference of the organic species, it is not possible to directly observe LA-LB interactions between CO2 and the M-acetate group through the in situ IR spectra. Our strategy was to use ATR-FTIR to study the CO2-impregnated sol-gel product, i.e. TiO2 and ZrO2 aerogels, with the acetate bidentate groups.

Figure 8.1. In situ IR spectra: (a) 1.3 M TMOS reacting with 5.3 M HOAc in CO2 at a reaction time of 360 minutes, at 50 °C and 4000 psig; (b) 1.10 M TIP reacting with 3.85 M HOAc in CO2 at a reaction time 40 minutes, at 60 °C and 4500 psig; and (c) 0.547 ZBO reacting with 1.76 M HOAc in CO2 at a reaction time of 40 minutes, at 40 °C and 4500 psig.

Figure 8.2. Schematic drawing of possible LA-LB interactions between CO2 and (a) the bridging acetate bidentate, (b) the chelating acetate bidentate, and (c) the acetate monodentate.  M: Si, Ti or Zr.

To study the interaction between CO2 and the colloidal particles semi-quantitatively, the solubility parameter method was used. The solubility parameter () is defined as the square root of the cohesive energy density () by Hildebrand:299

(8.1)

Solubility parameters provide a simple approach to predict the solubility behavior of the components, based on the knowledge of the individual components alone.300 As a result, solubility parameters have been widely used for correlating the interactions of solutes and solvents. For instance, the solubilities of Cu(II) and Cr(III) complexes in scCO2 have been studied using the Hildebrand equation and a group contribution method;301 the low solubility parameters of siloxane and fluoroalkyl groups were partially attributed to their CO2-philicity.302 In this chapter, Allada’s method and mixing rules were used to estimate the solubility parameters of CO2 and the solvent mixture, respectively.303, 304 The solubility parameters of macromolecules were estimated using Fedors’ group contribution method.305 Using the solubility parameter approach, the previous experimental conditions for stabilizing the colloidal particles can be justified.

## 8.2. Experimental

The TiO2 and ZrO2 aerogel particles (denoted as a-TiO2 and a-ZrO2, respectively) were synthesized using the methods previously described (Chapters 5 and 6). A-TiO2-A and a-TiO2–B aerogel were synthesized using 1.10 M titanium(IV) isopropoxide and 1.10 M titanium(IV) butoxide polycondensated with 4.95 M and 6.05 M acetic acid, respectively, at 40 (C and 6000 psig of scCO2. A-ZrO2 was synthesized using 1.13 M zirconium butoxide reacting with 2.52 M acetic acid at 40 (C and 6000 psig of scCO2. Since aerogels are well-known to adsorb significant quantities of water or organic solvents that also interact with CO2, special attention was made to dry the aerogels. ScCO2 drying and vacuum drying at 120 (C and 0.8 pa was conducted until the IR spectrum showed no traces of water peaks at 3000-3600 cm-1. Samples of the dried aerogels were calcined at 500 (C to obtain oxides.

The dried aerogels, with and without calcination, were studied using ATR-FTIR spectroscopy (ReactIR 4000, ASI Applied System Inc.). The experimental setup was described in detail in Chapter 3. Since the ATR-FTIR can only detect materials a few microns from the mirror, the absorbance peaks of powder is low. In order to obtain significant peaks, the aerogel powder was pressed against the diamond mirror by using the agitation shaft with a rubber disk in between (Figure 8.3). The spectra of the pure aerogels were collected before addition of CO2. Then, the temperature and pressure were kept at 40 (C and 4000 psig for 30 minutes after addition of CO2. Because of the strong absorbance of bulk CO2, which prevents clear observation of CO2 interacting with the aerogel, FTIR spectra were collected 1 minute after venting of CO2 from the autoclave when adsorbed CO2 was still present. FTIR spectra were collected from 600 to 4000 cm-1 with a resolution of 2 cm-1. The subtraction and curve fitting of the IR spectra were obtained using ACD UVIR Processor version 7.0 software (ACD Inc. Toronto, Ontario). The curve fitting was processed by assuming a Gaussian peak profile, and the limit of the half-peak width was set as 80 cm-1 for a better curve fit.

Figure 8.3. Schematic drawing of ATR-FTIR analysis. The aerogel powder was pressed against the diamond mirror to obtain higher absorbance peaks.

## 8.3. Results and Discussion

### 8.3.1. FTIR Spectroscopy and LA-LB interaction

Figure 8.4 shows the spectra of both the pure and CO2-impregnated aerogels of a-TiO2-A, a-TiO2-B and a-ZrO2. In the spectra, the peaks in the region of 1400-1600 cm-1 are attributed to M-acetate bidentate,229 those at 1325-1346 cm-1 to hydrocarbon groups,306 that at 1118 cm-1 to M-O-C, those at 1025-1026 cm-1 to bridging OR groups,228 and those lower than 900 cm-1 to oxo bonds. In the spectra of CO2-impregnated a-TiO2-A, a-TiO2-B and a-ZrO2, besides the peaks from the pure aerogels in the region of 680 –1680 cm-1, there are new peaks at 668, 654, 649 and 648 cm-1. The very sharp peak at 668 cm-1 is due to free CO2, while the relatively wide peaks in the 642-654 cm-1 region are the overlapping results of ν2 bending vibration of the impregnated CO2 and vibration of the oxo bonds.289

Figure 8.4. The ATR-FTIR spectra of (a) a-TiO2-A, (b) a-TiO2-B and (c) a-ZrO2 before addition of CO2 (black) and at one minute after venting of CO2 (red).

In order to examine the vibration wavenumbers of the impregnated CO2, subtraction of the corresponding aerogel spectrum is necessary. Figure 8.5 presents the spectra of CO2 impregnated in the aerogels after the subtraction and the curve-fitting results. The peaks in the region of 630–665 cm-1 were attributed to CO2 ν2 vibration splitting. Understanding the complex peaks requires a careful consideration of the electronic structures of metal-acetate and the nature of CO2 ν2 vibration.

Figure 8.5.  The IR spectra and the curve-fitting results of CO2 interacting with (a) a-TiO2-A, the residual sum of squares: 3.86E-3; (b) a-TiO2-B, the residual sum of squares: 4.01E-4; and (c) a-ZrO2, the residual sum of squares: 1.81E-3. Note: the black curves = experimental spectra; the pink curve = the fitting curve; blue curves = the individual Gaussian function curves; and the red curve = the residual curve.

In the bridging acetate bidentate, the atoms of the bridging carbon, oxygen and metal are sitting almost in one plane, as shown in Figure 8.2a. The π electrons are delocalized around the two bridging oxygen atoms and the α-carbon atom, which are sp2 hybridized. Previous studies by others showed that the chemical bond between transition metals and the oxygen of the bridging carboxylate is due to the overlap of the d orbital of the former, and the p orbital of the latter.307-311 Besides the p orbital and one σ bond (O-C), each of the two oxygen atoms still has two lone pairs, as shown in Figure 8.6. When a CO2 molecule approaches the lone pairs, the partial positive carbon can associate with the sp2 oxygen as either in plane or out-of-plane due to the LA-LB interaction, where the plane is defined as the lone pairs of the oxygen. The π bond of the bridging acetate is also an electron donor and has potential to interact with the partially positive carbon atom of CO2.

When we consider the molecular structure of CO2, there are two IR active bending modes. In the case of free CO2, the two bending vibrations absorb at the same frequency due to the symmetry of the CO2 molecule (Figure 8.7). In the case of LB-associated CO2, it is expected that the degeneracy would disappear, and two absorption peaks (in-plane and out-of-plane) will appear for each LA-LB association mode. From our IR experimental results, there are two distinct peaks (at 663 and 657 cm-1 before curve-fitting, and at 663 and 655 cm-1 after curve-fitting) from a-TiO2-A associated CO2 (Figure 8.5). This result is in a good agreement with the literature that CO2 bending peaks shifted to 662 and 654 cm-1 resulting from the carbonyl group of PMMA.289 This suggests that the split of CO2 ν2 vibration is mainly due to the lone pairs of the oxygen atom. In the case of a-TiO2-B and a-ZrO2 associated CO2, however, there is a wider combined peak. Four individual peaks were produced after curve-fitting, indicating more than one association mode exists, either due to the lone pairs or from the π bond. There is noticeable difference between the IR spectra of CO2 impregnated into a-TiO2-A and a-TiO2–B (Figure 8.5). This difference cannot be easily explained, because the detailed structures around the bridging acetate remain unknown. However, we may exclude the effect of the alkoxide groups in a-TiO2-A and -B, which are isopropoxide and n-butoxide, respectively, because of their small amounts in the aerogels, as shown by the IR spectra (Figure 8.4).

Figure 8.6.  Schematic of possible association modes of LA-LB interaction between CO2 and metal bridging acetate. (a) d-p orbital overlap between metal (M) and acetate, and CO2 associates with the π bond either in a vertical or a parallel mode; (b) the partial positive carbon CO2 associates with the lone pairs of oxygen either in T-shape or bended T-shape.

Figure 8.7.  The bending and stretching vibrations of a free CO2 molecule.  The two bending vibrations absorb at the same frequency of IR beam due to the symmetry of the CO2 molecule.

Figure 8.8 shows the IR spectra of CO2 impregnated into a-TiO2-A, a-TiO2-B and a-ZrO2 in the ν3 stretching mode region. These spectra show a high peak at 2337 cm-1 and an asymmetric wide peak around 2358 cm-1. The peak at 2337 cm-1 is assigned to the free CO2, while the small right shoulder of the peak at 2337 cm-1 can be assigned to the (ν2 + ν3) - ν3 band.289 The peak at 2358 cm-1 is due to the interaction between CO2 and the aerogels that caused the CO2 ν3 stretching mode split. When we compare Figure 8.8a and d, the free CO2 peak at 2337 cm-1 decreased faster than the peak at 2358 cm-1, suggesting that the free CO2 weakly interacts with the aerogel.

Figure 8.8.  IR spectra of CO2 impregnated into (a) a-TiO2-A, (b) a-TiO2-B and (c) a-ZrO2 in the ν3 stretching mode region, at one minute after venting of CO2; (d) CO2 impregnated into a-TiO2-A at five minutes after venting of CO2.

It is necessary to point out that the above discussion of the LA-LB interaction was based on the structure of the metal bridging acetate obtained from single crystal analysis. Although the IR spectra in Figure 8.4 indicates that the acetate bidentate structure remains in the aerogels, the detailed structure of the chemical environment around the acetate in the aerogels is unknown. From the IR experimental results, we cannot determine the exact LA-LB association mode; however, the splitting of the CO2 ν2 peak strongly supports that CO2 acts as an electron accepter.

From an electronic structure point of view, the above discussion has described the LA-LB interaction between a CO2 molecule and an aerogel with a complex metal-bridging acetate. In addition, a semi-quantitative study on the interaction can be carried out by calculation of the solubility parameters (δ) of the colloidal particles and comparison with that of the CO2-based reaction solvent.

### 8.3.2. Solubility Parameter Study

Estimation of ( of CO2. The solubility parameters of CO2 can be calculated either from the density by using Giddings Equation304 or from the models developed from an empirical equation of state (EOS).300, 303 According to Giddings et al.,312

(8.2)

where, is the critical pressure in atmospheres,  is the reduced density of CO2, = 2.66 is the reduced density of liquid CO2 at its normal boiling point,304 and  is the density of CO2 in mol/L. Giddings’ equation correctly predicts that a higher density of CO2 results in a higher solubility parameter; however, it was found to be poor for quantitative predictions.300 By using the EOS of Huang et al, Williams et al recently calculated the solubility parameters of CO2 under a variety of temperatures and pressures, and the calculated results were close to Allada’s.300 In Table 8.1, the solubility parameters of CO2 obtained from Allada’s method are listed, under the typical conditions at which the direct sol-gel synthesis in scCO2 was carried out in this thesis.

Table 8.1.  Solubility parameters of scCO2 under selected temperatures and pressures. 300, 303

| Temperature (°C) | 40 | 40 | 60 | 60 | 60 |
| --- | --- | --- | --- | --- | --- |
| Pressure (psia) | 4000 | 6000 | 4000 | 5000 | 6000 |
| Solubility parameters, (cal/cm3)1/2 | 6.99 | 7.46 | 6.23 | 6.65 | 6.83 |

Estimating ( of Alkoxides. The solubility parameters of solvents and small molecules can be calculated from the cohesive energy density or the molar energy of vaporization:313

(8.3)

where,  is the energy change upon isothermal vaporization of the saturated liquid to the ideal gas state at infinite dilution in cal/mol,  is the molar volume of the liquid in cm3/mol,  is the enthalpy change during vaporization in cal/mol,  is the gas law constant in cal/(mol·K), and  the temperature in K.

Using Equation 8.3 and the thermodynamic data from Bradley in Table 8.1,314, 315 the solubility parameters of titanium alkoxides at 298 K were calculated as presented in Table 8.2.

Table 8.2. The thermodynamic properties and the average solubility parameters of the alkoxides.

| Molecule | (Hf0 * (liquid) Kcal/mol | (Hf0 * (gas) Kcal/mol | (HV0 * Kcal/mol | 0(liquid) cm3/mol | ( (cal/cm3)1/2 |
| --- | --- | --- | --- | --- | --- |
| Ti(OPri)4 | -377** | -360** | 17 | 296*** | 7.44 |
| Ti(OBun)4 | -399** | -377** | 22 | 340*** | 7.93 |
| Note: * (Hf0, (HV0 and 0 denote the standard formation enthalpy, the enthalpy change of vaporization and the molar volume of the liquid, respectively. ** Ref. 314 *** The molar volume was calculated from the density at 293 K. The liquid volume change was neglected for temperature changes from 293 to 298 K. |

Estimating ( of Ti-acetate complexes and macromolecules. Fedors’ group contribution method has been widely used to estimate the solubility parameters of a variety of materials.316-318 This method is especially attractive when vaporization energies of the interested materials are available, as in the case of metal alkoxides. According to Fedors, the solubility parameters of small molecules and macromolecules can be calculated by using Equations 8.4 and 8.5, respectively.305, 319

(8.4)

where, Δei is the energy of vaporization in cal/mol, and Δυi the mole volume in cm3/mol. In the case of macromolecules,305

(8.5)

where Δeir is the energy of vaporization of the repeating unit in cal/mol, and Δυir is the mole volume of the repeating unit in cm3/mol. The related atomic and group contributions to the energy of vaporization and mole volume at 298 K are listed in Table 8.3.305 The detailed calculations of Ti atom’s group contributions are described in Appendix 11.

Table 8.3. The related atomic and group contributions to the energy of vaporization and mole volume at 25 °C.305

| Atom or group | Δei (cal/mol) | Δυi (cm3/mol) |
| --- | --- | --- |
| CH3 | 1125 | 33.5 |
| CH2 | 1180 | 16.1 |
| CH | 820 | -1.0 |
| COO | 4300 | 18.0 |
| O | 800 | 3.8 |
| Ti * | 500 ** | 7.2** |
| Note: * Calculated in this work. ** The values were the average calculated from the thermodynamics data of TIP and TBO in Table 8.2 using Equation 8.3 and 8.4. |

The titania colloidal particles were derived from the condensation of the hexamer complexes,105, 320 such as Ti6O6(OPri)6(OAc)6 (2) and Ti6O4(OBun)8(OAc)8 (1). Since the condensation takes place on the OR groups,105 the repeating unit of the macromolecules of a-TiO2-1 and a-TiO2-2 can be estimated to be -(Ti6O12(OAc)6)-, and -(Ti6O12(OAc)8)-, respectively. In the case of the SiO2 and ZrO2 colloidal particles, there is no building-block information available (i.e. crystal structure data). Based on the values in Table 8.3, the solubility parameters of the macromolecules with repeating units of -(Ti6O12(OAc)6)-, and -(Ti6O12(OAc)8)- can be calculated as shown in Table 8.4 (The detailed calculation is described in Appendix 11).

Table 8.4. Solubility parameters of the macromolecules calculated using the group contribution method.

| Repeating Unit | Δeir (cal/mol) | Δυir (cm3/mol) | δ (cal0.5cm-1.5) |
| --- | --- | --- | --- |
| -(Ti6O12(OAc)6)- | 45.2 ×1000 | 397.8 | 10.7 |
| -(Ti6O12(OAc)8)- | 56.0 ×1000 | 500.8 | 10.6 |
| -(Ti6O12)- * | 12.6 ×1000 | 88.8 | 11.9 |
| Note: * The imaginary repeating unit for comparison of with and without acetate. |

According to the results from Table 8.4, the solubility parameters of the macromolecules with acetate group are approximately 10.7 cal0.5cm-1.5. For comparison purpose, the solubility parameters of the corresponding macromolecules without bridging acetate were also calculated, which are approximately 11.9 cal0.5cm-1.5. The results show that the bridging acetate results in a lower solubility parameter which is closer to that of CO2, e.g., at 40 °C and 6000 psig when the solubility parameter is 7.46 cal0.5cm-1.5, and a favorable stabilization of the colloidal particles can be expected.

From the above study, we can see that the solubility parameter of the colloidal particles with Ti-acetate groups is still larger than that of CO2 under the utilized synthesis conditions. It can be expected that addition of a cosolvent may improve the solubility of the macromolecules in CO2. In fact, during the synthesis of the aerogel particles, extra acetic acid was added (Chapters 4-6), and in the case of ZrO2, extra alcohol was added (Chapter 6). In addition, the ester and alcohol were generated as by-products during the process. The polar organic species generally exhibit higher solubility parameters. For example, acetic acid, isopropanol and isopropyl acetate have solubility parameters of 9.83, 11.55 and 8.51 cal0.5cm-1.5, respectively.321 It can be anticipated that the existence of these species in CO2 will increase the solubility parameter. Using Equation 8.6, the solubility parameter of the mixed solvent can be calculated:321, 322

(8.6)

where,  is the solubility parameter of the mixed solvent, and  and  are the volume fraction and the solubility parameter of solvent i, respectively. For example, in a typical synthesis of titania nanomaterials, the volume fractions of acetic acid and CO2 are about 0.27 and 0.73, respectively.320 The calculated solubility parameter of the mixture of acetic acid and CO2 at 40 °C and 6000 psi is 8.10 cal0.5cm-1.5, with an increase of 8.6% from 7.46 cal0.5cm-1.5 of pure CO2. Even though the acetic acid is consumed during the reactions, the resulting ester, water and alcohol will compensate for the consumed acetic acid in regards to .

## 8.4. Conclusion

This research shows that the M-acetate group on the colloidal particles is CO2-philic, which is similar to C-F and carbonyl groups.289, 301, 302, 323 According to the FTIR study on the CO2 impregnated into the aerogels, it can be concluded that a LA-LB interaction exists between CO2 and the M-acetate groups. The electronic structure of the M-acetate shows the possible association modes, even though the exact modes cannot be discerned through the experimental results. The interactions have also been studied semi-quantitatively using a solubility parameter approach. The results show that the acetate group can decrease the solubility parameters of the macromolecules, which improves the interaction with CO2. This further confirms that the acetate group is the CO2-philic domain on the colloidal particles. However, the acetate group cannot make the solubility parameter of the macromolecules as low as that of CO2 under the operational synthesis conditions. The existence of cosolvent can promote the solubility parameter of the solvent mixture, which also contributes to the stabilization of the colloidal particles.

# Summary and Conclusions

## 9.1. Outline

The successful synthesis of well-defined SiO2, TiO2 and ZrO2 nanomaterials shows that the direct sol-gel process in CO2 is a promising technique. The advantages of this method include: (1) a high conversion, e.g. about 98 % conversions for TiO2 and ZrO2 aerogels; (2) a high yield, e.g. 20 g of TiO2 monolith was synthesized in a 100 ml autoclave; (3) a high surface area, e.g. the surface areas of TiO2 anatase were as high as 105-181 m2/g; and (2) environmental benignness. The disadvantages involve the relatively high-pressure apparatus, although this is not generally considered high pressure by industrial standards.

Although the chemistry of the direct sol-gel process of SiO2, TiO2 and ZrO2 in CO2 is relatively complex and different from one another, the reactions can be summarized as substitution, esterification, hydrolysis and condensation.

CO2 was also found to be a superior solvent for the sol-gel process. Because of the CO2-philicity of the metal-acetate group, the colloidal particles were stabilized by CO2. In addition, scCO2 exhibits a low interfacial tension, and is able to penetrate into the nanoparticles.324 This allows heterogeneous reactions taking place and formation of the well-defined gel network. Furthermore, scCO2 extraction and drying maintain a high surface area of the resulting materials.

During the sol-gel process in CO2, the temperature and pressure were in the range of 40-70 (C and 2000-7000 psig. This is because, at this temperature and pressure range, the system was homogenous at the initial stage, which is critical for formation of well-defined nanostructures. The optimum temperature and pressure were theoretically justified by the solubility parameters of CO2 and colloidal particles.

## 9.2. Synthesis, Characterization and Mechanism Studies

In order to synthesize the oxide nanomaterials, the direct sol-gel process in CO2 was carried out in either a view cell or an autoclave. The starting materials were mixed before addition of CO2 using a syringe pump. The system was maintained at a constant temperature and pressure until the nanomaterials were formed. In order to obtain TiO2 particles, CO2 was removed through either a quick depressurization or a RESS process before agglomeration took place. In the case of TiO2 and ZrO2, fresh CO2 was slowly passed through the reactor in order to extract the organic species and to maintain the nanomaterial microstructure.

In order to crystallize the amorphous resulting nanomaterials, calcination was carried out in the furnace at a temperature 380-600 °C. The nanomaterials were characterized by using electron microscopy, N2 physisorption, FTIR, XRD and thermal analysis.

The mechanism of nanomaterial formation, the kinetics of sol-gel reactions, and the interactions between CO2 and the Ti-acetate were studied by using ATR-FTIR spectrometry. The formation of TiO2 nanofibers was attributed to presence of the Ti-acetate hexamers that lead to one-dimensional condensation. In the case of SiO2 synthesis, the conversion of the precursor TEOS was favored by a higher temperature and lower pressure. In the cases of TiO2 and ZrO2 synthesis, the precursors quickly reacted with acetic acid to form metal acetate complexes, and the complexes consequently condensed into sol and gel either gradually or quickly after a critical point. The LA-LB interactions between CO2 and the metal-acetate were studied using ATR-FTIR spectrometry. The solubility parameter calculation results showed that the metal-acetate group is CO2-philic.

## 9.3. Chemistry of the Direct Sol-gel Process in CO2

In the sol-gel process, acetic acid has been used as a polycondensation agent for various alkoxides in CO2. The first step involves a substitution reaction, which resulted in alcohol. In the second step, the alcohol reacts with acetic acid and water is produced through esterification. Then, the generated water leads to hydrolysis and then subsequent condensation. The reactions can be written as:

Substitution :

≡M-OR + HOAc ⇌  ≡MOAc + ROH                             (9.1)

Esterification :

HOAc + ROH ⇌ ROAc + H2O                                  (9.2)

Hydrolysis :

H2O + ≡M-OR ⇌  ≡M-OH + ROH                              (9.3)

Condensation :

≡M-OH + ≡M-OR ⇌ ≡M-O-M≡ + ROH                      (9.4)

≡M-OH + ≡M-OH ⇌ ≡M-O-M≡ + H2O                       (9.5)

Where, M = Si, Ti or Zr ; R = Me, Et, Pri, Pr or Bu.

Although the reactions are very complicated after formation of oligomers and metal complexes, reactions 9.1-5 can be used as the general reactions for the sol-gel process in CO2.

## 9.4. The Synthesis Parameters of Direct Sol-Gel Process in CO2

During the aerogel synthesis processes, important parameters include: the temperature, pressure, concentrations of the reactants, scCO2 wash, and flow rate of CO2.

In this study, the temperature and pressure’s effect on TEOS conversion was studied by using the in situ IR spectrometry. It was found that a higher temperature and a lower pressure facilitate the consumption of Si-OEt. Surprisingly, in the range of 40-70 °C and 2000-7000 psig, there was no detectable effect of temperature and pressure on the TiO2 morphology. However, the reactants’ concentrations, especially the acid/alkoxide ratio, had a significant effect on the resulting oxide nanomaterials. In the case of SiO2, high concentrations of starting materials resulted in badly agglomerated micron-size particles. In the case of TiO2, different acid ratios resulted in different morphologies, i.e. fibers or spheres. In the case of zirconia, high concentrations of starting materials resulted in formation of mesoporous monolith, and low concentrations resulted in formation of spherical nanoparticles.

The CO2 flow rate during the extraction and venting step is also important to maintain the microstructure and a large surface area of the resulting materials. For example, when the reactor was less than 100 ml, a CO2 flow rate less than 1 ml/min was necessary.

## 9.5. Future Work Recommendation

Recommendations for future work include:

1. Study the effect of temperature and pressure on the kinetics of sol-gel synthesizing TiO2 and ZrO2 in CO2 using the in situ ATR-FTIR technique, which was not studied in this research.

2. Study the solubility of the precursors, e.g. TIP and ZBO in CO2 under various temperatures and pressures. Use the experimental data and empirical equations to estimate various important physical properties such as the critical points of metal alkoxides, which are useful for stringent thermodynamic studies.

3. Synthesis of other oxides or hybrid oxides using the direct sol-gel process in CO2. The successful synthesis of the oxide nanomaterials in this research is encouraging to extend the method for synthesizing other oxides, such as Al2O3, ZnO, and Fe2O3 and the hybrid materials.

4. Besides acetic acid, other carboxylic acids and polycarboxylic acids may also have potential to be used as polycondensation agents. Different molecular structures of the polycondensation agents may result in the formation of nanomaterials with different morphologies.

Bibliography

1.	Niederberger, M.; Garnweitner, G.; Buha, J.; Polleux, J.; Ba, J.; Pinna, N., Nonaqueous synthesis of metal oxide nanoparticles: Review and indium oxide as case study for the dependence of particle morphology on precursors and solvents. Journal of Sol-Gel Science and Technology 2006, 40, 259-266.

2.	Oskam, G., Metal oxide nanoparticles: synthesis, characterization and application. Journal of Sol-Gel Science and Technology  2006, 37, 161-164.

3.	Raveendran, P.; Fu, J.; Wallen, S. L., A simple and " green " method for the synthesis of Au, Ag, and Au-Ag alloy  nanoparticles. Green Chemistry 2006, 8, 34-38.

4.	Schultz, E., Fully Exploiting the Potential of the Periodic Table through Pattern Recognition. J Chem Educ 2005, 82, 1649.

5.	Walcarius, A.; Mandler, D.; Cox, J. A.; Collinson, M.; Lev, O., Exciting new directions in the intersection of functionalized sol-gel materials with electrochemistry. Journal of Materials Chemistry  2005, 15, 3663-3689.

6.	Gupta, G.; Shah, P. S.; Zhang, X.; Saunders, A. E.; Korgel, B. A.; Johnston, K. P., Enhanced Infusion of Gold Nanocrystals into Mesoporous Silica with Supercritical Carbon Dioxide. Chem Mater 2005, 17, 6728-6738.

7.	Do, T.-O., Nano - particles: potential  applications  in catalysis and nanotechnology. Recent Research Developments in Chemistry 2004, 2.

8.	Tarascon, J.-M.; Grugeon, S.; Laruelle, S.; Larcher, D.; Poizot, P., The key role of  nanoparticles  in reactivity of 3d metal  oxides  toward lithium. Lithium Batteries       2004, 220-246.

9.	Martin, C. R.; Kohli, P., The emerging field of nanotube biotechnology. Nat Rev Drug Discovery 2003, 2, 29-37.

10.	Zhou, S.; Wu, L.; Xiong, M.; He, Q.; Chen, G., Dispersion and UV-VIS properties of  nanoparticles  in coatings. Journal of Dispersion Science and Technology  2004, 25, 417-433.

11.	Pena, J.; Vallet-Regi, M.; San Roman, J., TiO2-polymer composites for biomedical applications. J Biomed Mater Res 1997, 35, 129-134.

12.	Gangopadhyay, R.; De, A., Conducting Polymer Nanocomposites: A Brief Overview. Chem Mater 2000, 12, 608-622.

13.	Min, B. K.; Santra, A. K.; Goodman, D. W., Understanding silica-supported metal  catalysts: Pd/silica as a case study. Catalysis Today  (2003),  2003, 85, 113-124.

14.	Somorjai, G. A.; Rioux, R. M., High technology catalysts towards 100% selectivity: Fabrication, characterization and reaction studies. Catalysis Today 2005, 100, 201.

15.	Zhang, S.-W.; Zhou, S.-X.; Weng, Y.-M.; Wu, L.-M., Synthesis of SiO2/Polystyrene Nanocomposite Particles via Miniemulsion Polymerization. Langmuir 2005, 21, 2124-2128.

16.	Ahn, J.-H.; Wang, G. X.; Liu, H. K.; Dou, S. X., Nanoparticle-dispersed PEO polymer electrolytes for Li batteries. J Power Sources 2003, 119-121, 422-426.

17.	Buck, S. M.; Koo, Y.-E. L.; Park, E.; Xu, H.; Philbert, M. A.; Brasuel, M. A.; Kopelman, R., Optochemical nanosensor PEBBLEs: photonic explorers for bioanalysis with biologically localized embedding. Current Opinion in Chemical Biology 2004, 8, 540.

18.	Brongersma, M. L., Nanoscale  photonics: Nanoshells: gifts in a gold wrapper. Nature Materials    2003, 2, 296-297.

19.	Barbé, C.; Bartlett, J.; Kong, L.; Finnie, K.; Lin, H. Q.; Larkin, M.; Calleja, S.; Bush, A.; Calleja, G., Silica Particles: A Novel Drug-Delivery System. Advanced Materials 2004, 16, 1959-1966.

20.	Schneider, M.; Baiker, A., Titania-Based Aerogels. Catal Today 1997, 35, 339-365.

21.	Gratzel, M., Solar Energy Conversion by Dye-Sensitized Photovoltaic Cells. Inorg Chem 2005, 44, 6841-6851.

22.	Mor, G. K.; Shankar, K.; Paulose, M.; Varghese, O. K.; Grimes, C. A., Use of Highly-Ordered TiO2 Nanotube Arrays in Dye-Sensitized Solar Cells. Nano Lett 2005.

23.	Bisquert, J.; Cahen, D.; Hodes, G.; Ruhle, S.; Zaban, A., Physical Chemical Principles of Photovoltaic Conversion with Nanoparticulate, Mesoporous Dye-Sensitized Soalr Cells. J. Phys. Chem. B 2003, 108, 8106-8118.

24.	Akbar, S.; Yoo, S., Ceramic nano-structure for chemical sensing. Chemical Sensors 2004, 20, 30-31.

25.	Wang, R.; Hashimoto, K.; Fujishima, A.; Chikuni, M.; Kojima, E.; Kitamura, A.; Shimohigoshi, M.; Watanabe, T., Light-induced amphiphilic surfaces. Nature 1997, 388, 431-432.

26.	Yu, D.-G.; An, J. H.; Bae, J. Y.; Ahn, S. D.; Kang, S.-Y.; Suh, K. S., Preparation of Titanium dioxide/poly(methyl methacrylate-co-n-butyl acrylate-co-methacrylic acid) hybrid composite particles via emulsion polymerization. J Appl Poym Sci 2005, 97, 72-79.

27.	Petrella, A.; Tamborra, M.; Curri, M. L.; Cosma, P.; Striccoli, M.; Cozzoli, P. D.; Agostiano, A., Colloidal TiO2 Nanocrystals/MEH-PPV Nanocomposites: Photoelectrochemical Study. J Phys Chem B 2005, 109, 1554-1562.

28.	Hu, Q.; Marand, E., In situ formation of nanosized TiO2 domains within poly(amide-imide) by a sol-gel process. Polymer 1999, 40, 4833-4943.

29.	Fernandez-Garcia, M.; Martinez-Arias, A.; Hanson, J. C.; Rodriguez, J. A., Nanostructured Oxides in Chemistry: Characterization and Properties. Chem Rev 2004, 104, 4063-4104.

30.	Cimino, S.; Pirone, R.; Lisi, L., Zirconia supported LaMnO3 monoliths for the catalytic combustion of methane. Appl Catal B-Environ 2002, 35, 243-254.

31.	Bahamonde, A.; Campuzano, S.; Yates, M.; Salerno, P.; Mendioroz, S., Influence of zirconia raw materials on the development of DeNOx monolithic catalysts. Appl Catal B-Environ 2003, 44, 333-346.

32.	Diamant, Y.; Chappel, S.; Chen, S. G.; Melamed, O.; Zaban, A., Core-shell nanoporous electrode for dye sensitized solar cells: the effect of shell characteristics on the electronic properties of the electrode. Coordination Chemistry Reviews 2004, 248, 1271.

33.	Yamahara, K.; Sholklapper, T. Z.; Jacobson, C. P.; Visco, S. J.; De Jonghe, L. C., Ionic conductivity of stabilized zirconia networks in composite SOFC electrodes. Solid State Ionics 2005, 176, 1359.

34.	Morita, Y.; Nakata, K.; Kim, Y.-H.; Sekino, T.; Niihara, K.; Ikeuchi, K., Wear properties of alumina/zirconia composite ceramics for joint prostheses measured with an end-face apparatus. Bio-Medical Materials and Engineering 2004, 14, 263-270.

35.	Fendler, J. H., Self-Assembled Nanostructured Materials. Chem Mater 1996, 8, 1616-1624.

36.	Lin, J.; Lin, Y.; Liu, P.; Meziani, M. J.; Allard, L. F.; Sun, Y. P., Hot-Fluid Annealing for Crystalline Titanium Dioxide Nanoparticles in Stable Suspension. J Am Chem Soc 2002, 124, 11514-11518.

37.	Chen, H.; Dai, K.; Peng, T.; Yang, H.; Zhao, D., Synthesis of thermally stable mesoporous titania nanoparticles via amine surfactant-mediated templating method. Mater Chem Phys 2006, 96, 176.

38.	Oh, C. W.; Seong, G.-D. L.; Park, S.; Ju, C.-S.; Hong, S.-S., Synthesis of nanosized TiO2 particles via ultrasonic irradiation and their photocatalytic activity. Reaction Kinetics and Catalysis Letters 2005, 85, 261.

39.	Cushing, B. L.; Kolesnichenko, V. L.; O'Connor, C. J., Recent Advances in the Liquid-Phase Syntheses of Inorganic Nanoparticles. Chem Rev 2004, 104, 3893-3946.

40.	Moran, P. D.; Bartlett, J. R.; Bowmaker, G. A.; Woolfrey, J. L.; Cooney, R. P., Formation of TiO2 sols, gels and nanopowders from hydrolysis of Ti(OiPr)4 in AOT reverse micelles. Journal of Sol-Gel Science and Technology 1999, 15, 251-262.

41.	Li, D.; Xia, Y., Direct Fabrication of Composite and Ceramic Hollow Nanofibers by Electrospinning. Nano Lett 2004, 4, 933-938.

42.	Li, D.; Xia, Y., Fabrication of titania nanofibers by electrospinning. Nano Lett 2003, 3, 555-560.

43.	Shao, C.; Guan, H.; Liu, Y.; Gong, J.; Yu, N.; Yang, X., A novel method for making ZrO2 nanofibres via an electrospinning technique. J Cryst Growth 2004, 267, 380-384.

44.	Kim, C. S.; Okuyama, K.; Nakaso, K.; Shimada, M., Direct measurement of nucleation and growth modes in titania nanoparticles generation by a CVD method. J Chem Eng Jpn 2004, 37, 1379.

45.	Nakaso, K.; Okuyama, K.; Shimada, M.; Pratsinis, S. E., Effect of reaction temperature on CVD-made TiO2 primary particle diameter. Chemical Engineering Science 2003, 58, 3327.

46.	Sudarshan, T. S. In Coated  powders - new horizons and applications, Advances in Surface Treatment: Research & Applications (ASTRA), Proceedings of the International Conference, Hyderabad, India, 2003; Hyderabad, India, 2003; pp 412-422.

47.	Kim, C.; Nakaso, K.; Xia, B.; Okuyama, K.; Shimada, M., A new observation on the phase transformation of TiO2 nanoparticles produced by a CVD method. Aerosol Sci Tech 2005, 39, 104-112.

48.	Mueller, R.; Jossen, R.; Pratsinis, S. E.; Watson, M.; Akhtar, M. K., Zirconia nanoparticles made in spray flames at high production rates. J Am Ceram Soc 2004, 87, 197-202.

49.	Liang, C.; Shimizu, Y.; Sasaki, T.; Koshizaki, N., Synthesis, characterization, and phase stability of ultrafine TiO2 nanoparticles by pulsed laser ablation in liquid media. J Mater Res 2004, 19, 1551-1557.

50.	Kim, T. H.; Kang, J. P.; Kwon, Y. K., Synthesis and characterization of hollow  titania  nanospheres using a cationic colloidal particle as a template. Polymer Preprints 2005, 46, 566-567.

51.	Li, X.; Lau, K. H. A.; Kim, D. H.; Knoll, W., High-Density Arrays of Titania Nanoparticles Using Monolayer Micellar Films of Diblock Copolymers as Templates. Langmuir 2005, 21, 5212-5217.

52.	Iwasaki, M.; Davis, S. A.; Mann, S., Spongelike Macroporous TiO2 Monoliths Prepared from Starch Gel Template. J Sol-Gel Sci Techn 2004, 32, 99-105.

53.	Lim, K. T.; Hwang, H. S.; Ryoo, W.; Johnston, K. P., Synthesis of TiO2 Nanoparticles Utilizing Hydrated Reverse Micelles in CO2. Langmuir 2004, 20, 2466-2471.

54.	Pierre, A. C.; Pajonk, G. M., Chemistry of Aerogels and Their Application. Chem Rev 2002, 102, 4243-4265.

55.	Jessop, P.; Leitner, W., Chemical Synthesis Using Supercritical Fluids. Weinheim: Wiley-VCH: 1999.

56.	McHugh, M. A.; Krukonis, V. J., Supercritical Fluid Extraction: Principles and Practice. Second ed.; Butterworth-Heinemann: Boston, 1994.

57.	Sun, Y.-P., Supercritical fluid technology in materials science and engineering: syntheses, properties, and applications. Marcel Dekker: New York, 2002; p ix, 582 p.

58.	Massey, B. S.; Ward-Smith, A. J., Mechanics of fluids. 8th ed.; Taylor & Francis: London; New York, 2006; p x, 696 p.

59.	Fenghour, A.; Wakeham, W. A.; Vesovic, V., The Viscosity of Carbon Dioxide. Journal of Physical and Chemical Reference Data  1998, 27, 31-44.

60.	NIST Chemistry WebBook: Thermophysical Properties of Fluid Systems. In National Institute of Standards and Technology: 2007.

61.	White, H. E., Modern college physics. 4th ed.; Van Nostrand: Princeton, N. J., 1966; p 755 p.

62.	Hahne, E.; Grigull, U., Heat transfer in boiling. Academic Press: New York, 1977; p xiv, 486 p.

63.	Ye, X.; Wai, C. M., Making Nanomaterials in Supercritical Fluids: A Review. J. Chem. Ed. 2003, 80, 198-203.

64.	Tan, H. S.; Borsadia, S., Particle Formation Using Supercritical Fluids: Pharmaceutical Applicatons. Exp. Opin. Ther. Patents 2001, 11, 861-872.

65.	Krukonis, V. In Supercritical Fluid Nucleation of Difficult to Comminute Solids, AIChE annual meeting, San Francisco, November, 1984; San Francisco, 1984; p paper 140 f.

66.	Matson, D. W.; Norton, K. A.; R.D.Smith, Chemtech 1989, 19, 480.

67.	Petersen, R. C.; Matson, D. W.; Smith, R. D., Polym Eng Sci 1987, 27, 1693.

68.	Reverchon, E., Supercritical antisolvent precipitation of micro- and nanoparticles. J. of Supercrit. Fluids. 1999, 15, 1-21.

69.	DeSimone, J. M.; Maury, E. E.; Menceloglu, Y. Z.; McClain, J. B.; Romack, T. J.; Combes, J. R., Dispersion Polymerizations in Supercritical Carbon Dioxide. Science 1994, 265, 356-359.

70.	Shaffer, K. A.; DeSimone, J. M., Chain Polymerizations in Inert Near and Supercritical Fluids. Trends in Polymer Science 1995, 3, 146-153.

71.	Super, M.; Berluche, E.; Costello, C.; E., B., Copolymerization of 1,2-Epoxycyclohexane and Carbon Dioxide Using Carbon Dioxide as Both Reactant and Solvent. Macromolecules 1997, 30, 368-372.

72.	Quadir, M. A.; DeSimone, J. M.; van Herk, A. M.; German, A. L., Pulsed_Laser Polymerization of Methyl Methacrylate in Liquid and Supercritical Carbon Dioxide. Macromolecules 1998, 31, 6481-6485.

73.	Charpentier, P. A.; Kennedy, K.; DeSimone, J. M.; Roberts, G. W., Continuous Polymerizations in Supercritical Carbon Dioxide:Chain-Growth Precipitation Polymerizations. Macromolecules 1999, 32, 5973-5975.

74.	Musie, G.; Wei, M.; Subramaniam, B.; Busch, D. H., Catalytic oxidations in carbon dioxide-based reaction media, including novel CO2 -expanded phases. Coordination Chemistry Reviews 2001, 219-221, 789-820.

75.	Tacke, T.; Wieland, S.; Panster, P., Selective and complete hydrogenation of vegetable oils and free fatty acids in  supercritical  fluids. Green Chemistry Using Liquid and Supercritical Carbon Dioxide 2003, 228-240.

76.	Matsuda, T.; Watanabe, K.; Harada, T.; Nakamura, K., Enzymatic reactions in supercritical CO2: carboxylation, asymmetric reduction and esterification. Catalysis Today 2004, 96, 103.

77.	Loy, D. A.; Russick, E. M.; Yamanaka, S. A.; Baugher, B. M., Direct Formation of Aerogels by Sol-gel Polymerizations of Alkoxides in Supercritical Carbon Dioxide. Chem Mater 1997, 9, 2264-2268.

78.	Moner-Girona, M.; Roig, A.; Molins, E., Sol-gel Route to Direct Formation of Silica Aerogel Microparticles Using Supercritical Solvents. J Sol-Gel Sci Techn 2003, 26, 645-649.

79.	Aymonier, C.; Loppinet-Serani, A.; Reveron, H.; Garrabos, Y.; Cansell, F., Review of supercritical fluids in inorganic materials science. Journal of Supercritical Fluids 2006, 38, 242-251.

80.	van Eldik, R.; Asano, T.; LeNoble, W. J., Activation and Reaction Volumes in Solution. 2. Chem. Rev. 1989, 89, 549-688.

81.	Savage, P. E.; Gopalan, S.; Mizan, T. I.; Martino, C. J.; Brock, E. E., Reactions at Supercritical Conditions: Application and Fundamentals. AIChE J 1995, 41, 1723-1778.

82.	Ellington, J. B.; Park, K. M.; Brennecke, J. F., Effect of local composition enhancements on the esterification of phthalic anhydride with methanol in supercritical carbon dioxide. Ind. Eng. Chem. Res. 1994, 33, 965-974.

83.	Johnston, K. P.; Haynes, C., Extreme solvent effects on reaction rate constants at supercritical fluid conditions. AIChE J 1987, 33, 2017-2026.

84.	Peng, D.-Y.; Robinson, D. B., A new two-constant equation of state. Ind Eng Chem Fundam 1976, 15, 59-64.

85.	Johnston, K. P., Safer solutions for chemists. Nature 1994, 368, 187-188.

86.	Turner, C. H.; Gubbins, K. E., Effects of supercritical clustering and selective confinement on reaction equilibrium: A molecular simulation study of the esterification reaction. J Chem Phys 2003, 119, 6057-6067.

87.	Ellington, J. B.; Brennecke, J. F., Pressure effect on the esterification of phthalic anhydride in supercritical carbon dioxide. Chemical Communications 1993, 13, 1094-5.

88.	Karen, A. K.; George, W. R.; Joseph, M. D., Heterogeneous Polymerization of Fluoroolefins in Supercritical Carbon Dioxide. 2005; p 329.

89.	Woods, H. M.; Silva, M. M. C. G.; Nouvel, C.; Shakesheff, K. M.; Howdle, S. M., Material Processing in Supercritical Carbon Dioxide: Surfactants, Polymers and Biomaterials. J Mater Chem 2004, 14, 1663-1678.

90.	O'Neil, A.; Watkins, J. J., Green chemistry in the microelectronics industry. Green Chem 2004, 6, 363-368.

91.	King, J. W.; Williams, L. L., Utilization of critical fluids in processing semiconductors and their related materials. Curr Opin Solid ST M 2003, 7, 413-424.

92.	Charpentier, P. A.; DeSimone, J. M.; Roberts, G. W., Continuous polymerizations in supercritical carbon dioxide. ACS Symposium Series 2002, 819, 113-135.

93.	McHugh, M. A.; Krukonis, V. J., Supercritical Fluid Extraction:

Principles and Practice. Second ed.; Butterworth-Heinemann: Boston, 1994.

94.	Darr, J. A.; Poliakoff, M., New Directions in Inorganic and Metal-Organic Coordination Chemistry in Supercritical Fluids. Chem Rev 1999, 99, 495-541.

95.	Pierre, A. C.; Pajonk, G. M., Chemistry of Aerogels and Their Application. Chem. Rev. 2002, 102, 4243-4265.

96.	Yoda, S.; Otake, K.; Takebayashi, Y.; Sugeta, T.; Sato, T., Effect of Supercritical Impregnation Conditions on the Properties of Silica-Titania Aerogels. J Non-Cryst Solids 2001, 285, 8-12.

97.	Stallings, W. E.; Lamb, H. H., Synthesis of Nanostructured Titania Powders via Hydrolysis of Titanium Isopropoxide in Supercritical Carbon Dioxide. Langmuir 2003, 19, 2989-2994.

98.	Suh, D. J.; Park, T.-J., Synthesis of High-Surface-Area Zirconia Aerogels with a Well-Developed Mesoporous Texture Using CO2 Supercritical Drying. Chem. Mater. 2002, 14, 1452-1454.

99.	Pai, R. A.; Humayun, R.; Schulberg, M. T.; Sengupta, A.; Sun, J.-N.; Watkins, J. J., Mesoporous Silicates Prepared Using Preorganized Templates in Supercritical Fluids. Science 2004, 303, 507-510.

100.	Hanrahan, J. P.; Copley, M. P.; Ryan, K. M.; Spalding, T. R.; Morris, M. A.; Holmes, J. D., Pore Expansion in Mesoprous Silicas Using Supercritical Carbon Dioxide. Chem. Mater. 2004, 16, 424-427.

101.	Rathke, J. W.; Klingler, R. J.; Krause, T. R., Propylene hydroformylation in supercritical carbon dioxide. Organometallics 1991, 10, 1350-1355.

102.	Reid, C.; Prausnitz, J. M.; Poling, B. E., The properties of gases and liquids. McGraw-Hill: New York, 1985.

103.	Hench, L. L.; West, J. K., The sol-gel process. Chemical Reviews 1990, 90, 33-72.

104.	Brinker, C. J.; Scherer, G. W., Sol-Gel Science:The Physics and Chemistry of Sol-Gel Processing. Academic Press: New York, 1990.

105.	Brinker, C. J.; Scherer, G. W., Sol-Gel Science: The Physics and Chemistry of Sol-Gel Processing. Academic Press: New York, 1990.

106.	Cansell, F.; Aymonier, C.; Loppinet-Serani, A., Review on materials science and supercritical fluids. Current Opinion in Solid State and Materials Science 2003, 7, 331.

107.	Gesser, H. D.; Goswami, P. C., Aerogels and related porous materials. Chem. Rev. 1989, 89, 765-788.

108.	Ebelmen, Untersuchungen uber die Verbindung der Borsaure und Kieselsaure mit. Aether  Ann. Chim. Phys., 1846, Ser. 3, 319-55.

109.	Kistler, S. S., J. Phys. Chem. 1932, 36, 52-64.

110.	Lev, O.; Wu, Z.; Bharathi, S.; Glezer, V.; Modestov, A.; Gun, J.; Rabinovich, L.; Sampath, S., Sol-Gel Materials in Electrochemistry. Chem Mater 1997, 9, 2354-2375.

111.	Roy, R., Ceramics by the Solution-Sol-Gel Route. Science 1987, 238, 1664-1669.

112.	Schmidt, M.; Schwertfeger, F., Applications for silica aerogel products. J. Non-Cryst. Solids 1998, 225, 364-368.

113.	Gesser, H. D.; Goswami, P. C., Aerogels and related porous materials. Chem Rev 1989, 89, 765-788.

114.	Campbell, L. K.; Na, B. K.; Ko, E. I., Chem. Mater. 1992, 4, 1329-1333.

115.	Brinker, C. J.; Scherer, G. W., Sol-Gel Science. Academic Press, New York: 1990.

116.	Loy, D. A.; Russick, E. M.; Yamanaka, S. A.; Baugher, B. M., Direct Formation of Aerogels by Sol-gel Polymerizations of Alkoxides in Supercritical Carbon Dioxide. Chem. Mater. 1997, 9, 2264-2268.

117.	Chhor, K.; Bocquet, J. F.; Pommier, C., Syntheses of submicron TiO2 powders in vapor, liquid and supercritical phases, a comparative study. Materials Chemistry and Physics 1992, 32, 249.

118.	Courtecuisse, V. G.; Bocquet, J. F.; Chhor, K.; Pommier, C., Modeling of a continuous reactor for TiO2 powder synthesis in a supercritical fluid - experimental validation. The Journal of Supercritical Fluids  1996, 9, 222-226.

119.	Brasseur-Tilmant, J.; Chhor, K.; Jestin, P.; Pommier, C., Ceramic membrane elaboration using supercritical fluid. Materials Research Bulletin 1999, 34, 2013.

120.	Znaidi, L.; Chhor, K.; Pommier, C., Batch and semi-continuous synthesis of magnesium oxide powders from hydrolysis and supercritical treatment of Mg(OCH3)2. Materials Research Bulletin 1996, 31, 1527.

121.	Chhor, K.; Bocquet, J. F.; Pommier, C., Syntheses of submicron magnesium oxide powders. Materials Chemistry and Physics 1995, 40, 63.

122.	Bocquet, J. F.; Chhor, K.; Pommier, C., Barium titanate powders synthesis from solvothermal reaction and supercritical treatment. Materials Chemistry and Physics 1999, 57, 273.

123.	Hu, M. Z. C.; Harris, M. T.; Byers, C. H., Nucleation and Growth for Synthesis of Nanometric Zirconia Particles by Forced Hydrolysis. Journal of Colloid and Interface Science 1998, 198, 87.

124.	Zeng, J.; Zhang, M.; Song, Z.; Wang, L.; Li, J.; Li, K.; Lin, C., Lead-zirconate-titanate thin films deposited on silicon using a novel technique at low temperature. Applied Surface Science 1999, 148, 137.

125.	Zeng, J.; Lin, C.; Li, J.; Li, K., Preparation of highly oriented Pb(Zr0.52Ti0.48)O3 thin films by sol -gel -hydrothermal process. Journal of Materials Research 1999, 14, 2712-2715.

126.	Zeng, J.; Lin, C.; Song, Z.; Li, K.; Li, J., Sol-gel-hydrothermal growth of oxide thin films at low temperatures. Philosophical Magazine Letters 2000, 80, 119-124.

127.	Shen, J.; Zhang, Q.; Wang, J.; Yang, T.; Deng, Z.; Zhou, B.; Chen, L., Sol - gel  processing of zirconia coating for HR mirrors with high laser damage threshold. Journal of Sol-Gel Science and Technology   2000, 19, 271-274.

128.	Zhang, Q.; Shen, J.; Wang, J.; Wu, G.; Chen, L., Sol-gel derived ZrO2-SiO2 highly reflective coatings. International Journal of Inorganic Materials 2000, 2, 319.

129.	Zhao, J.; Fan, W.; Wu, D.; Sun, Y., Stable nanocrystalline zirconia  sols  prepared by a novel method: alcohol thermal synthesis. Journal of Materials Research 2000, 15, 402-406.

130.	Hayashi, H.; Torii, K., Hydrothermal synthesis of  titania  photocatalyst under subcritical and supercritical water conditions. J Mater Chem 2002, 12, 3671-3676.

131.	Yang, J.; Mei, S.; Ferreira, J. M. F., Hydrothermal synthesis of well-dispersed TiO2 nano -crystals. J Mater Res 2002, 17, 2197-2200.

132.	Parvulescu, V.; Parvulescu, V. I.; Alifanti, M.; Jung, S. M.; Grange, P., One pot synthesis of mesoporous ternary V2O5-TiO2-SiO2 catalysts. Studies in Surface Science and Catalysis 2003, 146.

133.	Tai, C. Y.; Hsiao, B.-Y.; Chiu, H.-Y., Preparation of spherical hydrous-zirconia  nanoparticles  by low temperature hydrolysis in a reverse microemulsion. Colloids and Surfaces, A: Physicochemical and Engineering Aspects 2004, 237, 105.

134.	Corradi, A. B.; Bondioli, F.; Focher, B.; Ferrari, A. M.; Grippo, C.; Mariani, E.; Villa, C., Conventional and Microwave-Hydrothermal Synthesis of TiO2 Nanopowders. Journal of the American Ceramic Society 2005, 88, 2639-2641.

135.	Kang, M.; Ko, Y.-R.; Jeon, M.-K.; Lee, S.-C.; Choung, S.-J.; Park, J.-Y.; Kim, S.; Choi, S.-H., Characterization of Bi/TiO2 nanometer sized particle synthesized by solvothermal method and CH3CHO decomposition in a plasma-photocatalytic system. J Photochem Photobiol, A 2005, 173, 128.

136.	Tadros, M. E. A., Carol L. J.; Russick, Edward M.; Youngman, Michael P., Synthesis of titanium dioxide particle in supercritical CO2. J Supercrit Fluids 1996, 9, 172-176.

137.	Hong, S.-S.; Lee, M. S.; Lee, G.-D.; Lim, K. T.; Ha, B.-J., Synthesis of titanium dioxides in water-in-carbon dioxide microemulsion and their photocatalytic activity. Mater Lett 2003, 57, 2975.

138.	Reverchon, E.; Caputo, G.; Correra, S.; Cesti, P., Synthesis of titanium hydroxide nanoparticles in supercritical carbon dioxide on the pilot scale. The Journal of Supercritical Fluids 2003, 26, 253.

139.	Yoda, S.; Sakurai, Y.; Endo, A.; Miyata, T.; Yanagishita, H.; Otake, K.; Tsuchiya, T., Synthesis of titania-pillared montmorillonite via intercalation of titanium alkoxide dissolved in supercritical carbon dioxide. J Mater Chem 2004, 14, 2763-2767.

140.	Sun, D.; Liu, Z.; He, J.; Han, B.; Zhang, J.; Huang, Y., Surface sol-gel modification of mesoporous silica molecular sieve SBA-15 with TiO2 in supercritical CO2. Microporous and Mesoporous Materials 2005, 80, 165.

141.	Yamashita, H.; Kawasaki, S.; Ichihashi, Y.; Harada, M.; Takeuchi, M.; Anpo, M.; Stewart, G.; Fox, M. A.; Louis, C.; Che, M., Characterization of Titanium-Silicon Binary Oxide Catalysts Prepared by the Sol-Gel Method and Their Photocatalytic Reactivity for the Liquid-Phase Oxidation of 1-Octanol. Journal of Physical Chemistry B 1998, 102, 5870-5875.

142.	Jensen, H.; Joensen, K. D.; Iversen, S. B.; Sogaard, E. G., Low Temperature Synthesis of Metal Oxides by a Supercritical Seed Enhanced Crystallization (SSEC) Process. Ind Eng Chem Res 2006, ASAP.

143.	Jensen, H.; Bremholm, M.; Nielsen, R. P.; Joensen, K. D.; S, P. J.; Birkedal, H.; Chen, Y.-S.; Almer, J.; Sogaard, E. G.; Iversen, S. B.; Iversen, B. B., In situ high-energy synchrotron radiation study of sol-gel nanoparticle formation in supercritical fluids. Angewandte Chemie, International Edition 2007, 46, 1113-1116.

144.	Cabanas, A.; Enciso, E.; Carbajo, M. C.; Torralvo, M. J.; Pando, C.; Renuncio, J. A. R., Synthesis of SiO2-Aerogel Inverse Opals in Supercritical Carbon Dioxide. Chem Mater 2005, 17, 6137-6145.

145.	Cabanas, A.; Enciso, E.; Carmen Carbajo, M.; Torralvo, M. J.; Pando, C.; Renuncio, J. A. R., Studies on the porosity of SiO2-aerogel inverse opals synthesised in supercritical CO2. Microporous and Mesoporous Materials 2007, 99, 23.

146.	Levit, N.; Tepper, G., Supercritical CO2-assisted electrospinning. J Supercrit Fluids 2004, 31, 329-333.

147.	Lazzaroni, M. J.; Bush, D.; Jones, R.; Hallett, J. P.; Liotta, C. L.; Eckert, C. A., High-pressure phase equilibria of some carbon dioxide-organic-water systems. Fluid Phase Equilibria 2004, 224, 143-154.

148.	Schneider, M. S.; Grunwaldt, J.-D.; Burgi, T.; Baiker, A., High pressure view-cell for simultaneous in situ infrared spectroscopy and phase behavior monitoring of multiphase chemical reactions. Rev Sci Instrum 2003, 74, 4121-4128.

149.	Feng, L.; Berglund, K. A., ATR FTIR for determination optimal cooling curves for batch crystallization of succinic acid. J. of Crystal Growth 2002, 2, 449-452.

150.	Lewiner, F.; F`evotte, G.; Klein, J. P.; Puel, F., Improving Batch Cooling Seeded Crystallization of an Organic Weed-Killer Using On-Line ATR FTIR Measurement of Supersaturation. J. of Crystal Growth 2001, 226, 348-362.

151.	Burns, D. A.; Ciurczak, E. W., Handbook of near-infrared analysis. 2nd ed.; Dekker: New York, 2001; p xv, 814 p.

152.	Newbury, D. E.; Williams, D. B., The electron microscope: the materials characterization tool of the millennium. Acta Materialia 2000, 48, 323-346.

153.	Van der Mast, K. D., Ultramicrosc 1996, 64, 1.

154.	Horiuchi, S., Fundamentals of high-resolution transmission electron microscopy. North-Holland: Amsterdam; New York, 1994; p xv, 342 p.

155.	Zaefferer, S., Investigation of the correlation between texture and microstructure on a submicrometer scale in the TEM. Adv Eng Mater 2003, 5, 745-752.

156.	Egerton, R. F.; Li, P.; Malac, M., Radiation damage in the TEM and SEM. Micron 2004, 35, 399-409.

157.	Zhang, H.; Banfield, J. F., Understanding Polymorphic Phase transformation Behavior during Growth of Nanocrystalline Aggregates: Insights from TiO2. J Phys Chem B 2000, 104, 3481-3487.

158.	MATTER, U. m. s. d., Unit Cell. In The University of Liverpool: 2000.

159.	Huang, J. Y.; Park, B. H.; Jan, D.; Pan, X. Q.; Zhu, Y. T.; Jia, Q. X., High-resolution Transmission Electron Microscopy Study of Defects and Interfaces in Epitaxial TiO2 Films on Sapphire and LaAlO3. Philos Mag A 2002, 82, 735-749.

160.	Mittemeijer, E. J.; Scardi, P., Diffraction analysis of the microstructure of materials. Springer: Berlin; New York, 2004; p xxv, 549 p.

161.	Brunauer, S.; Emmett, P. H.; Teller, E., Adsorption of Gases in Multimolecular Layers. J Am Chem Soc 1938, 60, 309-319.

162.	Rouquerol, J.; Avnir, D.; Fairbridge, C. W.; Evertt, D. H.; Haynes, J. H.; Pernicone, N.; Ramsay, J. D. F.; Sing, K. S. W.; Unger, K. K., Recommendations for the characterization of porous solids. Pure Appl Chem 1994, 66, 1739.

163.	Barrett, E. P.; Joyner, L. G.; Halenda, P. P., The Determination of Pore Volume and Area Distributions in Porous Substances. I. Computations from Nitrogen Isotherms. J Am Chem Soc 1951, 73, 373-380.

164.	Gregg, S. J.; Sing, K. S. W., Adsorption, surface area, and porosity. 2nd ed.; Academic Press: London; Toronto, 1982; p xi, 303 p.

165.	Liu, H.; Zhang, L.; Seaton, N. A., Sorption hysteresis as a probe of pore structure. Langmuir 1993, 9, 2576-2582.

166.	Salmas, C. E.; Androutsopoulos, G. P., Rigid Sphere Molecular Model Enables an Assessment of the Pore Curvature Effect upon Realistic Evaluations of Surface Areas of Mesoporous and Microporous Materials. Langmuir 2005, 21, 11146-11160.

167.	Libby, B.; Monson, P. A., Adsorption/Desorption Hysteresis in Inkbottle Pores: A Density Functional Theory and Monte Carlo Simulation Study. Langmuir 2004, 20, 4289-4294.

168.	Kikkinides, E. S.; Kainourgiakis, M. E.; Stubos, A. K., Origin of Hysteresis of Gas Adsorption in Disordered Porous Media: Lattice Gas Model versus Percolation Theory. Langmuir 2003, 19, 3338-3344.

169.	Lukens, W. W.; Schmidt-Winkel, P.; Zhao, D.; Feng, J.; Stucky, G. D., Evaluating Pore Sizes in Mesoporous Materials: A Simplified Standard Adsorption Method and a Simplified Broekhoff-de Boer Method. Langmuir 1999, 15, 5403-5409.

170.	Dean, J. A., Analytical Chemistry Handbook. Academic Press, New York: 1995.

171.	Sui, R.; Rizkalla, A. S.; Charpentier, P. A., Synthesis and Formation of Silica Aerogel Particles By a Novel Sol-Gel Route in Supercritical Carbon Dioxide. J Phys Chem B 2004, 108, 11886-11892.

172.	Ye, S., A New Electrocatalyst Consisting of a Molecularly Homogeneous Platinum-Aerogel Nanocomposite. Can. J. Chem. 1997, 75, 1666-1673.

173.	Hair, L. M.; al., e., Local, Nano- and Micro-Structures of Mixed Metal Oxide Aerogels for Catalyst Applications. J. Non-Cryst. Solids 1995, 186, 168-176.

174.	Hrubesh, L. W., Aerogel applications. J. Non-Cryst. Solids 1998, 225, 335-342.

175.	Kistler, S. S., Coherent Expanded Aerogels and Jellies. Nature 1931, 127, 741.

176.	Cooper, A. I., Polymer synthesis and processing using supercritical carbon dioxide. J. Mater. Chem. 2000, 10, 207-234.

177.	Loy, D. A.; Russick, E. M.; Yamanaka, S. A.; Baugher, B. M., Chem. Mater. 1997, 749.

178.	Moner-Girona, M.; Roig, A.; Molins, E.; Llibre, J., J. Sol-Gel Sci. 2003, 26, 645-649.

179.	Tohge, N.; Moore, G. S.; Mackenzie, J. D., Structural Developments During the Gel to Glass Transition. J Non-Cryst Solids 1984, 63, 95-103.

180.	Pouxviel, J. C.; Boilot, J. P.; Beloeil, J. C.; Lalleman, J. Y., NMR Study of the Sol/Gel Polymerization. J. Non-Cryst. Solids 1987, 89, 345-360.

181.	Odian, G., Principles of Polymerization. 3rd ed.; John Wiley & Sons, Inc.: New York, 1991.

182.	Ota, T.; Imaeda, M.; Takase, H.; Kobayashi, M.; Kinoshita, N.; Hirashita, T.; Miyazaki, H.; Hikichi, Y., Porous titania ceramic prepared by mimicking silicified wood. J am Ceram Soc 2000, 83, 1521-1523.

183.	Yoshida, K.; Tanagawa, M.; Atsuta, M., Effects of filler composition and surface treatment on the characteristics of opaque resin composites. J Biomed Mater Res 2001, 58, 525-530.

184.	Suzuki, H.; Taira, M.; Wakasa, K.; Yamaki, M., Refractive-index-adjustable fillers for visible-light-cured dental resin composites: preparation of TiO2-SiO2 glass powder by the sol-gel process. J Dent Res 1991, 70, 883-888.

185.	Taruta, S.; Itou, Y.; Tausagawa, N.; Okada, K.; Otsuka, N., Influence of aluminum titanate formation on sintering of bimodal size-distributed alumina powder mixtures. J am Ceram Soc 1997, 80, 551-556.

186.	Takaba, H.; Way, J. D., Separation of Isomeric Xylenes Using Cyclodextrin-Modified Ceramic Membranes. Ind. Eng. Chem. Res. 2003, 42, 5697-5701.

187.	Tani, K.; Suzuki, Y., Investigation of the ion-exchange behavior of titania. Application as a packing material for ion chromatography. Chromatographia 1997, 46, 623-627.

188.	Lin, H.-M.; Kao, S.-T.; Lin, K.-M.; Chang, J.-R.; Shyu, S.-G., Grafting TiO2 on MCM-41 as a TiO2 support for vanadia for catalytic oxidation of ethanol-EXAFS and XANES analyses of vanadium. J Catal 2004, 224, 156-163.

189.	Rainone, F.; Kiwi-Minsker, L.; Bulushev, D. A.; Buffat, P. A.; Renken, A., Structural and catalytic properties of vanadia-based fibrous catalysts in toluene partial oxidation. Appl Catal A-Gen 2003, 244, 251-263.

190.	Herrmann, J. M., Electronic effects in strong metal-support interactions on titania deposited metal catalysts. J Catal 1984, 89, 404-412.

191.	Anpo, M.; Takeuchi, M., The design and development of highly reactive titanium oxide photocatalysts operating under visible light irradiation. J Catal 2003, 216, 505-516.

192.	Martyanov, I. N.; Klabunde, K. J., Comparative study of TiO2 particles in powder form and as a thin nanostructured film on quartz. J Catal 2004, 225, 408-416.

193.	Lukaski, A. C.; Muggli, D. S., Photocatalytic oxidation of methyl formate on TiO2: a transient DRIFTS study. J Catal 2004, 223, 250-261.

194.	Tseng, I.-H.; Wu, J. C. S.; Chou, H.-Y., Effects of sol-gel procedures on the photocatalysis of Cu/TiO2 in CO2 photoreduction. J Catal 2004, 221, 432-440.

195.	Yeung, K. L.; Yau, S. T.; Maira, A. J.; Coronado, J. M.; Soria, J.; Yue, P. L., The influence of surface properties on the photocatalytic activity of nanostructured TiO2. J Catal 2003, 219, 107-116.

196.	Bach, U.; Lupo, D.; Comte, P.; Moser, J., E; Weissortel, F.; Salbeck, J.; Spreitzer, H.; Gratzel, M., Solid-State Dye-Sensitized Mesoporous TiO2 Solar Cells with High Photon-to-Electron Conversion Efficiencies. Nature 1998, 395, 583-585.

197.	Bando, K. K.; Mitsuzuka, Y.; Sugino, M.; Sugihara, H.; Sayama, K.; Arakawa, H., Attachment of an Organic dye on a TiO2 Substrate in Supercritical CO2: Application to a Solar Cell. Chemistry Letters 1999, 853-854.

198.	Schumacher, B.; Denkwitz, Y.; Plzak, V.; Kinne, M.; Behm, R. J., Kinetics, mechanism, and the influence of H2 on the CO oxidation reaction on a Au/TiO2 catalyst. J Catal 2004, 224, 449-462.

199.	Nelson, B. P.; Candal, R.; Corn, R. M.; Anderson, M. A., Control of Surface and z Potentials on Nanoporous TiO2 Films by Potential-Determining and Specifically Adsorbed Ions. Langmuir 2000, 16, 6094-6101.

200.	Sakai, N.; Ebina, Y.; Takada, K.; Sasaki, T., Electronic Band Structure of Titania Semiconductor Nanosheets Revealed by Electrochemical and Photoelectrochemical Studies. J Am Chem Soc 2004, 126, 5851-5858.

201.	Navio, J.; Colon, G.; Macias, M.; Real, C.; Litter, M. I., Iron-doped titania semiconductor powders prepared by a sol-gel method. Part I. Synthesis and characterization. Appl Catal A-Gen 1999, 177, 111-120.

202.	Yoko, T.; Yuasa, A.; Kamiya, K.; Sakka, S., Sol-gel-derived titanium dioxide film semiconductor electrode for photocleavage of water.  Preparation and effects of postheating treatment on the photoelectrochemical behavior. J Electrochem Soc 1991, 138, 2279-2285.

203.	Fujishima, A.; Honda, K., Electrochemical photolysis of water at a semiconductor electrode. Nature 1972, 238, 37-8.

204.	Elder, S. H.; Cot, F. M.; Su, Y.; Heald, S. M.; Tyryshkin, A. M.; Bowman, M. K.; Gao, Y.; Joly, A. G.; Balmer, M. L.; Kolwaite, A. C.; Magrini, K. A.; Blake, D. M., The Discovery and Study of Nanocrystalline TiO2-(MoO3) Core-Shell Materials. J Am Chem Soc 2000, 122, 5138-5146.

205.	Choi, W.; Termin, A.; Hoffmann, M. R., The Role of Metal Ion Dopants in Quantum-Sized TiO2: Correlation between Photoreactivity and Charge Carrier Recombination Dynamics. J Phys Chem 1994, 98, 13669-13679.

206.	Asahi, R.; Morikawa, T.; Ohwaki, T.; Aoki, K.; Taga, Y., Visible-Light Photocatalysis in Nitrogen-Doped Titanium Oxide. Science 2001, 293, 269-271.

207.	Jung, H. S.; Lee, J. K.; Nastasi, M.; Lee, S. W.; Kim, J. Y.; Park, J. S.; Hong, K. S.; Shin, H., Preparation of Nanoporous MgO-Coated TiO2 Nanoparticles and Their Application to the Electrode of Dye-Sensitized Solar Cells. Langmuir 2005, 21, 10332-10335.

208.	Lee, S.; Jeon, C.; Park, Y., Fabrication of TiO2 Tubules by Template Synthesis and Hydrolysis with Water Vapor. Chem Mater 2004, 16, 4292-4295.

209.	Bosc, F.; Ayral, A.; Albouy, P. A.; Guizard, C., A Simple Route for Low-Temperature Synthesis of Mesoporous and Nanocrystalline Anatase Thin Films. Chem Mater 2003, 15, 2463-2468.

210.	Joo, J.; Kwon, S. G.; Yu, T.; Cho, M.; Lee, J.; Yoon, J.; Hyeon, T., Large-Scale Synthesis of TiO2 Nanorods via Nonhydrolytic Sol-Gel Ester Elimination Reaction and Their Application to Photocatalytic Inactivation of E. coli. J Phys Chem B 2005, 109, 15297-15302.

211.	Li, G.; Li, L.; Boerio-Goates, J.; Woodfield, B. F., High Purity Anatase TiO2 Nanocrystals: Near Room-Temperature Synthesis, Grain Growth Kinetics, and Surface Hydration Chemistry. J Am Chem Soc 2005, 127, 8659-8666.

212.	Baerns, M., Basic Principles in Applied Catalysis. Springer: New York, 2004.

213.	Yang, P.; Zhao, D.; Margolese, D. I.; Chmelka, B. F.; Stucky, G. D., Generalized Syntheses of Large-pore mesoporous Metal Oxides with Semicrystalline Frameworks. Nature 1998, 396, 152-155.

214.	Imhof, A.; Pine, D. J., Ordered Macroporous Materials by Emulsion Templating. Nature 1997, 389, 948-951.

215.	Li, D.; Zhou, H.; Honma, I., Design and Synthesis of Self-ordered Mesoporous Nanocomposite through Controlled in-situ Crystallization. Nature Materials 2004, 3, 65-72.

216.	Yun, H.-S.; Miyazawa, K.; Zhou, H.; Honma, I.; Kuwabara, M., Synthesis of Mesoporous Thin TiO2 Films with Hexagonal Pore Structures Using Triblock Copolymer Templates. Adv Mater 2001, 13, 1377-1380.

217.	Liu, C.; Fu, L.; Economy, J., A Simple, Template-Free Route for the Synthesis of Mesoporous Titanium Dioxide Materials. J Mater Chem 2004, 14, 11887-1187.

218.	Madhugiri, S.; Sun, B.; Smirniotis, P. G.; Ferraris, J. P.; Balkus Jr., K. J., Electrospun Mesoporous Titanium Dioxide Fibers. Microporous and Mesoporous Materials 2004, 69, 77-83.

219.	Bansal, V.; Rautaray, D.; Ahmad, A.; Sastry, M., Biosynthesis of zirconia nanoparticles using the fungus Fusarium oxysporum. J Mater Chem 2004, 14, 3303-3305.

220.	Flood, R. U.; Fitzmaurice, D., Preparation, Characterization, and Potential-Dependent Optical Adsorption Spectroscopy of Unsupported Large-Area Transparent Nanocrystalline TiO2 Membranes. J Phys Chem 1995, 99, 8954-8958.

221.	Yao, B.; Zhang, L., Preparation and characterization of mesoporous titania gel-monolith. J Mater Chem 1999, 34, 5983-5987.

222.	Krstic, V. D., Fracture of brittle solids in the presence of thermoelastic stresses. J Am Ceram Soc 1984, 67, 589-593.

223.	Hosono, H.; Sakai, Y.; Fasano, M.; Abe, Y., Preparation of monolithic porous titania-silica ceramics. J am Ceram Soc 1990, 73, 2536-2538.

224.	Maurer, S. M.; Ng, D.; Ko, E. I., Catal Today 1993, 16, 319.

225.	Suh, D. J.; Park, T.-J., Effect of aging conditions on the pore structural properties of titania aerogels. J Mater Sci Lett 1997, 16, 490.

226.	Campbell, L. K.; Na, B. K.; Ko, E. I., Synthesis and Characterization of Titania Aerogels. Chem Mater 1992, 4, 1329-1333.

227.	Boyle, T. J.; Tyner, R. P.; Alam, T. M.; Scott, B. L.; Ziller, J. W.; Potter, B. G., Jr., Implications for the Thin-Film Densification of TiO2 from Carboxylic Acid-Modified Titanium Alkoxides. Syntheses, Characterizations, X-ray Structures of Ti3(3-O)(O2CH)2(ONep)8, Ti3(3-O)(O2CMe)2(ONep)8, Ti6(3-O)6(O2CCHMe2)6(ONep)6, [Ti(-O2CCMe3)(ONep)3]2, and Ti3(3-O)(O2CCH2CMe3)2(ONep)8 (ONep = OCH2CMe3)1. J Am Chem Soc 1999, 121, 12104-12112.

228.	Perrin, F. X.; Nguyen, V.; Vernet, J. L., FT-IR Spectroscopy of Acid-Modified Titanium Alkoxides: Investigations on the Nature of Carboxylate Coordination and Degree of Complexation. J Sol-Gel Sci Techn 2003, 28, 205-215.

229.	Nakamoto, K., Infrared and Raman Spectra of Inorganic and Coordination Compounds. A Wiley-Interscience Publication: New York, 1997; Vol. Part B, p 59-62.

230.	Deacon, G. B.; Phillips, R. J., Relationships between the carbon-oxygen stretching frequencies of carboxylato complexes and the type of carboxylate coordination. Coord Chem Rev 1980, 33, 227-50.

231.	Rammal, A.; Brisach, F.; Henry, M., Hydrothermal synthesis of TiO2 anatase nanocrystals using hexaprismatic-shaped oxo-carboxylate complexes. Comptes Rendus Chimie 2002, 5, 59-66.

232.	Doeuff, S.; Dromzee, Y.; Taulelle, F.; Sanchez, C., Synthesis and solid- and liquid-state characterization of a hexameric cluster of titanium(IV): Ti6(m2-O)2(m3-O)2(m2-OC4H9)2(OC4H9)6(OCOCH3)8. Inorg Chem 1989, 28, 4439-45.

233.	Papiernik, R.; Hubert-Pfalzgraf, L. G.; Vaissermann, J.; Goncalves, M. C. H. B., Synthesis and characterization of new titanium hexanuclear oxo carboxylato alkoxides. Molecular structure of [Ti6(m3-O)6(m-O2CC6H4OPh)6(OEt)6]. J Chem Soc, Dalton Trans 1998, 14, 2285-2288.

234.	Sui, R.; Charpentier, P. A.; Rizkalla, A. S.; Jennings, M. C., Hexakis(m -acetato-k 2O,O')hexaisopropoxyhexa-m 3-oxo-hexatitanium. Acta Crystallogr 2006, E62, m373-m375.

235.	Wu, P.-G.; Ma, C.-H.; Shang, J. K., Effects of nitrogen doping on optical properties of TiO2 thin films. Appl Phys A 2005, 81, 1411-1417.

236.	Zhang, H.; Banfield, J. F., J. Mater Chem 1998, 8, 2073-2076.

237.	Zhang, H.; Banfield, J. F., Thermodynamic Analysis of Phase Stability of Nanocrystalline Titania. J Mater Chem 1998, 8, 2073-2076.

238.	Doeuff, S.; Henry, C.; Sanchez, C.; Livage, J., Hydrolysis of titanium alkoxides: modification of the molecular precursor by acetic acid. J Non-Cryst Solids 1987, 8, 206-216.

239.	Fink, R.; Hancu, D.; Valentine, R.; Beckman, E. J., Toward the Development of “CO2-philic” Hydrocarbons. 1. Used of side-Chain Functionalization to Lower the Miscibility Pressure of Polydimethylsiloxanes in CO2. J. Phys. Chem. B 1999, 103, 6441-6444.

240.	Raveendran, P.; Wallen, S. L., Sugar Acetates as Novel, Renewable CO2-philes. J. Am. Chem. Soc., 2002, 124, 7274-7275.

241.	Mu, T.; Han, B.; Zhang, J.; Li, Z.; Liu, Z.; Du, J.; Liu, D., Hydrogen bonding of acetic acid in CO2 + n-pentane mixed fluids in the critical region. J Supercrit Fluids 2004, 30, 17-24.

242.	Yamamoto, M.; Iwai, Y.; Nakajima, T.; Arai, Y., Fourier Transform Infrared Study on Hydrogen Bonding Species of Carboxylic Acids in Supercritical Carbon Dioxide with Ethanol. J Phys Chem A 1999, 103, 3525-3529.

243.	Liu, J.; Shi, J.; He, D.; Zhang, Q.; Wu, X.; Liang, Y.; Zhu, Q., Surface Active Structure of Ultra-fine Cu/ZrO2 Catalysts Used for the CO2+H2 to Methanol Reaction. Appl Catal A-Gen 2001, 218, 113-119.

244.	Koppel, R. A.; Stocker, C.; Baiker, A., Copper- and silver-zirconia aerogels: preparation, structural properties and catalytic behavior in methanol synthesis from carbon dioxide. J Catal 1998, 179, 515-527.

245.	Kalies, H.; Pinto, N.; Pajonk, G. M.; Bianchi, D., Hydrogenation of Formate Species Formed by CO Chemisorption on a Zirconia Aerogel in the Presence of Platinum. Appl Catal A-Gen 2000, 202, 197-205.

246.	Bahamonde, A.; Mohino, F.; Rebollar, M.; Yates, M. A., P.; Mendioroz, S., Pillared clay and zirconia-based monolithic catalysts for selective catalytic reduction of nitric oxide by methane. Catal Today 2001, 69, 233-239.

247.	Pacheco, G.; Zhao, E.; Garcia, A.; Sklyarov, A.; Fripiat, J. J., Synthesis of Mesoporous Zirconia with Anionic Surfactants. J. Mater. Chem. 1998, 8, 219-226.

248.	Crepaldi, E. L.; de A.A. Soler-Illia, G. J.; Grosso, D.; Albouy, P.-A.; Sanchez, C., Design and Post-functionalisation of Ordered Mesoporous Zirconia Thin Films. Chem. Commun. 2001, 1582-1583.

249.	Suh, D. J.; Park, T.-J., Synthesis of High-Surface-Area Zirconia Aerogels with a Well-Developed Mesoporous Texture Using CO2 Supercritical Drying. Chem Mater 2002, 14, 1452-1454.

250.	Somiya, S.; Yamamoto, N.; H. Yanagina, Science and Technology of Zirconia III. American Ceramic Society: Westerville, OH, 1988; Vol. 24A and 24B.

251.	Li, G.; Li, W.; Zhang, M.; Tao, K., Characterization and catalytic application of homogeneous nano-composite oxides ZrO2-Al2O3. Catal Today 2004, 93-95, 595-601.

252.	Kong, Y.-M.; Bae, C.-J.; Lee, S.-H.; Kim, H.-W.; Kim, H.-E., Improvement in biocompatibility of ZrO2-Al2O3 nano-composite by addition of HA. Biomaterials 2005, 26, 509-517.

253.	Badwal, S. P. S.; Ciacchi, F. T.; Giampietro, K. M., Analysis of the conductivity of commercial easy sintering grade 3 mol% Y2O3-ZrO2 materials. Solid State Ionics 2005, 176, 169.

254.	Shukla, S.; Seal, S.; Vanfleet, R., Sol-Gel Synthesis and Phase Evolution Behavior of Sterically Stabilized Nanocrystalline Zirconia. J Sol-Gel Sci Techn 2003, 27, 119-136.

255.	Willert, M.; Rothe, R.; Landfester, K.; Antonietti, M., Synthesis of Inorganic and Metallic Nanoparticles by Miniemulsification of Molten Salts and Metals. Chem Mater 2001, 13, 4681-4685.

256.	Limaye, A. U.; Helble, J. J., Morphological control of zirconia nanoparticles through combustion aerosol synthesis. J Am Ceram Soc 2002, 85, 1127-1132.

257.	Mondal, A.; Ram, S., Monolithic t-ZrO2 nanopowder through a ZrO(OH)2×xH2O polymer precursor. J Am Ceram Soc 2004, 87, 2187-2194.

258.	TORAYA, H., Whole-powder-pattern fitting without reference to a structural model: application to X-ray powder diffraction data. J Appl Cryst 1986, 19, 440-447.

259.	Rojas-Cervantes, M. L.; -Aranda, R. M. M.; -Peinado, A. J. L.; -Gonzalez, J. D. D. L., ZrO2 obtained by the sol-gel method: influence of synthesis parameters on physical and structural characteristics. Journal of Materials Science 1994, V29, 3743.

260.	Ward, D. A.; Ko, E. I., Synthesis and Structural Transformation of Zirconia Aerogels. Chem Mater 1993, 5, 956-969.

261.	Gregg, S. J.; Sing, K. S. W., Adsorption, Surface Area and Porosity. Academic Press: 1982.

262.	Phalippou, J.; Woignier, T.; Zarzycki, J., In Ultrastructure processing of ceramics, glasses, and composites, Hench, L. L.; Ulrich, D. R., Eds. Wiley: New York, 1984; pp 70-87.

263.	Weibel, A.; Bouchet, R.; Boulc'h, F.; Knauth, P., The Big Problem of Small Particles: A Comparison of Methods for Determination of Particle Size in Nanocrystalline Anatase Powders. Chem Mater 2005, 7, 2378-2385.

264.	Nakamoto, K., Infrared and Raman Spectra of Inorganic and Coordination Compounds. A Wiley-Interscience Publication: New York, 1997.

265.	Conley, R. T., Infrared spectroscopy. Allyn and Bacon: Boston, 1966; p ix, 293 p.

266.	Yi, G.; Sayer, M., An acetic acid/water based sol-gel PZT process. II: Formation of a water based solution. J Sol-Gel Sci Techn 1996, 6, 75-82.

267.	Sharp, K. G., A two-component, non-aqueous route to silica gel. J Sol-Gel Sci Techn 1994, 2, 35-41.

268.	Kickelbick, G.; Holzinger, D.; Brick, C.; Trimmel, G.; Moons, E., Hybrid Inorganic-Organic Core-Shell Nanoparticles from Surface-Functionalized Titanium, Zirconium, and Vanadium Oxo Clusters. Chem Mater 2002, 14, 4382-4389.

269.	Kickelbick, G.; Schubert, U., Oxozirconium methacrylate clusters. Zr6(OH)4O4(OMc)12 and Zr4O2(OMc)12 (OMc = methacrylate). Chem Ber/Recl 1997, 130, 473-477.

270.	Kickelbick, G.; Wiede, P.; Schubert, U., Variations in capping the Zr6O4(OH)4 cluster core: X-ray structure analyses of [Zr6(OH)4O4(OOC-CH=CH2)10]2([mu]-OOC-CH=CH2)4 and Zr6(OH)4O4(OOCR)12(PrOH) (R = Ph, CMe = CH2). Inorganica Chimica Acta 1999, 284, 1.

271.	Brown, S. D.; Sum, S. T.; Despagne, F.; Lavine, B. K., Chemometrics. Anal Chem 1996, 68, 21-62.

272.	Windig, W.; Guilment, J., Interactive self-modeling mixture analysis. Analytical Chemistry  1991, 63, 1425-32.

273.	Jung, Y. M.; Noda, I., New approaches to generalized two-dimensional correlation spectroscopy and its applications. Applied Spectroscopy Reviews  2006, 41, 515-547.

274.	Jiang, J.-H.; Liang, Y.; Ozaki, Y., Principles and methodologies in self-modeling curve resolution. Chemometrics and Intelligent Laboratory Systems  2004, 71, 1-12.

275.	Wallace, R. M., Analysis of Absorption Spectra of Multicomponent Systems. J Phys Chem 1960, 64, 899-901.

276.	Windig, W.; Stephenson, D. A., Self-modeling mixture analysis of second-derivative near-infrared spectral data using the SIMPLISMA approach. Analytical Chemistry  1992, 64, 2735-42.

277.	Sasic, S.; Amari, T.; Siesler, H. W.; Ozaki, Y., Polycondensation Reaction of Bis(hydroxyethylterephthalate)Self Modeling Curve Resolution Analysis of On-Line ATR/FT-IR Spectra. Applied Spectroscopy 2001, 55, 1181.

278.	Du, Y.; Jiang, J.; Liang, Y.; Amari, T.; Ozaki, Y., Chemometric resolution of ATR-IR spectra data for polycondensation reaction of bis(hydroxyethyl terephthalate) with a combination of self-modeling curve resolution (SMCR) and local rank analysis. Analyst 2003, 128, 1320-1325.

279.	Tummers, P. H. G.; Houben, E. J. E.; Jansen, J. F. G. A.; Wienke, D., Evaluation of advanced data analysis techniques on time resolved FT-IR spectroscopy data of photo-copolymerization reactions. Vibrational Spectroscopy 2007, 43, 116-124.

280.	Dupuy, N.; Batonneau, Y., Reliability of the contribution profiles obtained through the SIMPLISMA approach and used as reference in a calibration process: Application to Raman micro-analysis of dust particles. Analytica Chimica Acta 2003, 495, 205.

281.	Batonneau, Y.; Bremard, C.; Laureyns, J.; Merlin, J. C.; Windig, W., Polarization Effects of Confocal Raman Microspectrometry of Crystal Powders Using Interactive Self-Modeling Analysis. J Phys Chem B 2003, 107, 1502-1513.

282.	Chew, W.; Widjaja, E.; Garland, M., Band-Target Entropy Minimization (BTEM): An Advanced Method for Recovering Unknown Pure Component Spectra. Application to the FTIR Spectra of Unstable Organometallic Mixtures. Organometallics 2002, 21, 1982-1990.

283.	Windig, W.; Antalek, B.; Lippert, J. L.; Batonneau, Y.; Bremard, C., Combined Use of Conventional and Second-Derivative Data in the SIMPLISMA Self-Modeling Mixture Analysis Approach. Anal Chem 2002, 74, 1371-1379.

284.	Rauch, P. J.; Harrington, P. d.; Davis, D. M., Chemometric Resolution of Mixture Components by Cleardown Rates. Anal Chem 1998, 70, 716-723.

285.	Wasim, M.; Hassan, M. S.; Brereton, R. G., Evaluation of  chemometric  methods for determining the number and position of components in high-performance liquid chromatography detected by diode array detector and on-flow 1H nuclear magnetic resonance spectroscopy. Analyst   2003, 128, 1082-1090.

286.	Bu, D.; Brown, C. W., Self-Modeling Mixture Analysis by Interactive Principal Component Analysis. Applied Spectroscopy 2000, 54, 1214.

287.	O'Haver, T. C.; Green, G. L., Numerical error analysis of derivative spectrometry for the quantitative analysis of mixtures. Anal Chem 1976, 48, 312-318.

288.	Guan, Z.; Combes, J. R.; Menceloglu, Y. Z.; DeSimone, J. M., Homogeneous Free Radical Polymerizations in Supercritical Carbon Dioxide: 2. Thermal Decomposition of 2,2'-Azobis(isobutyronitrile). Macromolecules 1993, 26, 2663-2669.

289.	Kazarian, S. G.; Vincent, M. F.; Bright, F. V.; Liotta, C. L.; Eckert, C. A., Specific Intermolecular Interaction of Carbon Dioxide with Polymers. J Am Chem Soc 1996, 118, 1729-1736.

290.	Raveendran, P.; Wallen, S. L., Cooperative C-H---O Hydrogen Bonding in CO2-Lewis Base Complexes: Implications for Solvation in Supercritical CO2. J Am Chem Soc 2002, 124, 12590-12599.

291.	Yukihide, S.; Daisuke, A.; Naoki, T., pH-dependent color change of colloidal dispersions of gold nanoclusters: Effect of stabilizer. The European Physical Journal E - Soft Matter 2002, V8, 377.

292.	Sanchez, C.; Livage, J.; Henry, M.; Babonneau, F., Chemical modification of alkoxide precursors. J Non-Cryst Solids 1988, 100, 65-76.

293.	Xu, J.; Yan, J.; Wang, X.; Yu, H.; Milliken, T., Photochemical Reaction of Chrysene in Acetonitrile/Water. Polycyclic Aromatic Compounds 2004, 24, 249 - 256.

294.	Meredith, J. C.; Johnston, K. P.; Seminario, J. M.; Kazarian, S. G.; Eckert, C. A., Quantitative Equilibrium Constants between CO2 and Lewis Bases from FTIR Spectroscopy. J Phys Chem 1996, 100, 10837-10848.

295.	Blatchford, M. A.; Raveendran, P.; Wallen, S. L., Spectroscopic Studies of Model Carbonyl Compounds in CO2: Evidence for Cooperative C-H---O Interactions. J Phys Chem A 2003, 107, 10311-10323.

296.	Nelson, M. R.; Borkman, R. F., Ab Initio Calculations on CO2 Binding to Carbonyl Groups. J Phys Chem A 1998, 102, 7860-7863.

297.	Meredith, J. C.; Johnston, K. P.; Seminario, J. M.; Kazarian, S. G.; Eckert, C. A., Quantitative Equilibrium Constants between CO2 and Lewis Bases from FTIR Spectroscopy. J. Phys. Chem. 1996, 100, 10837-10848.

298.	Dobrowolski, J. C.; Jamroz, M. H., Infrared evidence for carbon dioxide electron donor-acceptor complexes. Journal of Molecular Structure  1992.

299.	Krevelen, D. W. v., Properties of polymers: their correlation with chemical structure, their numerical estimation and prediction from additive group contributions. 3rd, completely rev. ed.; Elsevier: Amsterdam; New York, 1990; p xxii, 875 p.

300.	Williams, L. L.; Rubin, J. B.; Edwards, H. W., Calculation of Hansen Solubility Parameter Values for a Range of Pressure and Temperature Conditions, Including the Supercritical Fluid Region. Ind Eng Chem Res 2004, 43, 4967-4972.

301.	Lagalante, A. F.; Hansen, B. N.; Bruno, T. J.; Sievers, R. E., Solubilities of Copper(II) and Chromium(III).beta.-Diketonates in Supercritical Carbon Dioxide. Inorg Chem 1995, 34, 5781-5785.

302.	Yazdi, A. V.; Beckman, E. J., Design, Synthesis, and Evaluation of Novel, Highly CO2-Soluble Chelating Agents for Removal of Metals. Ind Eng Chem Res 1996, 35, 3644-3652.

303.	Allada, S. R., Solubility Parameters of Supercritical Fluids. Ind Eng Chem Process Des Dev 1984, 23, 344-348.

304.	Guigard, S. E.; Stiver, W. H., A Density-Dependent Solute Solubility Parameter for Correlating Solubilities in Supercritical Fluids. Ind Eng Chem Res 1998, 37, 3786-3792.

305.	Fedors, R. F., Method for estimating both the solubility parameters and molar volumes of liquids. Polymer Engineering and Science 1974, 14, 147-54.

306.	Wade, L. G., Organic chemistry. 6th ed.; Pearson Prentice Hall: Upper Saddle River, N.J., 2006; p xli, 1262, 7, 1, 14 p.

307.	Elmali, A.; Zeyrek, C. T.; Elerman, Y., Crystal structure, magnetic properties and molecular orbital calculations of a binuclear copper(II) complex bridged by an alkoxo-oxygen atom and an acetate ion. Journal of Molecular Structure 2004, 693, 225.

308.	Delfs, C. D.; Stranger, R., Oxidation State Dependence of the Geometry, Electronic Structure, and Magnetic Coupling in Mixed Oxo- and Carboxylato-Bridged Manganese Dimers. Inorg Chem 2001, 40, 3061-3076.

309.	Hay, P. J.; Thibeault, J. C.; Hoffmann, R., Orbital  interactions in metal dimer complexes. Journal of the American Chemical Society 1975, 97, 4884-99.

310.	Norman Jr., J. G.; Kolari, H. J.; Gray, H. B.; Trogler, W. C., Electronic structure of dimolybdenum tetraformate, dimolybdenum(4+) ion, and dimolybdenum. Inorg Chem 1997, 16, 987-993.

311.	Acho, J. A.; Ren, T.; Yun, J. W.; Lippard, S. J., Dimolybdenum(II) Calixarene Complexes: Synthesis, Structure, Raman Spectroscopy, and Bonding. Inorganic Chemistry 1995, 34, 5226-33.

312.	Giddings, J. C.; Myers, M. N.; McLaren, L.; Keller, R. A., High pressure gas chromatography of nonvolatile species. Compressed gas is used to cause migration of intractable solutes. Science 1968, 162, 67-73.

313.	Fried, J. R., Polymer science and technology. 2nd ed.; Prentice Hall Professional Technical Reference: Upper Saddle River, NJ, 2003; p xvii, 582 p.

314.	Bradley, D. C., Alkoxo and aryloxo derivatives of metals. Academic Press: San Diego, 2001; p ix, 704 p.

315.	Bradley, D. C.; Mehrotra, R. C.; Gaur, D. P., Metal alkoxides. Academic Press: London; New York, 1978; p viii, 411 p.

316.	Galia, A.; Argentino, A.; Scialdone, O.; Filardo, G., A new simple static method for the determination of solubilities of condensed compounds in supercritical fluids. The Journal of Supercritical Fluids 2002, 24, 7.

317.	Agrawal, A.; Saran, A. D.; Rath, S. S.; Khanna, A., Constrained nonlinear optimization for solubility parameters of poly(lactic acid) and poly(glycolic acid)-validation and comparison. Polymer 2004, 45, 8603-8612.

318.	Martini, L. G.; Avontuur, P.; George, A.; Willson, R. J.; Crowley, P. J., Solubility parameter and oral absorption. European Journal of Pharmaceutics and Biopharmaceutics  1999, 48, 259-263.

319.	Fedors, R. F., Method for estimating both the solubility parameters and molar volumes of liquids.  Addendum.    Polymer Engineering and Science. Polymer Engineering and Science  1974, 14, 472.

320.	Sui, R.; Rizkalla, A. S.; Charpentier, P. A., FTIR Study on the Formation of TiO2 Nanostructures in Supercritical CO2. J Phys Chem B 2006, 110, 16212-16218.

321.	Barton, A. F. M., CRC handbook of solubility parameters and other cohesion parameters. CRC Press: Boca Raton, Fla., 1983; p 594 p.

322.	Gordon, L. J.; Scott, R. L., Enhanced Solubility in Solvent Mixtures. I. The System Phenanthrene-Cyclohexane-Methylene Iodide. J Am Chem Soc 1952, 74, 4138-4140.

323.	Yazdi, A. V.; Beckman, E. J., Design of Highly CO2-Soluble Chelating Agents. 2. Effect of Chelate Structure and Process Parameters on Extraction Efficiency. Ind Eng Chem Res 1997, 36, 2368-2374.

324.	Johnston, K. P.; Shah, P. S., Making Nanoscale Materials with Supercritical Fluids. Science 2004, 303, 482-483.

Appendices

Appendix 1. American Chemical Society’s Policy on Theses and Dissertations

If your university requires a signed copy of this letter see contact information below:

Thank you for your request for permission to include your paper(s) or portions of text from your paper(s) in your thesis. Permission is now automatically granted; please pay special attention to the implications paragraph below. The Copyright Subcommittee of the Joint Board/Council Committees on Publications approved the following:

Copyright permission for published and submitted material from theses and dissertations

ACS extends blanket permission to students to include in their theses and dissertations their own articles, or portions thereof, that have been published in ACS journals or submitted to ACS journals for publication, provided that the ACS copyright credit line is noted on the appropriate page(s).

Publishing implications of electronic publication of theses and dissertation material:

Students and their mentors should be aware that posting of theses and dissertation material on the Web prior to submission of material from that thesis or dissertation to an ACS journal may affect publication in that journal. Whether Web posting is considered prior publication may be evaluated on a case-by-case basis by the journal’s editor. If an ACS journal editor considers Web posting to be “prior publication”, the paper will not be accepted for publication in that journal. If you intend to submit your unpublished paper to ACS for publication, check with the appropriate editor prior to posting your manuscript electronically.

If your paper has not yet been published by ACS, we have no objection to your including the text or portions of the text in your thesis/dissertation in print and microfilm formats; please note, however, that electronic distribution or Web posting of the unpublished paper as part of your thesis in electronic formats might jeopardize publication of your paper by ACS. Please print the following credit line on the first page of your article: "Reproduced (or 'Reproduced in part') with permission from [JOURNAL NAME], in press (or 'submitted for publication'). Unpublished work copyright [CURRENT YEAR] American Chemical Society." Include appropriate information.

If your paper has already been published by ACS and you want to include the text or portions of the text in your thesis/dissertation in print or microfilm formats, please print the ACS copyright credit line on the first page of your article: “Reproduced (or 'Reproduced in part') with permission from [FULL REFERENCE CITATION.] Copyright [YEAR] American Chemical Society." Include appropriate information.

Submission to a Dissertation Distributor: If you plan to submit your thesis to UMI or to another dissertation distributor, you should not include the unpublished ACS paper in your thesis if the thesis will be disseminated electronically, until ACS has published your paper. After publication of the paper by ACS, you may release the entire thesis (not the individual ACS article by itself) for electronic dissemination through the distributor; ACS’s copyright credit line should be printed on the first page of the ACS paper.

Use on an Intranet: The inclusion of your ACS unpublished or published manuscript is permitted in your thesis in print and microfilm formats. If ACS has published your paper you may include the manuscript in your thesis on an intranet that is not publicly available. Your ACS article cannot be posted electronically on a publicly available medium (i.e. one that is not password protected), such as but not limited to, electronic archives, Internet, library server, etc. The only material from your paper that can be posted on a public electronic medium is the article abstract, figures, and tables, and you may link to the article’s DOI or post the article’s author-directed URL link provided by ACS. This paragraph does not pertain to the dissertation distributor paragraph above.

Questions? Call +1 202/872-4368/4367. Send e-mail to copyright@acs.org or fax to +1 202-776-8112. 10/10/03, 01/15/04, 06/07/06

Appendix 2. Copyright Permissions of Acta Crystallographica Journals

If you wish to include material from your own article in a publication, prior permission is not required, subject to the following conditions:

- Reproduction is intended in a primary journal, secondary journal, CD-ROM, book or thesis.

- The original article in which the material appeared is cited.

- IUCr's copyright permission is indicated next to the Figure/Table in print. In electronic form, this acknowledgement must be visible at the same time as the Figure/Table, and must be hyperlinked to Crystallography Journals Online (http://journals.iucr.org/).

Crystallography Journals Online partners and site credits. 
Copyright © International Union of Crystallography

Appendix 3. Physical Properties of the Raw Materials Used in This Thesis.

| Name | Formula | Molecular weight (g/mol) | Density (g/cm3) | Purity (%) | Boiling point (°C) | Melting point (°C) |
| --- | --- | --- | --- | --- | --- | --- |
| Tetramethyl orthosilicate | C4H12O4Si | 152.22 | 1.032 | 98 | 120~122 | -4 |
| Tetraethyl orthosilicate | C8H20O4Si | 208.33 | 0.934 | 98 | 168 | -77 |
| Titanium isopropoxide | C12H28Ti | 284.26 | 0.97 | 97 | 240 | 18-20 |
| Titanium butoxide | C16H36Ti | 340.36 | 1.08 | 97 | 310-314 | -55 |
| Zirconium propoxide | C12H28Zr | 327.58 | 1.058 | 70 | - | - |
| Zirconium butoxide | C16H36Zr | 383.7 | 1.049 | 80 | - | - |
| Aluminum isopropoxide | C9H21Al | 204.24 | 1.035 | 98 | 125-130 | 128-135 |
| Acetic acid | C2H4O2 | 60.05 | 1.06 | 99.7 | 117.9 | 16.6 |
| Formic acid | CH2O2 | 46.03 | 1.21 |  | 100.7 | 8.3 |
| Benzoic acid | C7H6O2 | 122.12 | 1.32 | 99 | 248.9 | 121 |
| Chloroacetic acid | C2H3ClO2 | 94.50 | 1.58 |  | 188 | 61-62 |
| Methanol | CH4O | 32.04 | 0.791 | 99.93 | 64.7 | -98 |
| Ethanol | C2H6O | 46.07 | 0.789 | 99.95 | 78.3 | -114.1 |
| 2-Propanol | C3H8O | 60.10 | 0.785 | 99.5 | 82.4 | -88.5 |
| n-Butanol | C4H10O | 74.12 | 0.81 |  | 117.6 | -89.5 |
| Acetone | C3H6O | 58.08 | 0.786 | 99.5 | 56.2 | -94.3 |

Appendix 4. Powder XRD Analysis Conditions.

Experimental parameters for Bruker D8 Discover diffractometer

| Type of radiation | CuKα1+Kα2 = 1.54184 Å |
| --- | --- |
| Power | 40 kV x 40 mA |
| Type of scan | Coupled |
| Number of frames | 3 (merged) |
| Beam Diameter | 500 µm |
| 2θ range | 4.9° - 93.95° |
| Number of samples analyzed | 6 |

Experimental parameters for Rigaku (Rigaku - Geigerflex CN2029) diffractometer

| Type of radiation | CuKα1+Kα2 = 1.54184 Å |
| --- | --- |
| Power | 40 kV x 35 mA |
| Type of scan | Coupled |
| Step Size | 0.05 |
| Step Time | 2sec |
| 2θ range | 2.0° - 115.0° |
| Number of samples analyzed | 7 |

Appendix 5. N2 Physisorption Analysis Conditions.

Isotherm collection pressure table

|  | Relative Pressure | BET Surf. area | Lang. Surf. Area | t-Plot | BJH Adsorption | BJH Desorption |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.005000000 |  |  |  |  |  |
| 2 | 0.010000000 |  |  | x |  |  |
| 3 | 0.023265306 |  |  |  |  |  |
| 4 | 0.030000000 |  |  | x |  |  |
| 5 | 0.041530612 |  |  |  |  |  |
| 6 | 0.059795918 |  |  |  |  |  |
| 7 | 0.060000000 | x | x | x |  |  |
| 8 | 0.078000000 |  |  |  |  |  |
| 9 | 0.080000000 | x | x | x |  |  |
| 10 | 0.096326531 |  |  |  |  |  |
| 11 | 0.100000000 | x | x | x |  |  |
| 12 | 0.114591837 |  |  |  |  |  |
| 13 | 0.120000000 | x | x | x |  |  |
| 14 | 0.132857143 |  |  |  |  |  |
| 15 | 0.140000000 | x | x | x | x |  |
| 16 | 0.151122449 |  |  |  |  |  |
| 17 | 0.160000000 | x | x | x | x |  |
| 18 | 0.169387755 |  |  |  |  |  |
| 19 | 0.180000000 | x | x | x | x |  |
| 20 | 0.187653061 |  |  |  |  |  |
| 21 | 0.200000000 | x | x | x | x |  |
| 22 | 0.205918367 |  |  |  |  |  |
| 23 | 0.224183673 |  |  |  |  |  |
| 24 | 0.242448980 |  |  |  |  |  |
| 25 | 0.250000000 |  |  | x | x |  |
| 26 | 0.260714286 |  |  |  |  |  |
| 27 | 0.278979592 |  |  |  |  |  |
| 28 | 0.297244898 |  |  |  |  |  |
| 29 | 0.300000000 |  |  | x | x |  |
| 30 | 0.315510204 |  |  |  |  |  |
| 31 | 0.333775510 |  |  |  |  |  |
| 32 | 0.350000000 |  |  | x | x |  |
| 33 | 0.352040816 |  |  |  |  |  |
| 34 | 0.370306122 |  |  |  |  |  |
| 35 | 0.388571429 |  |  |  |  |  |
| 36 | 0.400000000 |  |  | x | x |  |
| 37 | 0.406836735 |  |  |  |  |  |
| 38 | 0.425102041 |  |  |  |  |  |
| 39 | 0.443367347 |  |  |  |  |  |
| 40 | 0.450000000 |  |  | x | x |  |
| 41 | 0.461632653 |  |  |  |  |  |
| 42 | 0.479897959 |  |  |  |  |  |
| 43 | 0.498163265 |  |  |  |  |  |
| 44 | 0.500000000 |  |  | x | x |  |
| 45 | 0.516428571 |  |  |  |  |  |
| 46 | 0.534693878 |  |  |  |  |  |
| 47 | 0.550000000 |  |  | x | x |  |
| 48 | 0.552951984 |  |  |  |  |  |
| 49 | 0.571224490 |  |  |  |  |  |
| 50 | 0.589489796 |  |  |  |  |  |
| 51 | 0.600000000 |  |  | x | x |  |
| 52 | 0.607755102 |  |  |  |  |  |
| 53 | 0.626020408 |  |  |  |  |  |
| 54 | 0.644285714 |  |  |  |  |  |
| 55 | 0.650000000 |  |  | x | x |  |
| 56 | 0.662551020 |  |  |  |  |  |
| 57 | 0.680816327 |  |  |  |  |  |
| 58 | 0.699061633 |  |  |  |  |  |
| 59 | 0.700000000 |  |  |  | x |  |
| 60 | 0.717346939 |  |  |  |  |  |
| 61 | 0.735612245 |  |  |  |  |  |
| 62 | 0.750000000 |  |  |  | x |  |
| 63 | 0.753877551 |  |  |  |  |  |
| 64 | 0.772142857 |  |  |  |  |  |
| 65 | 0.790408163 |  |  |  |  |  |
| 66 | 0.800000000 |  |  |  | x |  |
| 67 | 0.808673469 |  |  |  |  |  |
| 68 | 0.820000000 |  |  |  | x |  |
| 69 | 0.826938776 |  |  |  |  |  |
| 70 | 0.845204082 |  |  |  |  |  |
| 71 | 0.850000000 |  |  |  | x |  |
| 72 | 0.863469388 |  |  |  |  |  |
| 73 | 0.875000000 |  |  |  | x |  |
| 74 | 0.881734694 |  |  |  |  |  |
| 75 | 0.900000000 |  |  |  | x |  |
| 76 | 0.925000000 |  |  |  | x |  |
| 77 | 0.950000000 |  |  |  | x |  |
| 78 | 0.975000000 |  |  |  | x |  |
| 79 | 0.980000000 |  |  |  | x |  |
| 80 | 0.990000000 |  |  |  | x |  |
| 81 | 0.995000000 |  |  |  | x | x |
| 82 | 0.990000000 |  |  |  |  | x |
| 83 | 0.980000000 |  |  |  |  | x |
| 84 | 0.975000000 |  |  |  |  | x |
| 85 | 0.950000000 |  |  |  |  | x |
| 86 | 0.925000000 |  |  |  |  | x |
| 87 | 0.900000000 |  |  |  |  | x |
| 88 | 0.875000000 |  |  |  |  | x |
| 89 | 0.850000000 |  |  |  |  | x |
| 90 | 0.825000000 |  |  |  |  | x |
| 91 | 0.800000000 |  |  |  |  | x |
| 92 | 0.750000000 |  |  |  |  | x |
| 93 | 0.700000000 |  |  |  |  | x |
| 94 | 0.650000000 |  |  |  |  | x |
| 95 | 0.600000000 |  |  |  |  | x |
| 96 | 0.550000000 |  |  |  |  | x |
| 97 | 0.500000000 |  |  |  |  | x |
| 98 | 0.450000000 |  |  |  |  | x |
| 99 | 0.400000000 |  |  |  |  | x |
| 100 | 0.350000000 |  |  |  |  | x |
| 101 | 0.300000000 |  |  |  |  | x |
| 102 | 0.250000000 |  |  |  |  | x |
| 103 | 0.200000000 |  |  |  |  | x |
| 104 | 0.140000000 |  |  |  |  | x |

Collect ROA Data:                                               No

ROA Sample Interval:                                          10.00 secs

ROA Dose Amount:                                              5.00 cm3/g STP

Maximum ROA Samples:                                     100

Target pressure options:

Use first pressure fixed dose:                               No

Use maximum volume increment:                        No

Absolute pressure tolerance:                                 5.000 mmHg

Relative pressure tolerance:                                  5.0%

Low pressure dosing:                                            No

Analysis preparation options:

Fast evacuation:                                                   Yes

Evacuation time:                                                  0 .10 hours

Leak test:                                                              No

Free Space

Free space group:                                                 Measured

Low dewar after free space:                                 Yes

Evacuation time:                                                   0.10 hour

Outgas test:                                                           Yes

Outgas test duration:                                             180 secs

Po and Temperature options:

Po type:                                                                 Measured

Measurement interval:                                          120 minutes

Temperature type:                                                 Entered

Temperature:                                                          77.35 K

Measurement gas:                                                 Nitrogen @ 77.35 K (N2)

Psat Vs. Temperature Table

|  | Saturation Pressure (mmHg) | Temperature (K) |
| --- | --- | --- |
| 1 | 600.193 | 75.40 |
| 2 | 634.512 | 75.85 |
| 3 | 674.383 | 76.35 |
| 4 | 720.420 | 76.90 |
| 5 | 742.119 | 77.15 |
| 6 | 759.833 | 77.35 |
| 7 | 777.867 | 77.55 |
| 8 | 805.525 | 77.85 |
| 9 | 853.268 | 78.35 |
| 10 | 903.122 | 78.85 |

Equilibration options:

Equilibration interval:                                                    5 secs

Min. equil. delay at P/Po ≥ 0.995:                                  600 secs

Sample backfill options:

Backfill at start of analysis:                                            Yes

Backfill at end of analysis:                                              Yes

Backfill Gas:                                                                    Analysis gas

Appendix 6. Block Panel of LabView VI’s.

Block panel of pressure control

Appendix 7. Instrumentation and Configuration of the Temperature and Pressure Control

| Port Number | COM1 | COM3 |
| --- | --- | --- |
| Port Type | 9 pins 232 serial port | 9 pins 232 serial port |
| Baud Rate | 9600 | 115200 |
| Network Interface | - | FieldPoint FP-1000 |
| I/O Modual | - | FP-TB-100 | FP-TC-120 |
| Channel 10 | - | Temperature control analog output (0.004-0.2 mA) | Thermocouple input |
| Channel 11 | - | Pressure control analog output (0.004-0.2 mA) | Thermocouple input |
| Channel 12 | - | Pressure transducer analog signal input (0-100 mV) | - |

Appendix 8. Synthesis and Characterization of the Ti-Acetate Single Crystals

The information in this section is reproduced from a report by the author: Hexakis(μ-acetato-κ 2O,O') hexaisopropoxyhexa -μ 3-oxo-hexatitanium, with permission from Acta Crystallographica Section E, (2006), 2, m373-375, IUCr's Copyright (http://journals.iucr.org/).

Synthesis of Ti-acetate crystals. 0.273 g of acetic acid (99.7%, Aldrich) and 1 g of titanium isopropoxide (97%, Aldrich) were quickly put in the 10 ml view cell, followed by addition of CO2 (99.99%, BOC Canada) to 6000 psig at 40 ºC under mixing with a magnetic stirrer. The stirring was stopped at reaction time of 8 hours. A light yellow granular crystal was formed after about 7 days and a colorless plate crystal was formed after about 15 days in the view cell. The crystals were washed by 200 ml of CO2 at 6000 psig and 40 ºC with a flow rate of 0.5 ml/min, followed by venting of CO2.

Single Crystal XRD. The single crystal XRD was operated on Nonius KappaCCD X-ray diffractometer. Two types of crystals were produced, yellow blocks and colorless plates. The yellow blocks were found to be the structure Ti6O4(OPri)8(OAc)8 3 (rutilane shape), and the colorless plates to be the structure Ti6O6(OPri)6(OAc)6 2 (hexaprismane shape) (Figure A1).234

Figure A1.  The molecular structure of Ti6O6(OPri)6(OAc)6 (2).234 Ti: green, O: red, and C: grey.

FTIR (KBr, Bruker IFS55, cm-1). Structure 2: 2972 (m), 2933 (m), 2875 (m), 1604 (s), 1543 (s), 1458 (s), 1375 (w), 1361 (w), 1348 (w), 1327 (w), 1165 (m), 1132 (s), 1016 (s), 858 (m), 727 (s), 658 (s), 627 (s), 611 (s).  Structure 3: 2970 (m), 2931 (m), 2866 (w), 1581 (s), 1560 (s), 1452 (s), 1410 (s), 1360 (w), 1338 (w); 1165 (m), 1122 (m); 1018 (m), 991 (m), 951 (w), 852 (w), 835 (w), 800 (s), 692 (m), 660 (s), 633 (s), 615 (s), 592 (m), 542 (m).

1H NMR (chloroform, Inova 400 MHz). Structure 2: δ 7.22 (s), δ 5.07 (sept., JH-H = 6.2 Hz, OCHMe2), δ 1.97 (s, O2CCH3), δ 1.35 (d, JH-H = 6.2 Hz, OCHMe2), δ . 13C NMR (chloroform, 101 MHz): δ 177.9, δ 82.0, δ 77.2, δ 24.9, δ 23.1.

Appendix 9. Description of the SIMPLISMA Modeling

In the system with a pure material, the IR spectrum in the range 600-4000 cm-1 with a scanning step of 1 cm-1 can be written as a matrix with one row and 3401 columns:

Bpure = [b600, b601, b602 … bj…, b3999, b4000]                              (A8.1)

Where, Bpure is the matrix of a pure material IR spectrum, bj denotes the IR absorbance at wavenumber j.

In a reaction system with n components, a set of in situ IR spectra collected at different reaction times can be written as a matrix, D. As D is a function of the concentration and the absorbance (Bpure) of each component, it can be expressed as:

D = C ×B                                              (A8.2)

or:

=  ×

(A8.3)

where D is the known rw matrix transformed from in situ IR spectra, C is the to-be-determined rn matrix representing concentration coefficients, and B is the to-be-determined nw matrix representing n pure component spectra; dij, cij and bij are the element of the matrix D, C and B, respectively, at i-th row and j-th column.286

In the SIMPLISMA method, first, the mean value of dij is calculated from the matrix D using Equation A8.4; then, the standard deviation is calculated using Equation A8.5.

(A8.4)

(A8.5)

Where, dij is the element of the matrix D in the i-th row and j-th column,  is the mean value of dij in the j column of the matrix D,  is the standard deviation of dij, and r is the number of matrix rows (spectra). As there are w columns in matrix D, the calculation using Equation A8.4 results in a mean value matrix M:

Μ = [μ1, μ2, ... μj,…, μw]                                     (A8.6)

Similarly, the calculation using Equation A8.5 results in a standard deviation matrix Σ:

Σ = [σ1, σ 2, ... σ j,…, σ w]                                      (A8.7)

After calculations of matrices Μ and Σ, the “purity”, qj, is calculated as:

(A8.8)

where, α is an empirical parameter called offset, which is added to the mean value in order to suppress the noise in the region where the absorbance is close to zero. Typical values for α range from 1-5 % of the maximum μj for the conventional method; for the second-derivative method as described later, however, α is normally selected as 20 %.276, 287

A pure variable is defined as the wavenumber where only one component contributes to the absorbance in the whole column of matrix D.

The calculation using Equation A8.8 results in a purity matrix Q:

Q = [q1, q2, ... q j,…, q w]                                             (A8.9)

where, Q is the purity matrix.

The first ‘pure variable’ is selected as the wavenumber that has the highest qj value. Then the second pure variable is selected, which is independent of the first variable. Theoretically, totally n independent variables should be select as there are n components. The absorbance of the pure variables from all components in matrix D can be used to calculate matrix C using the linear correlation of Beer-Lambert law. With the known matrices D and C, Matrix B can be calculated with a least-squares method.272, 274, 276, 286

E = ║C ×B - D ║2                                            (A8.10)

where, E is the square of the residual matrix.

If the pure variables do not exist for all components, the conventional SIMPLISMA method described above may fail. To solve this problem, in the revised SIMPLISMA method the raw spectral data were replaced by their second derivatives. In the beginning of this revised method, the conventional SIMPLISMA method was used to calculate matrices C and B; then the calculated matrix B was used to recalculate a new C denoted as C’ using the least square approximation. Thus the matrix C’ provides the second-derivative concentrations. Using matrices D and C’, the second-derivative pure component spectra B’ can be obtained.

Appendix 10. Statistical Results of the SIMPLISMA Modeling

Table A10.1. Statistics results of the SIMPLISMA modeling in the region of 750-1250 cm-1: the IR spectra were collected during the reaction of 0.088 M TEOS reacting with 0.362M HOAc in scCO2, at a reaction time of 0-360 minutes and at 3000 psig and 50 ºC.

| No. | Pure Var. (cm-1) | TSS | TSSR | Coefficient | RRSSQ | RSD | IE | IND | Variance | %C- Variance | %R- Variance |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1108 | 56.8 | 1.61 | 218.26 | 0.03 | 0.1 | 0.02 | 0 | 0.02 | 95.03 | 4.97 |
| 2 | 1062 | 8.9 | - | 62.44 | 0.02 | 0.01 | 0 | 0 | 0.96 | 99.95 | 0.05 |

Note: as one more pure variable is selected, either the component coefficient is negative, or a negative concentration profile is obtained, indicating the new variable being redundant.

Table A10.2. Statistics results of the SIMPLISMA modeling in the region of 1400-1650 cm-1: the IR spectra were collected during the reaction of 1.10 M TIP reacting with 6.05 M HOAc in scCO2, at reaction time of 10-610 minutes and at 4500 psig and 60 ºC.

| No. | Pure Var. (cm-1) | TSS | TSSR | Coefficient | RRSSQ | RSD | IE | IND | Variance | %C- Variance | %R- Variance |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1603 | 37.9 | 2.64 | 51.71 | 0.41 | 0.20 | 0.05 | 0.00 | 0.16 | 94.23 | 5.77 |
| 2 | 1555 | 1.86 | - | 73.33 | 0.03 | 0.03 | 0.01 | 0.00 | 0.73 | 99.88 | 0.12 |

Note: as one more pure variable is selected, either the component coefficient is negative, or a negative concentration profile is obtained, indicating the new variable being redundant.

Table A10.2. Statistics results of the SIMPLISMA modeling in the region of 1300-1650 cm-1: the IR spectra were collected during the reaction of 0.547 M ZBO reacting with 1.76 M HOAc in scCO2, at reaction time of 10-3720 minutes and at 4500 psig and 40 ºC.

| No. | Pure Var. (cm-1) | TSS | TSSR | Coefficient | RRSSQ | RSD | IE | IND | Variance | %C- Variance | %R- Variance |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1565 | 8.47 | 11.8 | 123.9 | 0.05 | 0.02 | 0.00 | 0.00 | 0.75 | 99.87 | 0.13 |
| 2 | 1480 | 0.42 | - | 46.2 | 0.01 | 0.00 | 0.00 | 0.00 | 0.21 | 99.99 | 0.01 |

Note: as one more pure variable is selected, either the component coefficient is negative, or a negative concentration profile is obtained, indicating the new variable being redundant.

Statistics Table Notes:

No.: ordinal number of the component (pure variable).

Pure Var units: displays the pure variables.

TSS: total sum integral intensity of the purity-corrected standard deviation spectrum corresponding to pure variable. TSS indicates the percent amount of residual variance (unaccounted information) in the data. The initial sum of standard deviations (before the first pure variable effect was removed) is taken as 100%. For the first (significant) n components it rapidly decreases and then shows saturation at values close to zero, as the n approaches the actual size of the model.

TSSR:	relative TSS. Ratio of TSS of the current component to TSS of the next one.

Coefficient:	SIMPLISMA component coefficient. Component share in the total spectral intensity (TSI, plot of integral intensities of the raw spectral Vs their numbers in series) approximation. A negative value of the coefficient for any of currently accepted n is a strong indication of improperly chosen number of components (insufficient or excessive).

RRSSQ: square root of the sum-of-squares difference between TSI and LSQ (residual sum of squares) divided by the square root of the sum of squares of the TSI. Thus, RRSSQ is a relative RSSQ and varies between 0 and 1. RRSSQ shows saturation after the actual number of components.

RSD: residual standard deviation. The standard deviation of the residual matrix versus the component number.

IE: imbedded error.

IND: indicator function. The IND value exhibits a minimum at a proper n.

Variance: variance in the data modeled by a single component.

%C-Variance:	cumulative %variance. Percent data variance explained by the model.

%R-Variance:	residual %variance. Percent variance not explained by the model. %R-Variance gets saturated after n exceeding the internal dimensionality of the data.

Appendix 11. Calculation of Solubility Parameters Using Group Contribution Method

- Calculation of Ti’s group contributions of Δe(Ti) and Δυ (Ti).

Δe(Ti):

Using the data of Ti(OPri)4 in Table 8.1,

=17×1000 cal/mol − 1.987(cal/mol.K) ×298 K = 16.41 kcal/mol

(A10.1)

Using the data in Table 8.2, for Ti(OPri)4:

∑Δei = Δe(Ti) + 4×Δe(O) + 4×Δe(CH) + 8×Δe(CH3) = Δe(Ti) + 4×800 cal/mol + 4×820 cal/mol + 8×1125 cal/mol = Δe(Ti) + 15.48 kcal/mol.                                                           (A10.2)

Since = ∑Δei,                                                                                                    (A10.3)

Δe(Ti) = 16.41(1.6) kcal/mol −15.48 kcal/mol = 0.9 kcal/mol.                              (A10.4)

Similarly, using the data of Ti(OBun)4 in Table 8.1 and Table 8.2,

Δe(Ti)΄ denotes the energy of vaporization calculated from Ti(OBun)4 and can be calculated as:

=22 ×1000 cal/mol − 1.987(cal/mol.K) ×298 K = 21.41 kcal/mol = ∑Δei = Δe(Ti)΄+ 4×Δe(O) + 12×Δe(CH2) + 4×Δe(CH3) = Δe(Ti)΄+ 4×800 cal/mol + 12×1180 cal/mol + 4×1125 cal/mol = Δe(Ti)΄ + 21.86 kcal/mol,                                                                           (A10.5)

and Δe(Ti)΄ = 0.1 kcal/mol.                                                                                         (A10.6)

Thus,  the average Δe(Ti) = (Δe(Ti) + Δe(Ti)΄)/2 = 0.5 kcal/mol                                   (A10.7)

Δυ (Ti):

Using the data of Ti(OPri)4 in Table 8.1 and Table 8.2,

∑Δυi = 296 cm3/mol = Δυ (Ti) + 4×Δυ (O) + 4×Δυ (CH) + 8×Δυ (CH3) = Δυ (Ti) + 4×3.8 cm3/mol + 4× (-1) cm3/mol (CH) + 8× 33.5 cm3/mol = Δυ (Ti) + 279                         (A10.8)

So, Δυ (Ti) = 16.8 cm3/mol.                                                                                        (A10.9)

Using the data of Ti(OBun)4 in Table 8.1 and Table 8.2,

∑Δυi΄= 340 cm3/mol = Δυ (Ti)΄+ 4×Δυ (O) + 12×Δυ (CH2) + 4×Δυ (CH3) = Δυ (Ti)΄+ 4×3.8 cm3/mol + 12×16.1 cm3/mol + 4×33.5 cm3/mol = Δυ (Ti)΄+ 342.4 cm3/mol.          (A10.10)

So, Δυ (Ti)΄= -2.4 cm3/mol.                                                                                      (A10.11)

Thus, the average of Ti’s mole volume is:

= 7.2 cm3/mol.                                                                                                (A10.12)

- Calculation of the solubility parameter of the macromolecule with a repeating unit of -(Ti6O12(OAc)6)-

For the repeating unit -(Ti6O12(OAc)6)-,

Δeir = 6×Δe(Ti) + 12×Δe(O) + 6×Δe(COO) + 6×Δe(CH3) = 6×0.5 ×1000 cal/mol + 12×800 cal/mol + 6×4300 cal/mol + 6×1125 cal/mol = 45.2 ×1000 cal/mol.                    (A10.13)

Δυir = 6×Δυ (Ti) + 12×Δυ (O) + 6×Δυ (COO) + 6×Δυ (CH3) = 6×7.2 cm3/mol + 12×3.8 cm3/mol + 6×18 cm3/mol + 6×33.5 cm3/mol = 397.8 cm3/mol.                                           (A10.14)

= [45.2 ×1000 cal/mol /397.8 cm3/mol]0.5 = 10.7 cal0.5cm-1.5.        (A10.15)

Curriculum Vitae

| Name Post-secondary Education and Degrees: Honors and Awards: Related Work Experience: | Ruohong Sui Heilongjiang University Harbin, Heilongjiang, P.R. China 1980-1984 B.Sc. The University of Western Ontario London, Ontario, Canada 2002-2007 Province of Ontario Graduate Scholarship 2005-2006 Western Engineering Graduate Thesis Research Awards 2005-2006 Teacher Harbin Chemical Industrial School, Harbin, P.R. China 1984-1988 Deputy General Engineer Leidi Sci. & Tech. Enterprise, Ltd., Shenzhen, P.R. China 1994-1997 Chemical Engineer Ginkgo Biological Group Company, Beijing, P.R. China 1998-2000 |
| --- | --- |

Publications:

(1) Sui, R.; Rizkalla, A. S; Charpentier, P. A.  Kinetics Study on Direct Sol-Gel Reactions in ScCO2 by Using In Situ ATR-FTIR. In preparation

(2) Sui, R.; Rizkalla, A. S; Charpentier, P. A.  Stabilization of the Colloidal Particles in ScCO2. In preparation

(3) Sui, R.; Liu, S.; Lajoie, G. A; Rizkalla, A. S; Charpentier, P. A.  Synthesis of TiO2 Monolithic Aerogel in the Liquid Chromatography Columns in scCO2. In preparation

(4) Khaled, S. M.; Sui, R.; Rizkalla, A. S.; Charpentier, P. A. Synthesis of Titanate Nanotubes from Amorphous Aerogels in Aqueous KOH. In preparation

(5) Lucky, R.; Sui, R.; Charpentier, P. A.; Jennings, M. C. Synthesis of Ti-Zr-Acetate Complex in Supercritical CO2. In preparation

(6) Hojjati, B.; Sui, R.; Charpentier, P. A. Synthesis of TiO2/PAA Nanocomposite by RAFT Polymerization. Polymer (Under revision)

(7) Khaled, S. M.; Sui, R.; Rizkalla, A. S.; Charpentier, P. A. (2007) Synthesis of TiO2-PMMA Nanocomposite: Using Methacrylic Acid as a Coupling Agent. Langmuir 23 (7) 3988-3995

(8) Sui, R.; Rizkalla, A. S.; Charpentier, P. A. (2006) FTIR Study on Formation of TiO2 Nanostructures in Supercritical CO2. J. Phys. Chem. B. 110 (33) 16212-16218.

(9) Sui, R.; Rizkalla, A. S; Charpentier, P. A.  (2006) Direct Synthesis of Zirconia Aerogel Nanoarchitecture in Supercritical CO2. Langmuir 22 (9) 4390-4396.

(10) Sui, R.; Charpentier, P. A; Rizkalla, A. S; Jennings, M. C, (2006) Hexakis ( -acetato- 2O,O') hexaisopropoxyhexa- 3-oxo-hexatitanium. Acta Crystallographica E62 (2) m373-m375.

(11) Sui, R.; Rizkalla, A. S; Charpentier, P. A.  (2005) Formation of Titania Nanofibers: A Direct Sol-Gel Route in Supercritical CO2, Langmuir 21 (14) 6150-6153.

(12) Sui, R.; Rizkalla, A. S; Charpentier, P. A.  (2004) Synthesis and Formation of Silica Aerogel Particles by a Novel Sol-Gel Route in Supercritical Carbon Dioxide.    J. Phys. Chem. B. 108 (32), 11886-11892.

Conference Proceedings:

(1) Sui, R.; Rizkalla, A. S; Charpentier, P. A.  (2005) Synthesis of Metal Oxide Nanoaerogels via a Sol-Gel Route in Supercritical CO2.    AIChE Annual Meeting, Cincinnati, OH.

(2) Sui, R.; Rizkalla, A. S.; Charpentier, P. A. (2005) Synthesis and Characterization of Titania and Zirconia Aerogel via a Novel Sol-Gel Route in Supercritical Carbon Dioxide. International Symposium on Supercritical Fluids, Orlando, FL.

(3) Sui, R.; Li, X.; Rizkalla, A. S; Charpentier, P. A.  (2004) Synthesis of Silica Aerogel Particles and Polyethylene Nanocomposites by a Novel Sol-Gel Route in Supercritical Carbon Dioxide. 227th ACS National Meeting, Anaheim, CA.

(4) Sui, R.; Rizkalla, A. S.; Charpentier, P. A.  (2003) Particle Synthesis and Composite Formation Utilizing Supercritical CO2. The 53rd CSChE Conference, Hamilton, ON.

# Text boxes

Metal alkoxide

+ alcohol + stabilization agent

Calcination

Supercritical

extraction

Aging

Condensation

Hydrolysis

Water + acid (or NH3)

+ alcohol